Supporting Information

Direct Decoration of Polystyrene by Diazonium Salt

Huynh Quoc Thang

Department of Chemical Engineering, Pohang University of Science and Technology, 77 Cheongam-ro, Nam-gu, Pohang-si, Gyeongsangbuk-do (37673)

Email: quocthangdr@gmail.com
General Considerations.

Chemical reagents obtained from commercial sources (Aldrich, Alfa Aesar, TCI and Acros) were used without further purification

Measurements. 1H-NMR spectra were obtained on a 400 MHz Bruker Avance III HD Fourier transform NMR spectrometer and referenced to the residual protonated solvent. Gel permeation chromatography (GPC) analyses with refractive index (RI) detection were used to determine the number-average molecular weights (Mn), weight-average molecular weights (Mw), and polydispersities (Mw/Mn). The RI measurements were carried out using an instrument composed of a Waters 1515 isocratic pump, a 2414 differential refractive index detector, and a column-heating module with Shodex KF-804, KF-803, and KF-802.5 columns in series. The columns were eluted with tetrahydrofuran (preservative-free HPLC grade, Fisher or Daejung Chemical Company) at 40 B and 1.0 mL/min and calibrated using 14 monodisperse polystyrene standards (purchased from Alfa Aesar). Infrared spectra were obtained on a Bruker Alpha Fourier transform IR spectrometer equipped with ATR module.

All lamps were purchased from this website:  http://www.hijungu.com/shop/main/index.php

UV lamp, http://www.hijungu.com/shop/goods/goods_view.php?goodsno=3242&category=001008012#detail01 (20W, 353nm).

Spectra Collection