Supporting Information

Modulation of spin dynamics in Ni/Pb(Mg1/3Nb2/3)O3-PbTiO3 multiferroic heterostructure

Hang XU, a,b Bo WANG, a Ji QI, a,b Mei LIU, a Fei TENG, *,a,c, Linglong HU, a Yuan ZHANG, a Chaoqun QU, *,a Ming FENG *,a

a Key Laboratory of Functional Materials Physics and Chemistry of the Ministry of Education, Jilin Normal University, Changchun 130103, P.R. China

b Condensed Matter Science and Technology Institute, School of Instrumentation Science and Engineering, Harbin Institute of Technology, Harbin 150080, P.R. China

c College of Mathematics, Jilin Normal University, Siping 136000, P.R. China

Under a cyclic E-field of ±6.7 kV/cm, we obtained FMR spectra of Ni/PMN-PT at the angles of 0°, 45° and 90° between H-field and heterostructure plane. Fig. S1 presents the in-plane FMR spectra of Ni/PMN-PT heterostructure while applied E-field to the PMN-PT substrate. The measured shift of FMR field (Hr) is ca. 350 Oe when the PMN-PT under the E-field from 0 kV/cm to +6.7 kV/cm as shown in Fig. S1a, the Hr is ca. 280 Oe when the PMN-PT under the E-field from +6.7 kV/cm to +2.7 kV/cm as shown in Fig. S1b, and the Hr is ca. 250 Oe when the PMN-PT under the E-field from 0 kV/cm to –6.7 kV/cm as shown in Fig. S1c.

Fig. S1 In-plane E-field dependence of FMR spectra of Ni/PMN-PT multiferroic heterostructure while applied E-field to the PMN-PT substrate.

Fig. S2 shows the FMR spectra of Ni/PMN-PT heterostructure at the angles of 45° between H-field and heterostructure plane while applied E-field to the PMN-PT substrate. The Hr is ca. 300 Oe when the PMN-PT under the E-field from 0 kV/cm to +6.7 kV/cm as shown in Fig. S2a, the Hr is ca. 130 Oe when the PMN-PT under the E-field from +6.7 kV/cm to +2.7 kV/cm as shown in Fig. S2b, and the Hr is ca. 350 Oe when the PMN-PT under the E-field from 0 kV/cm to –6.7 kV/cm as shown in Fig. S2c.

Fig. S2 The FMR spectra of Ni/PMN-PT multiferroic heterostructure at the angles of 45° between H-field and heterostructure plane while applied E-field to the PMN-PT substrate.

Fig. S3 presents the out-of-plane FMR spectra of Ni/PMN-PT heterostructure while applied E-field to the PMN-PT substrate. The Hr is ca. 150 Oe when the PMN-PT under the E-field from 0 kV/cm to +6.7 kV/cm as shown in Fig. S3a, and the Hr is ca. –130 Oe when the PMN-PT under the E-field from +6.7 kV/cm to 0 kV/cm as shown in Fig. S3b. The Hr is ca. 130 Oe when the PMN-PT under the E-field from 0 kV/cm to –6.7 kV/cm as shown in Fig. S3c.

Fig. S3 Out-of-plane E-field dependence of FMR spectra of Ni/PMN-PT multiferroic heterostructure while applied E-field to the PMN-PT substrate.