Table S1 | Indexing of the peaks identified on the alkaline vents analogues’ diffractograms (1h, 5h, 24h, 48h, 72h, 96h and 10d). For each phase, peaks are labelled with chloride green rust (PDF4 ID: 00-040-0127 / noted Cl – green rust), carbonated green rust (PDF4 ID: 00-052-0163), magnetite (PDF4 ID: 01-076-1849), amakinite (COD ID: 00-900-9104), halite (PDF4 ID: 00-005-0628) and iron (PDF4 ID: 01-087-0722).

| 5h |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 4.86 | 4655 | [1 1 1] 4.8497 Magnétite |
| 2.97 | 3927 | [2 2 0] 2.9698 Magnétite |
| 2.82 | 13453 | [2 0 0] 2.8210 Halite |
| 2.53 | 5677 | [3 1 1] 2.53270 Magnétite |
| 2.10 | 3140 | [4 0 0] 2.1000 Magnétite |
| 1.99 | 3155 | [2 2 0] 1.9940 Halite |
| 1.61 | 2787 | [5 1 1] 1.6166 Magnétite |
| 1.48 | 2920 | [4 4 0] 1.4849 Magnétite |

| 24h |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 7.82 | 8494 | [0 0 3] 7.9300 Cl - Green Rust |
| 4.86 | 6681 | [1 1 1] 4.8497 Magnétite |
| 3.90 | 5054 | [0 0 6] 3.9700 Cl - Green Rust |
| 3.26 | 4295 | [1 1 1] 3.2600 Halite |
| 2.96 | 6335 | [2 2 0] 2.9698 Magnétite |
| 2.83 | 4788 | [2 0 0] 2.8210 Halite |
| 2.69 | 4116 | [0 1 2] 2.7100 Green Rust |
| 2.53 | 11314 | [3 1 1] 2.5327 Magnétite |
| 2.10 | 4693 | [4 0 0] 2.1000 Magnétite |
| 1.99 | 3435 | [2 2 0] 1.9940 Halite |
| 1.72 | 3083 | [4 2 2] 1.7146 Magnétite |
| 1.62 | 3698 | [5 1 1] 1.6166 Magnétite |
| 1.49 | 3874 | [4 4 0] 1.4849 Magnétite |

| 48h |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 7.59 | 26045 | [0 0 3] 7.4970 CO3 - Green Rust |
| 4.85 | 18783 | [1 1 1] 4.8497 Magnétite |
| 4.62 | 15664 | [0 0 1] 4.6050 Amakinite |
| 3.79 | 14960 | [0 0 6] 3.7530 CO3 - Green Rust |
| 2.97 | 22705 | [2 2 0] 2.9698 Magnétite |
| 2.82 | 13954 | [1 0 0] 2.8215 Amakinite |
| 2.68 | 14909 | [0 1 2] 2.6980 CO3 - Green Rust |
| 2.53 | 51806 | [3 1 1] 2.5327 Magnétite |
| 2.41 | 14876 | [1 0 -1] 2.4058 Amakinite |
| 2.35 | 13141 | [0 1 5] 2.3470 CO3 - Green Rust |
| 2.10 | 20600 | [4 0 0] 2.1000 Magnétite |
| 2.03 | 11291 | [1 1 0] 2.0229 Iron |
| 1.99 | 11209 | [2 2 0] 1.9940 Halite |
| 1.97 | 11638 | [0 1 8] 1.9650 CO3 - Green Rust |
| 1.78 | 11407 | [1 0 -2] 1.7839 Amakinite |
| 1.72 | 12910 | 4 2 2] 1.7146 Magnétite |
| 1.62 | 17850 | [5 1 1] 1.6166 Magnétite |
| 1.49 | 20363 | [4 4 0] 1.4849 Magnétite |

| 72h |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 7.60 | 9781 | [0 0 3] 7.4970 CO3 - Green Rust |
| 4.87 | 7142 | [1 1 1] 4.8497 Magnétite |
| 4.61 | 6937 | [0 0 1] 4.6050 Amakinite |
| 4.19 | 5426 |  |
| 3.80 | 5477 | [0 0 6] 3.75300 CO3 - Green Rust |
| 2.97 | 7749 | [2 2 0] 2.9698 Magnétite |
| 2.82 | 5495 | [1 0 0] 2.8215 Amakinite |
| 2.67 | 5016 | [0 1 2] 2.6730 CO3 - Green Rust |
| 2.53 | 15730 | [3 1 1] 2.5327 Magnétite |
| 2.41 | 5856 | [1 0 -1] 2.4058 Amakinite |
| 2.35 | 4430 | [0 1 5] 2.3470 CO3 - Green Rust |
| 2.10 | 6341 | [4 0 0] 2.1000 Magnétite |
| 2.03 | 4369 | [1 1 0] 2.0229 Iron |
| 1.97 | 3877 | [0 1 5] 1.9650 CO3 - Green Rust |
| 1.78 | 3877 | [1 0 -2] 1.7839 Amakinite |
| 1.72 | 4174 | [4 2 2] 1.7146 Magnétite |
| 1.63 | 3940 | [2 -1 0] 1.6290 Amakinite |
| 1.62 | 5203 | [5 1 1] 1.6166 Magnétite |
| 1.55 | 3605 |  |
| 1.54 | 3534 |  |
| 1.49 | 5801 | [4 4 0] 1.4849 Magnétite |

| 96h |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 7.59 | 9290 | [0 0 3] 7.4970 CO3 - Green Rust |
| 4.85 | 8430 | [1 1 1] 4.8497 Magnétite |
| 4.59 | 7880 | [0 0 1] 4.6050 Amakinite |
| 3.79 | 5830 | [0 0 6] 3.7530 CO3 - Green Rust |
| 2.97 | 9391 | [2 2 0] 2.9698 Magnétite |
| 2.82 | 6262 | [1 0 0] 2.8215 Amakinite |
| 2.68 | 5480 | [0 1 2] 2.6730 CO3 - Green Rust |
| 2.53 | 18543 | [3 1 1] 2.5327 Magnétite |
| 2.41 | 6660 | [1 0 -1] 2.4058 Amakinite |
| 2.35 | 4825 | [0 1 5] 2.3470 CO3 - Green Rust |
| 2.10 | 7290 | [4 0 0] 2.1000 Magnétite |
| 2.03 | 4970 | [1 1 0] 2.0229 Iron |
| 1.78 | 4396 | [1 0 -2] 1.7839 Amakinite |
| 1.71 | 4591 | [4 2 2] 1.7146 Magnétite |
| 1.63 | 4435 | [2 -1 0] 1.6290 Amakinite |
| 1.62 | 5870 | [5 1 1] 1.6166 Magnétite |
| 1.49 | 6540 | [4 4 0] 1.4849 Magnétite |

| 10d |  |  |
| --- | --- | --- |
| d-spacing (Å) | Relative intensity (I %) | h k l |
| 7.58 | 10520 | [0 0 3] 7.4970 CO3 - Green Rust |
| 4.85 | 6230 | [1 1 1] 4.8497 Magnétite |
| 4.60 | 6185 | [0 0 1] 4.6050 Amakinite |
| 3.95 | 4840 |  |
| 3.79 | 5080 | [0 0 6] 3.7530 CO3 - Green Rust |
| 2.97 | 5583 | [2 2 0] 2.9698 Magnétite |
| 2.82 | 4030 | [1 0 0] 2.8215 Amakinite |
| 2.67 | 4100 | [0 1 2] 2.6730 CO3 - Green Rust |
| 2.53 | 9323 | [3 1 1] 2.5327 Magnétite |
| 2.41 | 4130 | [1 0 -1] 2.4058 Amakinite |
| 2.35 | 3576 | [0 1 5] 2.3470 CO3 - Green Rust |
| 2.10 | 4155 | [4 0 0] 2.1000 Magnétite |
| 2.03 | 3360 | [1 1 0] 2.0229 Iron |
| 1.97 | 3050 | [0 1 5] 1.9650 CO3 - Green Rust |
| 1.78 | 2852 | [1 0 -2] 1.7839 Amakinite |
| 1.72 | 2852 | [4 2 2] 1.7146 Magnétite |
| 1.62 | 3437 | [2 -1 0] 1.6290 Amakinite |
| 1.59 | 2661 | [5 1 1] 1.6166 Magnétite |
| 1.49 | 3483 | [4 4 0] 1.4849 Magnétite |

Figure S2 | Evolution of the blue area, i.e. the contact with de dialysis membrane (bottom black area on the images). In the course of time, the area does not significantly evolve.

Figure S3 | Evolution of the cyan area, i.e. the extension of the contact area with the dialysis membrane. In the course of time, the area does not significantly evolve, except for a better structuring of the laminae and an increase in the grain size of the magnetite.

Figure S4 | TEM observation of the FIB section. The blue highlights a zone of high porosity, which we interpret as the zone of Fe(OH)2 oxidation producing Fe3O4 and H2.The red highlights the zone of Fe2+ disproportionation (from Fe(OH)2) into Fe3+ (Fe3O4) and Fe0.