| S.no | Peak Position (cm⁻¹) | Vibrational Mode | Functional Group |
| --- | --- | --- | --- |
|  | 3279.3 | O–H stretching | Alcohols, phenols |
|  | 2922.7 | C–H stretching | Alkanes |
|  | 1562.1 | C=C or N–H bending | Aromatic ring / Amides |
|  | 1316.8 | P=O or C–N stretching | Phosphates / Amines |
|  | 1152.5 | C–O–C stretching | Ethers / Polysaccharides (chitosan) |
|  | 1018.4 | C–O stretching | Alcohols / Ethers |
|  | 823.7 | Zn–O stretching | Zinc oxide nanoparticles |
|  | 656.8 | Zn–O bending/stretching | Zinc oxide nanoparticles |
|  | 611.27 | Zn–O bending/stretching | Zinc oxide nanoparticles |

Table 1 FTIR peak assignments indicating functional groups present in the B. purpurea leaf extract-based chitosan-ZnO nanocomposite.