[image: image1.emf] 
Figure S1: The stability of Ag@PEG NPs also checked for 5 moth old NPs solution (stored at RT) using DLS and Zeta potential techniques and found no significant detonation of the stability of NPs. Figure shows the hydro-dynamic size by dynamic light scattering (DLS) and zeta potential determination of Ag@ PEG-NPs after synthesis and after 5 months. Here, A: The average particle size of Ag@PEG after synthesis had a Z average diameter of 58.89± 16 nm; B: The average particle size of Ag@PEG after 5 months of synthesis had a Z average diameter of 62.75± 21 nm. C: Ag@PEG after synthesis showed the zeta potential was −4.08 mV; D: Ag@PEG after 5 months of synthesis showed the zeta potential was -5.15mV.
B





A





C





D








[image: image2.emf][image: image3.emf][image: image4.emf]