Table1 Adsorption isotherm model and parameters.

| Isotherm models | Equation | Parameter |
| --- | --- | --- |
| Langmuir | qeQ0=K1Ce1+K1Ce | Q0(mg/g) is the maximum adsorption capacity K1 is the adsorption constant |
| Freundlich | Inqe=InK2+1nInCe | K2 and n are adsorption constants, which are obtained by data fitting |
| Temkin | qe=BInCe+A | A and B are constants |

Table2 Kinetic model and parameters.

| Kinetic models | Equation | Parameter |
| --- | --- | --- |
| Pseudo-first order | Inqe-qt=Inqe-Kft | Kf(min-1) is the adsorption rate constant |
| Pseudo-second order | tqt=1Ksqe2+tqt | Ks(mg·g-1·min-1) is the adsorption rate constant |
| Intragranular diffusion | qt=Kdift+C | Kdif (mg·g-1·min1/2) is the internal diffusion rate constant |

Table 3. Catalytic kinetic parameters of three materials.

| Kinetic model | Catalyst | K | R2 |
| --- | --- | --- | --- |
| Pseudo-first order | 0.13g-TiO2/Ti3+/AC | 0.00895 | 0.99437 |
|  | 0.13g-TiO2/Ti3+ | 0.00245 | 0.94220 |
|  | AC | 0.00012 | 0.90826 |
| Pseudo-second order | 0.13g-TiO2/Ti3+/AC | 0.00729 | 0.95066 |
|  | 0.13g-TiO2/Ti3+ | 0.00635 | 0.88655 |
|  | AC | 0.14703 | 0.84680 |

Table 4 Comparison of the removal rate of Rh-B by TiO2 composite.

| Sample | Dose(g) | Dye volume (ml） | concentration (mg/L) | Degradation rate (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| TiO2/Ti3+/AC | 0.1 | 200 | 150 | 96.17 | this work |
| TiO2/GC | 0.1 | 180 | 75 | >70 | [71] |
| TiO2/GRO | 0.02 | 80 | 10 | 88.8 | [72] |
| TiO2/DME | 0.05 | 100 | 10 | 96 | [73] |
| TiO2/SCA-16 | 0.005 | 10 | 5 | 97 | [74] |

Table5 Adsorption isotherm parameters at 303~323K.

| Adsorption isotherm model | Parameter | Temperature（K） |  |  |
| --- | --- | --- | --- | --- |
|  |  | 303 | 313 | 323 |
| Langmuir | qmax | 233.309 | 237.774 | 244.375 |
|  | Q0 | 239.02591 | 242.33450 | 250.93024 |
|  | K1 | 0.52549 | 0.59704 | 0.65847 |
|  | R2 | 0.98769 | 0.96587 | 0.98619 |
| Freundlich | 1/n | 0.20895 | 0.21141 | 0.21793 |
|  | K2 | 108.961 | 111.9129 | 116.5601 |
|  | R2 | 0.83836 | 0.86801 | 0.85150 |
| Temkin | R2 | 0.90775 | 0.92225 | 0.91371 |

Table6 Adsorption kinetics parameters at 283K.

| Kinetic model | C0(mg/L) | qe, cal (mg/g) | qe, exp(mg/g) | K | R2 |
| --- | --- | --- | --- | --- | --- |
| Pseudo-first-order | 50 | 98.9182 | 99.170 | 0.02230 | 0.96485 |
|  | 100 | 151.1226 | 159.003 | 0.00647 | 0.87118 |
|  | 150 | 157.7699 | 169.968 | 0.00287 | 0.78239 |
|  | 200 | 161.6723 | 175.322 | 0.00180 | 0.7255 |
| Pseudo-second-order | 50 | 98.9182 | 100.085 | 0.00920 | 0.99821 |
|  | 100 | 151.1226 | 155.509 | 0.00520 | 0.99221 |
|  | 150 | 157.7699 | 162.407 | 0.00510 | 0.99096 |
|  | 200 | 161.6723 | 165.755 | 0.00510 | 0.99041 |
| Intragranular diffusion | 50 | 98.9182 | 105.266 | 6.24061 | 0.77157 |
|  | 100 | 151.1226 | 164.008 | 15.37255 | 0.89601 |
|  | 150 | 157.7699 | 172.132 | 15.37576 | 0.85343 |
|  | 200 | 161.6723 | 175.992 | 14.99806 | 0.81998 |

Table7 Adsorption kinetics of 150mg/L at 283K.

| Kinetic model | Adsorbent | qe, cal (mg/g) | qe, exp(mg/g) | K | R2 |
| --- | --- | --- | --- | --- | --- |
| Pseudo-first-order | 0.13g-TiO2/Ti3+AC | 157.7699 | 169.968 | 0.00287 | 0.78239 |
|  | 0.13g-TiO2/Ti3+ | 6.0166 | 6.415 | 0.00008 | 0.93183 |
|  | AC | 115.466 | 123.473 | 0.00206 | 0.89549 |
| Pseudo-second-order | 0.13g-TiO2/Ti3+AC | 157.7699 | 162.407 | 0.0051 | 0.99096 |
|  | 0.13g-TiO2/Ti3+ | 6.0166 | 6.000 | 0.11394 | 0.99452 |
|  | AC | 115.466 | 117.316 | 0.00626 | 0.99630 |
| Intragranular diffusion | 0.13g-TiO2/Ti3+/AC | 157.7699 | 172.132 | 15.37576 | 0.85343 |
|  | 0.13g-TiO2/Ti3+ | 6.0166 | 6.226 | 0.70905 | 0.98407 |
|  | AC | 115.466 | 122.845 | 13.10587 | 0.94808 |