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[bookmark: _GoBack]The morphology of the prepared PCL membrane was analyzed from images obtained by a scanning electron microscope (SEM) (Vega S3B EasyProbe, Tescan Orsay Holding a.s., Czech Republic). The average fiber diameter was counted from 300 measurements using ImageJ software (v.1.54k). The PCL membrane was produced with an average fiber diameter 1.33 ± 0.93 µm. The average areal weight of material was 40 g/m2. 
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Fig. S1.: Representative SEM picture and the corresponding histogram of fiber diameter distributions; scale bar = 10 μm. 
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