Supporting Information

Formation Mechanism of Well-ordered Densely Packed Nanoparticle Superlattices Deposited from Gas Phase on Template-free Surfaces

Chang Liu1,2, Fei Liu1,2, Chen Jin1,2, Sishi Zhang2, Lianhua Zhang1, Min Han*1,2

1National Laboratory of Solid State Microstructures and Collaborative Innovation Centre of Advanced Microstructures, Nanjing University, Nanjing 210093, China

2Department of Materials Science and Engineering and Jiangsu Key Laboratory of Artificial Functional Materials, Nanjing University, Nanjing 210093, China

*Correponding author

E-mail address: sjhanmin@nju.edu.cn.

Size distribution of Fe nanoparticles

The size distribution of the deposited nanoparticles is determined from the TEM image based on a statistical analysis using a minimum of 300 nanoparticles.  Histograms of the sizes of the Fe nanoparticles in the samples prepared with different deposition rates are shown in Fig. S1. The size distribution can be approximatively fitted with a log-normal function.

Fig. S1. Size distributions of Fe nanoparticles in the samples prepared with different deposition rates (a) 0.1Å∙s−1 (b) 0.3Å∙s−1 (c) 0.5Å∙s−1(d) 0.7Å∙s−1.

- The element distribution of Fe nanoparticle arrays

The Fe nanoparticle arrays are analyzed using Energy Dispersive X-ray spectroscopy (EDX) to confirm the composition of the nanoparticles. Fig. S3a shows a typical High-Angle Annular Dark-Field (HAADF) image of the ordered Fe nanoparticle arrays, on which elemental mapping analysis is carried. Fig. S3b,c show the corresponding EDX elemental mappings of Fe and O, respectively. It is clear that O always presents accompanying with Fe, revealing that the nanoparticles are oxidized. The merged image (Fig. S3d) further approves the mainly overlapping of the two elements.

Fig. S2. HAADF image (a) of the Fe nanoparticle arrays and EDX elemental mapping images of the marked area for Fe element (b) and O element (c) as well as the merge of Fe and O (d).

Oxidation state of Fe nanoparticle arrays

To analyze the oxidation state of the Fe nanoparticle arrays, X-ray Photoelectron Spectroscopy (XPS) was carried out with an ESCALABMK-II spectrometer using a monochromatic Mg Kα source. Fig. S4 shows the photoemission data of the Fe 2p core levels measured from the Fe nanoparticle arrays before and after Ar+ sputtering. Before Ar+ sputtering, the peaks of Fe 2p3/2 and Fe 2p1/2 core levels are mainly contributed by Fe2O3 (with a binding energy of 710.2eV and 723.6eV, respectively). Only very weak peaks related to pure Fe (with a binding energy of 706.3eV for 2p3/2 core level and 719.6eV for 2p1/2 core level) can be decomposed. After Ar+ sputtering, which removes a certain number of atom layers from the nanoparticle surface, photoemissions from pure Fe become the main contributors of the XPS peaks instead, as can be seen from Fig. S4. The result clearly demonstrates the Fe core and Fe oxide shell structure of the nanoparticles.

Fig. S3. XPS Fe 2p core level spectrum of the Fe nanoparticle assembled arrays before and after Ar+ cleaning.