Supplementary Information

One step, In-situ phosphating construction of encapsulated Co2P and Co3(PO4)2 nanoparticles within 3D reticulated carbon for rechargeable Zn-Air batteries

Gang Chen a, Lina Zhou b, c*, Xin Xiong d, Xiaonan Xu b and Yingying Wang e*

a Wuhan SolidLi New Energy Technology Co., Ltd, Wuhan, 430000, P. R. China

b Hubei Key Laboratory of Photoelectric Materials and Devices, College of Material Science and Engineering, Hubei Normal University, Huangshi, 435002, P. R. China

c National Laboratory of Solid State Microstructures, Nanjing University, Nanjing 210093, China

d College of Physics and Electronic Science, Hubei Normal University, Huangshi 435002, China

e School of Automation, Hubei University of Science and Technology, Xianning 437100, China

*Corresponding authors.

E-mail address: zhlina@hbnu.edu.cn (Lina Zhou), wangyy@hbust.edu.cn (Yingying Wang)

Experimental section:

1.1 Materials

Aniline, HCl (37 wt.%), ammonium persulfate ((NH4)2S2O8, APS), phytic acid (70 wt.%), and cobalt nitrate hexahydrate (Co(NO3)2.6H2O) were purchased from Sigma-Aldrich. No further purification was required for any of the chemical reagents.

1.2 Synthesis of CoPO-Co2P@NPC electrocatalysts

The synthesis of polyaniline-phytic acid nanorods can be described as follows: Initial, 100 mL of deionized water, 4 mL of phytic acid, and 16 mL of concentrated HCl (37 wt.%) were mixed together with 1 g of aniline monomer. The mixture was stirred vigorously at 10°C for 5 mins. The polymerization reaction was initiated by dropwise adding of initiator solution (2.45 g of (NH4)2S2O8 dissolved in 50 mL of deionized water), the reaction was lasted for 6 h. In order to get the pANI-PA powder, the resultant dark green powder was filtered, washed with ethanol, and dried at 60°C overnight. For comparison, pure pANI was prepared without the use of phytic acid. As can be shown in Figure S1, the as-fabricated pANI-PA product exhibits a uniform nanorod-like shape throughout its whole surface.

A 20 mL ethanol solution was ultrasonically mixed with 0.2 g of as-prepared pANI-PA nanorods for 30 mins. Afterwards, 0.25 mmol of Co(NO3)2.6H2O was dissolved in the aforementioned solution to produce a uniform mixed phase. The mixture was then dried at 60°C for 12 hours. The obtained dark green powder was subjected to pre-annealing at a temperature of 400°C in N2 atmosphere for 2 h, with a heating rate of 2°C/min. The temperature was then raised to 900°C (at a rate of 5°C/min) and maintained for another 5 hours. The carbon composite derived from the pANI-PA was marked as CoPO-Co2P@NPC.

Without the use of Co(NO3)2.6H2O, NPC was synthesized using the same method.

  - Material characterization

The X-ray diffraction (XRD) analysis was performed utilizing Cu Ka radiation (k = 0.154178 nm) through a Hitachi SmartLab SE X-ray diffractometer. The catalyst morphologies were acquired by the use of scanning electron microscopy (SEM; Zeiss Gemini SEM300) and transmission electron microscopy (TEM; Thermo Fisher Talos F200S). HRTEM measurements were conducted using the Thermo Fisher Talos F200S instrument, accompanied by EDX analysis. The X-ray photoelectron spectra were acquired using the Thermo VG VG MultiLab 2000 instrument, while the differential scanning calorimetry (DSC) examination was conducted utilizing a TA/DSC analyzer (NETZSCH STA 449F5). The Fourier transform infrared (FT-IR) spectra were acquired using a Tensor 27 FT-IR spectrometer. The Raman spectrum was acquired via a HORIBA Evolution Raman Microscope spectrometer, employing an excitation wavelength of 532 nm.

  - Electrochemical measurements

The electrochemical analysis was carried out with the use of a Princeton electrochemical workstation and Pine Instruments Co. Ltd. The electrochemical measurements were performed using a three-electrode system in a 0.1 M potassium hydroxide (KOH) solution. A carbon rod served as the counter electrode, with silver/silver chloride (3 M KCl) serving as the reference. The working electrode was a rotating disc electrode (RDE).

The electrocatalyst ink was made using the following procedure: 4 mg of the as-fabricated catalyst was dispersed in a 15 μL Nafion (5 wt.%) and 300 μL isopropanol solution. The mixture was then ultrasonically mixed for at least an hour to generate a well-dispersed suspension. A small amount (10 μL) of catalyst ink was carefully dropped onto the 5 mm diameter working electrode, with an approximate loading of 0.45 mg cm-2. Cyclic voltammograms (CVs) and linear sweep voltammograms (LSVs) were conducted in the potential range of -1.2 to 0.2 V (against Ag/AgCl) and 0.2 to -1.0 V (versus Ag/AgCl) for the oxygen reduction reaction (ORR). The LSV curves were obtained at different rotational speeds (400, 625, 900, 1225, and 1600 rpm) using a scan rate of 5 mV/s. The measured potential was converted to the reversible hydrogen electrode (RHE) using the Nernst equation: ERHE = EAg/AgCl + 0.197 + 0.059pH. LSV profiles were obtained for the OER reaction with a scan rate of 5 mV/s from 1.2 to 1.8 V versus RHE. The K-L equation (Eqs. 1-2) was employed to calculate the electron transfer number (n) from the RDE measurements:

(1)

(2)

J: the measured current density; Jk: kinetic current density; JL: diffusion-limiting current density; ω: angular velocity (rpm); F: Faraday constant (96500 C mol-1); n: electron transfer number; ν: viscosity of the electrolyte (1.0×10-2 cm2 s-1); Do: diffusion coefficient of O2 in 0.1 M KOH (1.9×10-5 cm2 s-1); Co: bulk concentration of O2 (1.2×10-6mol cm-3).

1.6 Assembly of rechargeable Zn-air batteries (ZABs):

A polished zinc plate (with a purity surpassing 99.99%) is used as the anode in both the liquid Zn-air and the flexible Zn-air batteries. The cathode was a carbon cloth that has been thoughtfully loaded with an electrocatalyst, with a mass loading of 1 mg cm−2. The electrolyte was a solution of 6 M potassium hydroxide (KOH). In addition, the air electrode was constructed by mixing 50 wt.% of Pt/C and 50 wt.% of RuO2 as reference. A metal-air battery has been constructed and its galvano-static discharge and polarization curves were examined at a current density of 5 5 mA cm−2, throughout the voltage range of 1.6 to 0 V.

Figure S1 The SEM images of NPC

Table S1 The structure parameters of catalysts

| Electrocatalyst | SBET a (m2/g) | Vt b (cc/g) |
| --- | --- | --- |
| NPC | 654.7 | 0.69 |
| CoPO-Co2P@NPC | 260.3 | 0.25 |

a SBET: BET specific surface area; b Vt: pore volume at P/Po = 0.995.

Figure S2 The BJH pore size distribution plots of NPC and CoPO-Co2P@NPC.

Table S2 Comparison of ORR catalytic activity of the catalysts in this work with the recently reported catalysts in alkaline solutiona.

| Electrocatalysts | E1/2 (vs. RHE) | Eonset (vs. RHE) | Tafel slope (mV dec-1) | Ref |
| --- | --- | --- | --- | --- |
| CoPO-Co2P@NPC | 0.80 | 0.99 | 81.65 | This work |
| 20% Pt/C | 0.78 | 1.15 | 109.27 | This work |
| Co2P@NCNTs-15 | 0.82 | 0.90 | undefined | 1 |
| Co-NCNTs//CCM | 0.79 | 0.86 | 80 | 2 |
| Co2P/CoP@NPC | 0.77 | undefined | undefined | 3 |
| CoNi-SAs/NC | 0.76 | 0.88 | undefined | 4 |
| Co2P@CNF | 0.803 | 0.91 | 77.1 | 5 |

a All the potentials values above are converted to vs. RHE for comparison. In 0.1 M KOH electrolyte (pH=13), E(vs. RHE) = E(vs. Ag/AgCl) + 0.197 V + 0.0591pH.

Table S3 Comparison of OER catalytic activity of the catalysts in this work with the recently reported catalysts in alkaline solution.

| Electrocatalysts | EOER at 10 mA cm-2 (vs. RHE) | Tafel slope (mV dec-1) | Ref |
| --- | --- | --- | --- |
| CoPO-Co2P@NPC | 1.73 | 145.13 | This work |
| RuO2 | 1.56 | 127.70 | This work |
| Co-NCNTs//CCM | 1.64 | 131 | 2 |
| Co2P@NPC | 1.61 | 87 | 3 |
| C-Co2P | 1.64 | 86.8 | 6 |
| Co2P | 1.58 | 61.9 | 7 |
| Co2P@Co3O4 | 1.57 | 60 | 8 |

Table S4 Performances of recently reported Zn-air batteries based on bi-functional catalysts.

| Electrocatalysts | Open-circuit voltage (V) | Peak power density (mW cm-2) | Durability | Ref |
| --- | --- | --- | --- | --- |
| CoPO-Co2P@NPC | 1.43 | 265 | Over 450 hours@5 mA/cm2 | This work |
| Pt/C¦¦RuO2 | 1.42 | 211 | 270 hours@5 mA/cm2 | This work |
| Co2P@NCNTs-15 | 1.30 | 159.7 | 100 hours@10 mA/cm2 | 1 |
| Co2P@NPC | 1.43 | 157 | 140 hours@10 mA/cm2 | 3 |
| Co2P-PCA-800 | 1.44 | 58 | 32 hours@10 mA cm-2 | 9 |
| 7% Cu-Co2P/CNFs | 1.36 | 230 | 80 hours@5 mA cm-2 | 10 |
| CoO/CoxP | 1.40 | 122.73 | 200 hours@5 mA cm-2 | 11 |
| 7.1%Cu-Co2P@2D-NPC | 1.40 | 236.1 | 160 hours@10 mA cm-2 | 12 |

References:

1.	Peng, X.;  Liu, Y.;  Hu, S.;  Zheng, P.;  Fu, Y.;  Dong, P.;  Xiao, J.;  Han, L.; Zhang, Y., Synthesis of a highly efficient bifunctional Co2P@N-doped carbon nanotubes electrocatalyst by GO-Induced assembly strategy for rechargeable Zn-air batteries. Journal of Alloys and Compounds 2021, 889.

2.	Zhou, G.;  Liu, G.;  Liu, X.;  Yu, Q.;  Mao, H.;  Xiao, Z.; Wang, L., 1D/3D Heterogeneous Assembling Body as Trifunctional Electrocatalysts Enabling Zinc-Air Battery and Self-Powered Overall Water Splitting. Adv Mater 2021, 32 (4), e2107608.

3.	Shi, Q.;  Liu, Q.;  Zheng, Y.;  Dong, Y.;  Wang, L.;  Liu, H.; Yang, W., Controllable Construction of Bifunctional CoxP@N,P-doped Carbon Electrocatalysts for Rechargeable Zinc–Air Batteries. Energy & Environmental Materials 2021, 11 (2), 515-523.

4.	Han, X.;  Ling, X.;  Yu, D.;  Xie, D.;  Li, L.;  Peng, S.;  Zhong, C.;  Zhao, N.;  Deng, Y.; Hu, W., Atomically Dispersed Binary Co-Ni Sites in Nitrogen-Doped Hollow Carbon Nanocubes for Reversible Oxygen Reduction and Evolution. Adv Mater 2019, 31 (49), e1905622.

5.	Gao, J.;  Wang, J.;  Zhou, L.;  Cai, X.;  Zhan, D.;  Hou, M.; Lai, L., Co2P@N,P-codoped Carbon Nanofiber as Free-standing Air-electrode for Zn-air Batteries: Synergy Effects of CoNx Satellites shells. ACS Appl Mater Interfaces 2019, 12 (10), 10364-10372.

6.	Song, M.;  He, Y.;  Zhang, M.;  Zheng, X.;  Wang, Y.;  Zhang, J.;  Han, X.;  Zhong, C.;  Hu, W.; Deng, Y., Controllable synthesis of Co2P nanorods as high-efficiency bifunctional electrocatalyst for overall water splitting. Journal of Power Sources 2018, 402, 345-352.

7.	Hua, Y.;  Xu, Q.;  Hu, Y.;  Jiang, H.; Li, C., Interface-strengthened CoP nanosheet array with Co2P nanoparticles as efficient electrocatalysts for overall water splitting. Journal of Energy Chemistry 2019, 37, 1-6.

8.	Yao, L.;  Zhang, N.;  Wang, Y.;  Ni, Y.;  Yan, D.; Hu, C., Facile formation of 2D Co2P@Co3O4 microsheets through in-situ toptactic conversion and surface corrosion: Bifunctional electrocatalysts towards overall water splitting. Journal of Power Sources 2018, 374, 142-148.

9.	Xiao, Y.;  Pei, Y.;  Hu, Y.;  Ma, R.;  Wang, D.; Wang, J., Co2P@P-Doped 3D Porous Carbon for Bifunctional Oxygen Electrocatalysis. Acta Phys. -Chim. Sin. 2021, 37 (7), 2009051.

10.	Sun, X.;  Liang, H.;  Yu, H.;  Bai, J.; Li, C., Embedding Co2P nanoparticles in Cu doping carbon fibers for Zn-air batteries and supercapacitors. Nanotechnology 2022, 33, 135202.

11.	Niu, Y.;  Xiao, M.;  Zhu, J.;  Zeng, T.;  Li, J.;  Zhang, W.;  Su, D.;  Yu, A.; Chen, Z., Trimurti Heterostructured Hybrid with Intimate CoO/CoxP Interface as Robust Bifunctional Air Electrode for Rechargeable Zn-air Batteries. Journal of Materials Chemistry A 2020, 8 (18), 9177-9184.

12.	Diao, L.;  Yang, T.;  Chen, B.;  Zhang, B.;  Zhao, N.;  Shi, C.;  Liu, E.;  Ma, L.; He, C., Electronic reconfiguration of Co2P induced by Cu doping enhancing oxygen reduction reaction activity in zinc-air batteries. Journal of Materials Chemistry A 2019, 7 (37), 21232-21243.