Supporting Information

Design of C3N-based single-atom catalysts and calculation of the performance in electrocatalytic NO reduction reaction

Wei Songa, Pengfei Mac, Xiao Liua, Chaozheng Hed,e, Jinlong Wangb*
aSchool of Science, Henan Institute of Technology, Xinxiang, 453003, P.R. China

bSchool of Electronic Engineering, Tongling University, Tongling, 244061, P.R. China

cSchool of 3D Printing, Xinxiang University, Xinxiang, 453003, P.R. China
dSchool of Materials Science and Chemical Engineering, Xi'an Technological University, Xi'an, 710021, P. R. China
eInstitute of Environmental and Energy Catalysis, School of Materials Science and Chemical Engineering, Xi’an Technological University, Xi’an, 710021, P. R. China

*Corresponding authors:

E-mail: 396292346@qq.com (J. Wang).
Table S1 The adsorption energy (Eads in eV) of NO on TM-C@C3N and TM-N@C3N in N-end-on, O-end-on and side-on configuration (TM= Ti–Ni).
	TM-C@C3N
	End-on (NO)
	End-on (ON)
	Side

	Ti
	–2.082
	–1.195
	–1.527

	V
	–2.915
	–1.941
	–2.514

	Cr
	–2.816
	–1.589
	–2.210

	Mn
	–3.112
	–1.690
	–2.587

	Fe
	–2.815
	–1.453
	–2.162

	Co
	–3.042
	–1.469
	–2.741

	Ni
	–3.730
	–1.965
	–2.925

	TM-N@C3N
	End-on (NO)
	End-on (ON)
	Side

	Ti
	–2.693
	–2.198
	–2.233

	V
	–2.890
	–1.708
	–2.541

	Cr
	–2.715
	–1.643
	–2.431

	Mn
	–3.055
	–1.737
	–1.991

	Fe
	–2.232
	–1.403
	–1.358

	Co
	-2.085
	–1.002
	–1.658

	Ni
	–2.549
	–1.239
	–2.123


Table S2 The V–N bond length (dV-N in Å), Bader charge (Q in e) and adsorption energy (Eads in eV) for reaction intermediates on V-C@C3N via O-distal, O-alternative, N-distal and N-alternative pathway, respectively.
	O-distal
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.915

	*NOH
	1.711
	0.839
	–3.750

	*N
	1.628
	1.244
	–4.577

	*NH
	1.704
	0.997
	–4.886

	*NH2
	1.909
	0.656
	–4.075

	*NH3
	2.205
	–0.014
	–1.382

	O-alternative
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.915

	*NOH
	1.711
	0.839
	–3.750

	*HNOH
	1.963
	0.640
	–3.067

	*NH
	1.704
	0.997
	–4.886

	*NH2
	1.909
	0.656
	–4.075

	*NH3
	2.205
	–0.014
	–1.382

	N-distal
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.915

	*NHO
	1.930
	0.979
	–2.832

	*H2NO
	2.193
	0.615
	–3.602

	*H2NOH
	1.730
	1.082
	–3.232

	*NH2
	1.909
	0.656
	–4.075

	*NH3
	2.205
	–0.014
	–1.382

	N-alternative
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.915

	*NHO
	1.930
	0.979
	–2.832

	*HNOH
	1.963
	0.640
	–3.067

	*H2NOH
	1.730
	1.082
	–3.232

	*NH2
	1.909
	0.656
	–4.075

	*NH3
	2.205
	–0.014
	–1.382


Table S3 The V–N bond length (dV-N in Å), Bader charge (Q in e) and adsorption energy (Eads in eV) for reaction intermediates on V-N@C3N via O-distal, O-alternative, N-distal and N-alternative pathway, respectively.
	O-distal
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.890

	*NOH
	1.711
	1.839
	–3.729

	*N
	1.628
	2.668
	–4.464

	*NH
	1.704
	0.997
	–4.780

	*NH2
	1.909
	0.656
	–3.984

	*NH3
	2.205
	–0.014
	–1.378

	O-alternative
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.890

	*NOH
	1.711
	1.839
	–3.729

	*HNOH
	1.963
	0.640
	–3.048

	*NH
	1.704
	0.997
	–4.780

	*NH2
	1.909
	0.656
	–3.984

	*NH3
	2.205
	–0.014
	–1.378

	N-distal
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.890

	*NHO
	1.930
	0.979
	–2.620

	*H2NO
	2.193
	0.615
	–3.371

	*H2NOH
	1.730
	1.082
	–3.108

	*NH2
	1.909
	0.656
	–3.984

	*NH3
	2.205
	–0.014
	–1.378

	N-alternative
	dV-N
	Q
	Eads

	*NO
	1.782
	0.792
	–2.890

	*NHO
	1.930
	0.979
	–2.620

	*HNOH
	1.963
	0.640
	–3.048

	*H2NOH
	1.730
	1.082
	–3.108

	*NH2
	1.909
	0.656
	–3.984

	*NH3
	2.205
	–0.014
	–1.378


