Supplementary document

Enhanced Electrochemical Corrosion Resistance of GO/ZnO/Epoxy Nanocomposite Coatings on Magnesium Alloy in Saline Environment

Khaled A. Jilo a, Khaled M. Chahrour *a, Hayrettin Ahlatçı b, Ahmed Abdel Nazeer c

- Mechanical Engineering Dept., Faculty of Engineering, Karabuk University, 78050, Karabuk, Turkiye.

- Metallurgical and Materials Engineering Dept., Faculty of Engineering, Karabuk University,78050, Karabuk, Turkiye

- Electrochemistry Laboratory, Physical Chemistry Department, National Research Center, Giza, Egypt.

*Corresponding author email: Khaledchahrour@karabuk.edu.tr

Table S1. Tafel polarization results  of bare substrate, Epoxy coating, ZnO1.36/Ep coating, ZnO2.53/Ep coating, ZnO4.10/Ep coating, ZnO5.20/Ep coating, GO0.8/ZnO4.1/Ep, GO0.4/ZnO4.1/Ep, GO0.2/ZnO4.1/Ep and GO0.05/ZnO4.1/Ep.

| Coating | Icorr (A/cm2) | Ecorr (V) | Corrosion Rate (mmpy) |
| --- | --- | --- | --- |
| Bare substrate | 6.682×10-7 | -1.523 | 2940.9 |
| Epoxy Coating | 4.030×10-7 | -1.333 | 854.4 |
| ZnO1.36/Ep | 3.486×10-7 | -1.155 | 793.2 |
| ZnO2.53/Ep | 5..300×10-8 | -0.808 | 193.3 |
| ZnO4.10/Ep | 5.565×10-9 | -0.518 | 43.54 |
| ZnO5.20/Ep | 3.750×10-8 | -0.713 | 233.4 |
| GO0.8/ZnO4.1/Ep | 2.500×10-7 | -1.180 | 442.4 |
| GO0.4/ZnO4.1/Ep | 1.900×10-7 | -1.024 | 234.3 |
| GO0.2/ZnO4.1/Ep | 5.856×10-8 | -0.997 | 195.1 |
| GO0.05/ZnO4.1/Ep | 3.485×10-9 | -0.422 | 4.170 |

Table S2. EIS fitted Nyquist curve results of bare substrate. The Epoxy coating. ZnO1.36/Ep coating. ZnO2.53/Ep coating. ZnO4.10/Ep coating. ZnO5.20/Ep coating. GO0.8/ZnO4.1/Ep. GO0.4/ZnO4.1/Ep. GO0.2/ZnO4.1/Ep and GO0.05/ZnO4.1/Ep.

| Coating | Rct (Ωcm-2) | Rs (Ωcm-2) | Rc (Ωcm-2) | CPEdl (Ω-1cm-2sn ) |  | CPEc (Ω-1cm-2sn) |
| --- | --- | --- | --- | --- | --- | --- |
| Bare substrate | 28150 | 25.46 | - |  | 94.02×10-6 | - |
| Epoxy Coating | 54232 | 22.83 | 38020 |  | 7.318×10-6 | 11.37×10-6 |
| ZnO1.36/Ep | 57105 | 11.72 | 33030 |  | 6.276×10-6 | 8.627×10-6 |
| ZnO2.53/Ep | 81440 | 33.71 | 1681 |  | 5.394×10-6 | 7.326×10-6 |
| ZnO4.10/Ep | 129000 | 0.232 | 3705 |  | 4.248×10-6 | 9.024×10-7 |
| ZnO5.20/Ep | 113580 | 20.1×10-6 | 264.7 |  | 4.376×10-6 | 2.160×10-6 |
| GO0.8/ZnO4.1/Ep | 133475 | 6.607 | 3247 |  | 2.995×10-6 | 6.913×10-8 |
| GO0.4/ZnO4.1/Ep | 165420 | 7930 | 20210 |  | 1.758×10-6 | 5.754×10-9 |
| GO0.2/ZnO4.1/Ep | 319050 | 0.002 | 0.032 |  | 1.471×10-6 | 7.869×10-10 |
| GO0.05/ZnO4.1/Ep | 499020 | 657.4 | 84020 |  | 7.864×10-7 | 9.815×10-11 |

Figure S1. The Tafel plots of bare substrate and Epoxy-coated substrate.

Figure S.2. The Tafel plots of ZnO1.36/Ep, ZnO2.53/Ep, ZnO4.10/Ep and ZnO5.20/Ep coatings.

Figure S3. The Tafel plots of GO0,8/ZnO4.10/Ep. GO0,4/ZnO4.10/Ep, GO0,2/ZnO4.10/Ep and GO0,05/ZnO4.10/Ep coatings.

Figure S4. The Nyquist plots of bare substrate and Epoxy-coated substrate.

Figure S5. The Nyquist plots of ZnO1.36/Ep, ZnO2.53/Ep, ZnO4.10/Ep and ZnO5.20/Ep coatings.

Figure S6. The Nyquist plots of GO0,8/ZnO4.10/Ep. GO0,4/ZnO4.10/Ep, GO0,2/ZnO4.10/Ep and GO0,05/ZnO4.10/Ep coatings.

Figure S7. The Bode plots of bare substrate and Epoxy-coated substrate.

Figure S8. The Bode plots of ZnO1.36/Ep, ZnO2.53/Ep, ZnO4.10/Ep and ZnO5.20/Ep coatings.

Figure S9. The Bode plots of GO0,8/ZnO4.10/Ep. GO0,4/ZnO4.10/Ep, GO0,2/ZnO4.10/Ep and GO0,05/ZnO4.10/Ep coatings.