Applied Microbiology and Biotechnology Express

Novel method to achieve crystallinity of calcite by Bacillus subtilis in coupled and non-coupled calcium-carbon sources

Ferral-Pérez H.ab, Galicia-García M.b, Alvarado-Tenorio B.c, Izaguirre-Pompa Ad, Aguirre-Ramírez M.a*

a Laboratorio de Biología Celular y Molecular. b Laboratorio de Electroquímica. c Laboratorio de Bioquímica Funcional y Proteómica del Estrés. Departamento de Ciencias Químico-Biológicas, Instituto de Ciencias Biomédicas, Universidad Autónoma de Ciudad Juárez, Cd. Juárez, Chih., 32310. México.

d Laboratorio de Geología. Departamento de Ingeniería Civil y Ambiental, Instituto de Ingeniería y Tecnología, Universidad Autónoma de Ciudad Juárez, Cd. Juárez, Chih.

* Corresponding author: Marisela Aguirre-Ramírez, marisela.aguirre@uacj.mx

Supplementary material:

Fig S1. pH values of B. subtilis cultures grown in Nutrient Broth supplemented conditions. Data represents the average of three independent experiments  standard deviation.

Fig. S2 Thin section micrograph of BCC-ACE observed under bright field and polarized light. Scale: 100 µm.

Fig. S3 Thin section micrograph of BCC-GLC observed under polarized light. Mineral botryoidal growth, triple or double joins in twinned crystal, and baciliar shapes are shown. Scale: 10 µm

Fig. S4 SEM images showing the crystallites formed over EPS of BCC-GLY (a) and BCC-GLC (b). Scale: 500 nm.

Fig. S5 Micrograph of BCC formed in ACE conditions. The mineralized cell-filaments are observed. Scale: 10 µm.

.

Fig. S6 BCC composition. (a) Bars correspond to the average of six punctual EDX measurements taken over four different crystals of BCC-GLY (white), BCC-GLC (black), BCC-LAC (dark gray) and BCC-ACE (gray). Error bars indicate standard deviation. (b) FTIR-ATR spectrum of all BCC. The main functional vibrations groups for calcite (C), polysaccharides (PS), phosphates (PO) and amides (A) are marked.