Supplementary information of

High-temperature helical edge states in BiSbTeSe2/graphene van der Waals heterostructure

- Calculation the resistance of a six-terminal quantum spin Hall bar with the disorder of contact electrodes or the elastic spin flip back scattering at between two contact electrodes.

In non-local transport measurements of quantum spin Hall insulators, it was observed that there are slight deviations in resistance from the ideal quantized value. These deviations could possibly be attributed to the effects of disorder in the electrodes used for contact and elastic spin flip back scattering on the helical edge channel at low temperatures where the inelastic spin flip back scattering is suppressed as discussed in the main text [1, 2]. To clarify these effects on the observed resistance, we calculated the resistance with various conditions. In the following calculations, we always used contact electrodes 1 and 4 as current input and output electrodes, and the voltage drop was calculated between electrodes 2 and 3, or between 1 and 4. Using these combinations of current and voltage electrodes, R1423 and R1414 are calculated [1].

First, we showed the effects of the disorder in the contact electrodes on the helical edge resistance. Figure S1 a, and b displayed a schematic view of a six probe Hall bar device of quantum spin Hall insulators with the disorders in the contact electrodes. In the case of Fig. S1(a), due to the potential mismatch between the helical edge and the contact electrode 2, the transmission of electrode 2 is imperfect. Therefore, the transmission and reflection rates of electrode 2, Ttrans2 and R2, were set as variable parameters under the condition Ttrans2+R2=1, and the transmission rates of other contact electrodes of 1,3,4,5,6 (Ttrans i,i=1,3,4,5,6) were set to 1. With these conditions, the conductance matrix was derived using Landauer-Büttiker formalism [3] as follows:

Gij=-e2h-2Ttrans2R2001Ttrans2-2Ttrans2T2000R2T2-2100001-2100001-2110001-2  .

Using Vj=Gij-1Ii, the voltage drops between electrodes 2 and 3 and electrodes 1 and 4 were estimated. Finally, R14;23=V2-V3I and R14;14=V1-V4I were derived using R2 as a variable parameter as shown in Fig. S1 c and d. In both cases, R14;23 and R14;14 decreased from the ideal values of RQ2 and 32RQ with increasing R2. Alternatively, if the electrode 1 had a disorder effect and 0≤Ttrans1≤1, R14;14 gradually increased from ideal 32RQ with increasing R2 while R14;23 was constant around ideal RQ2.

In the case of Fig. S1 b, the disorders induced imperfect transmissions were assumed for electrode 1 and 2. Therefore, Ttrans1 and R1 and,  Ttrans2 and R2 for electrode 1 and 2 were set as variable parameters with the condition Ttrans1+Rtrans1=Ttrans2+Rtrans2=1, and the transmission rate of other contact electrodes of 3,4,5,6 (Ttransi,i=3,4,5,6) were set to 1. The conductance matrix was set as follows:

Gij=-e2h-2Ttrans1Ttrans1Ttrans2Ttrans1R200Ttrans1Ttrans1Ttrans2-2Ttrans2Ttrans200R1Ttrans1Ttrans1R2Ttrans2-210R1R2001-2100001-21Ttrans1R1Ttrans2R1R201-2.

We set R1=Ttrans1=0.5 and R2=1-Ttrans2 was used variable parameters for calculations as shown in Fig. S1 e and f. R14;23 is ~30% higher than RQ2 when R2=0, and it gradually increased with increasing R2 while R14;14 was almost constant ∼23RQ against R2. The results of calculations represented that the disorder of the electrodes can cause the positive and negative deviation of the electrical resistance of the helical edge states from the ideal quantized resistance.

Secondly, we also represented the effects of the elastic spin flip back scattering on resistance of the helical edge states. Figure S2a, and b showed the schematic view of a six probe Hall bar device of quantum spin Hall insulators with a elastic spin flip back scattering source at the helical edge channel between electrode 1 and 2 , and 2 and 3. In the case of Fig. S2a (Fig. S2 b). Due to the elastic spin flip back scattering, the transmission of the helical edge between electrodes 1 and 2 (2 and 3) was imperfect, i.e., Ttrans_12 (Ttrans_23) was set in the range of 0≤Ttrans_12≤1 (0≤Ttrans_23≤1) with Ttrans_12+R12=1 (Ttrans_23+R23=1) condition. The conductance matrix was set for Fig. S2 a case as follows:

Gij=-e2h-2Ttrans_122Ttrans_12-100012Ttrans_12-1-2Ttrans_12-100001-2100001-2100001-2110001-2.

For the Fig. S2 b case, the conductance matrix was set as follows:

Gij=-e2h-2100011-2Ttrans_232Ttrans_23-100002Ttrans_23-1-2Ttrans_23100001-2100001-2110001-2.

The R12 dependence of R14;23 and R14;14 for Fig. S2 a case were shown in Fig. S2 c and d. With increasing R12 in the range of 0≤R12≤0.4, R14;23 gradually decreased while R14;14 increased. For Fig. S2b case, the R23 dependence of R14;23 and R14;14 were shown in Fig. S2 e and f. With increasing R23 in the range of 0≤R23≤0.4, both R14;23 and R14;14 increased gradually. The calculation results showed that the elastic backscattering can also cause the positive and negative deviations in the electrical resistance of the helical edge states from the ideal quantized resistance.

- Band calculation of BiSbTeSe2/graphene vdW heterostructure with different atomic stacking configurations.

To identify the stable configuration and maximize the Kekulé gap, we examined four different atomic stacking arrangements between graphene and two quintuple layers (QLs) of BiSbTeSe2 with an interlayer C–Te distance of approximately 3.7  Å as illustrated in Fig. S3. The configurations considered include the following: (i) Te atoms positioned at the center of graphene hexagons (C-mid), (ii) Te atoms located directly above carbon atoms (C-top), (iii) Te atoms situated above the C–C bonds (C-bridge), and (iv) a randomly distributed arrangement. Among these, the C-mid configuration was found to be the most energetically favorable, yielding a band gap of approximately Δ ~ 6.5 meV. Notably, this magnitude of the band gap aligns well with the transport-measured Kekulé gap Δ2 of  ~ 7 meV observed for the 2 nm BiSbTeSe2  device as shown in Fig. 3a of the main text and in Extended Data Fig. 6a.

- Evolution of the Kekulé band gap as the function of C-Te distance

We calculated the Kekulé band gap as a function of the C–Te interlayer distance in the C-mid stacking configuration with SOI, as shown in Fig. S4, for 3QL BiSbTeSe2. As the distance d increases from 3.5 to 3.9 Å  the Kekulé gap decreases from 15.6 meV to 5.4 meV.

- TEM images

From the TEM images in Figure S5, we can clearly identify the monolayer graphene and BiSbTeSe2 layers. The gap between graphene and BiSbTeSe2 is found to be approximately 3.89 Å while the thickness of 1 QL BiSbTeSe2 layer is about 9.97 Å.

FigureS1 | Calculating the resistance of a six-terminal quantum spin Hall bar with disordered electrodes. a Electrode 2 has disorder, and the transmission and reflection of electrode 2 (Ttrans_2 and R2 ) are parameters for resistance calculation. b Both electrodes 1 and 2 have disorder, and the transmission and reflection of electrodes 1 and 2 (Ttrans_1, R1 and Ttrans_2, R2) are parameters for resistance calculation. c,d Calculated R14;23 and R14;14 for case a. R2 is a variable parameter. e,f Calculated R14;23 and R14;14 for case b. Ttrans_1=R1= 0.5 and R2 is a variable parameter.

FigureS2 | Calculation of the resistance of a six-terminal quantum spin Hall bar with an elastic spin flip back scattering source. The figure shows a schematic view of a six-terminal quantum spin Hall bar with elastic spin flip back scattering source at the position between a electrode 1 and 2. b electrode 2 and 3. Transmission and reflection are Ttrans_12, R12 and Ttrans_23,R23 with Ttrans_12+R12=1 and Ttrans_23+R23=1. c,d Calculated R14;23 and R14;14 for the case of a. e,f Calculated R14;23 and R14;14 for the case of b. R12 and R23 are variable parameters.

FigureS3 | Calculated Kekulé gap of 2 QL BiSbTeSe2/ graphene using DFT without (NSOC) and with (SOC) spin – orbit – interaction for different stacking configurations.

FigureS4 | Evolution of the Kekulé band gap as a function of the C-Te distance d from 3.5 to 3.9 Å.

FigureS5 |TEM data of 30-nm BiSbTeSe₂/graphene vdW heterostructures a. High-resolution TEM image showing the layered BiSbTeSe₂/graphene film. Region labeled 1 indicates the interfacial gap between the graphene and the topmost BiSbTeSe₂ layer, while region 2 highlights a single quintuple layer (QL) of BiSbTeSe₂. The scale bar is 5 nm. b. Line profile measurement of the image intensity taken along the vertical axis from the bottom to the top. The measured interfacial gap between graphene and BiSbTeSe₂ is approximately 3.89 Å, and the thickness of one QL of BiSbTeSe₂ is about 9.97 Å.

Reference

[1] Arjun Mani and Colin Benjamin: J. Phys.: Condens. Matter 28 (2016) 145303.

[2] Dyakonov, M. I. & Perel, V. I. Spin relaxation of conduction electrons in noncentrosymmetric semiconductors. Soviet Physics Solid State 13, 3023–3026 (1972). / Yafet, Y. Solid State Physics (F. Seitz and D. Turnbull, 1963).

[3] M. Büttiker, Phys. Rev. Lett. 57, 1761 (1986).