Supplementary Note 1: Symmetry breaking and second-harmonic generation in Gr- Ge(110) moiré heterostructure

Optical second-harmonic generation (SHG) exhibits exceptional sensitivity to crystal structural symmetry and occurs exclusively in non-centrosymmetric materials1, making it an ideal probe to investigate symmetry properties in mixed-dimensional Gr-Ge(110) heterostructures. The inversion symmetry-breaking effect in epitaxial Gr-Ge(110) heterostructures manifest through the emergence of optical second-harmonic generation, as demonstrated in Fig. 1j and Extended Data Fig. 2. In contrast, monolayer graphene transferred onto the SiO2/Si substrate exhibits a negligible SHG response due to the centrosymmetric lattice structure of quasi-free-standing graphene, wherein the inversion center at the hollow sites of the hexagonal lattice (Extended Data Fig. 2a).

The SHG intensity for epitaxial Gr-Ge(110) heterostructure exhibits a linear dependence on the incidence power when analyzed on a double-logarithmic scale (Extended Data Fig. 2b). Linear fitting yields a slope of 1.903 ± 0.02, unambiguously confirming the SHG process. Anisotropic polarization-dependent SHG measurements reveal the predicted C1v symmetry (Fig. 1j)2,3. Remarkably, the optical second-order susceptibility 2 value of 1,102 pm V-1 for the Gr-Ge(110) moiré heterostructure substantially exceeds those reported for MoS24, WS24 and LiNbO31 (Extended Data Fig. 2c), primarily due to its low-symmetry.

Supplementary Note 2: Scaling analysis of the NLHE for Gr-Ge moiré heterostructure

To perform the scaling and understand underlying mechanisms of the nonlinear Hall effect (NLHE) in Gr/Ge (110) heterostructure, Vy2ω, Vx2ω and Vxω are measured simultaneously at a 5 A a.c. stimulation at different temperatures. The measured first-harmonic longitudinal voltage Vxω is plotted in Extended Data Fig. 6a. The second-order nonlinear Hall (Ey2ω) and longitudinal (Ex2ω) electric field are calculated, respectively, according to the relationship Ey2ω=Vy2ωW and Ex1ω=Vx1ωL to account for different device dimensions, where W = 20 m and L = 50 m are the transverse and longitudinal dimensions of the Hall bar device. The temperature-dependent behavior of Ey2ω and Ex2ω is illustrated in Extended Data Fig. 6b. Both Ey2ω and Ex2ω exhibit the same temperature dependence characterized by a peak at around 250 K and suppression at a lower temperature. This non-monotonic behavior excludes the heating effect as the dominant mechanism, since such effects typically become more substantial at a low temperature. The NLHE strength5, defined as Ey2ωEx1ω2, exhibits a similar temperature dependence versus the linear conductivity σxx (Extended Data Fig. 6c), suggesting a potential correlation between the NLHE strength and σxx.

To explicitly demonstrate this relationship, Ey2ωExω2 versus σxx is plotted on log-log scales in the main panel of Fig. 2c. The data show excellent agreement with the power-law formula Ey2ωExω2~σvT, where the exponent v is pronouncedly temperature-dependent, which approaches saturation at v≈2 at elevated temperatures (T>250 K) as illustrated in the inset of Fig. 2c. Below a critical conductivity (T<250 K), v increases monotonically above 2, resulting in accelerated Ey2ωEx1ω2 growth. Consequently, Ey2ωEx1ω2 can be approximately linearly fitted with σxx2 in T>250 K region:

Ey2ωEx1ω2=Aσxx2+B                         (1)

where A and B are constants. The slope term A quantifies the contributions from extrinsic skew-scattering mechanisms, while the intercept term B captures the intrinsic contributions, such as Berry curvature dipole (BCD) or extrinsic side-jump effects that remain independent of the longitudinal conductivity6–8. The side-jump contribution is usually neglected for the clean sample with high-conductivity such as graphene systems9–11. The extracted A = 3.3×108 μm V-1 Ω2 and B = 134 μm V-1 demonstrate that the extrinsic skew-scattering dominates over other possible mechanisms at higher temperature, driving the room-temperature NLHE in our Gr-Ge(110) heterostructure. At lower temperatures, BCD contributions emerge and become increasingly significant, leading to deviations of Equation (1).

Supplementary Note 3: Rectification voltage induced by the NLHE

According to the NLHE theory12,13, the transverse second-order responses inherently involve both double-frequency (2ω) and d.c. components in response to an oscillating electric field Et= RE∙eiωt, where the d.c. component is harnessed for rectification. The d.c. and 2ω components can be expressed as JaDC=χabc Ebω Ecω*  and Ja2ω=χabc Ebω Ecω, where χabc is the nonlinear conductivity tensor (a, b,c=x, y,z). To detect the NLHE experimentally, an a.c. current Ixω= I0 sinωt is applied to the Hall-bar device along x-axis and the nonlinear transverse voltage VyNLH scaling quadratically with Ixω is extracted through harmonic measurements. Explicitly, there is

VyNLH=RyNLH∙Ixω2 ,                        (2)

where RyNLH is proportional to the nonlinear conductivity χyxx and can be treated as a constant for simplicity. Equation (2) can be further expanded as by substituting Equation (1) into it:

VyNLH=RyNLH∙I0 sinωt2=12RyNLH∙I02+12RyNLH∙I02∙sin⁡(2ωt-π2) .  (3)

The first and second terms in Equation (3) represent the rectified d.c. and out-of-phase 2ω components of second-order nonlinear Hall responses, respectively, which indicates that the rectified Hall voltage (Vyd.c.) is the same as the peak-to-peak value of the second-harmonic voltage (i.e. Vyd.c.=Vy2ω, peak). It is worth mentioning that Vyd.c. is directly recorded from a nanovoltmeter while the second-harmonic voltage Vy2ω measured by a lock-in amplifier in our work is the root-main-square (RMS) value. Consequently, there is

Vy2ω=Vy2ω, peak2=Vyd.c.2,                   (4)

which accounts for the constant ratio of Vyd.c.Vy2ω shown in the inset of Fig. 2e.

Supplementary Table 1. Comparison of NLHE strength for various material systems

| Materials | Mechanism | Input current maximum (A) | Output voltage maximum (V) | Ey2ωExω2 (m V-1) | RT operation | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Few-layer WTe2 | Intrinsic and extrinsic | 600 | 30 | 1.410-3 @2 K 5.810-4 @100 K | No | 6 |
| Bilayer WTe2 | Intrinsic | 1 | 170 | 0.14 @10 K | No | 13 |
| Bilayer MoTe2 | Intrinsic dominated | 97 | 125 | 0.07 @3 K 6.610-4 @100 K | No | 14 |
| Td-MoTe2 (c-axis) | Extrinsic | 5000 | 1 | 4105 @2 K 150 @40 K | No | 5 |
| Strained monolayer WSe2 | Intrinsic | 4.5 | 20 | 0.53 @140 K | No | 15 |
| Bi2Se3 | Extrinsic | 1500 | 20 | 710-4 @50 K 410-4 @200 K | No | 16 |
| MnBi2Te4 | Intrinsic | 10 | 200 | 1.6 @2 K 1.2 @10 K | No | 17 |
| Corrugated bilayer graphene | Intrinsic | 0.1 | 1 | 10 @3 K 1 @15 K | No | 18 |
| Graphene/hBN superlattice | Extrinsic | 5 | 100 | 200 @1.7 K 0.8 @200 K | No | 10 |
| BP/MnBi2Te4/BP heterostructure | Intrinsic | 10 | 350 | 0.2 @2 K 0.02 @20 K | No | 19 |
| Twisted bilayer WSe2 | Intrinsic | 0.004 | 50000 | 9500 @1.5 K 0.35 @30 K | No | 20 |
| Twisted bilayer graphene | Extrinsic | 5 | 600 | 50 @1.7 K 4.6 @80 K | No | 9 |
| Twisted bilayer graphene (strained) | Intrinsic and Extrinsic | 0.15 | 10 | 2.2104 @1.5 K 2103 @70 K | No | 21 |
| Twisted double bilayer graphene | Intrinsic | 0.1 | 150 | 1.8104 @1.5 K | No | 22 |
| Twisted bilayer MoS2 | Intrinsic | 0.0015 | 1000 | 533 @70 K 18 @285 K | YES | 23 |
| TaIrTe4 | Intrinsic and extrinsic | 600 | 120 | 25 @2 K 4.5 @300 K | YES | 24 |
| BiTeBr | Extrinsic | 5 | 100 | 7 @20 K 0.5 @300 K | YES | 25 |
| BaMnSb2 | Intrinsic | 200 | 400 | 1.2103 @200 K 163 @300 K | YES | 26 |
| Te | Extrinsic dominated | 51 | 105 | 0.08 @200 K 0.02 @300 K | YES | 27 |
| Bi | Extrinsic | 60 | 3 | 0.01 @293 K | YES | 28 |
| Pt | Extrinsic | 50 | 80 | 1.65 @175 K 320 @300 K | YES | 29 |
| Epitaxial-Gr/Ge moiré superlattice | Intrinsic and extrinsic | 100 | 15000 | 3.67 @175 K 1487 @300 K | YES | This work |

Supplementary Reference

1.	Boyd, R. W. Nonlinear Optics 4th edn (Academic Press, 2020).

2.	Wu, S. et al. Polarization photodetectors with configurable polarity transition enabled by programmable ferroelectric-doping patterns. Nat. Commun. 15, 8743 (2024).

3.	Song, Y. et al. Second harmonic generation in atomically thin MoTe2. Adv. Opt. Mater. 6, 1701334 (2018).

4.	Bredillet, K. et al. Dispersion of the nonlinear susceptibility of MoS2 and WS2 from second-harmonic scattering spectroscopy. Phys. Rev. B 102, 235408 (2020).

5.	Tiwari, A. et al. Giant c-axis nonlinear anomalous Hall effect in Td-MoTe2 and WTe2. Nat. Commun. 12, 2049 (2021).

6.	Kang, K., Li, T., Sohn, E., Shan, J. & Mak, K. F. Nonlinear anomalous Hall effect in few-layer WTe2. Nat. Mater. 18, 324–328 (2019).

7.	Du, Z. Z., Wang, C. M., Li, S., Lu, H.-Z. & Xie, X. C. Disorder-induced nonlinear Hall effect with time-reversal symmetry. Nat. Commun. 10, 3047 (2019).

8.	Xiao, C., Zhou, H. & Niu, Q. Scaling parameters in anomalous and nonlinear Hall effects depend on temperature. Phys. Rev. B 100, 161403 (2019).

9.	Duan, J. et al. Giant second-order nonlinear Hall effect in twisted bilayer graphene. Phys. Rev. Lett. 129, 186801 (2022).

10.	He, P. et al. Graphene moiré superlattices with giant quantum nonlinearity of chiral Bloch electrons. Nat. Nanotechnol. 17, 378-383 (2022).

11.	Isobe, H., Xu, S.-Y. & Fu, L. High-frequency rectification via chiral Bloch electrons. Sci. Adv. 6, eaay2497 (2020).

12.	Sodemann, I. & Fu, L. Quantum nonlinear Hall effect induced by Berry curvature dipole in time-reversal invariant materials. Phys. Rev. Lett. 115, 216806 (2015).

13.	Ma, Q. et al. Observation of the nonlinear Hall effect under time-reversal-symmetric conditions. Nature 565, 337–342 (2019).

14.	Ma, T. et al. Growth of bilayer MoTe2 single crystals with strong non-linear Hall effect. Nat. Commun. 13, 5465 (2022).

15.	Qin, M.-S. et al. Strain tunable Berry curvature dipole, orbital magnetization and nonlinear Hall Effect in WSe2 monolayer. Chin. Phys. Lett. 38, 017301 (2021).

16.	He, P. et al. Quantum frequency doubling in the topological insulator Bi2Se3. Nat. Commun. 12, 698 (2021).

17.	Wang, N. et al. Quantum-metric-induced nonlinear transport in a topological antiferromagnet. Nature 621, 487–492 (2023).

18.	Ho, S.-C. et al. Hall effects in artificially corrugated bilayer graphene without breaking time-reversal symmetry. Nat. Electron. 4, 116–125 (2021).

19.	Gao, A. et al. Quantum metric nonlinear Hall effect in a topological antiferromagnetic heterostructure. Science 381, 181–186 (2023).

20.	Huang, M. et al. Giant nonlinear Hall effect in twisted bilayer WSe2. Natl. Sci. Rev. 10, nwac232 (2023).

21.	Huang, M. et al. Intrinsic nonlinear Hall effect and gate-switchable Berry curvature sliding in twisted bilayer graphene. Phys. Rev. Lett. 131, 066301 (2023).

22.	Sinha, S. et al. Berry curvature dipole senses topological transition in a moiré superlattice. Nat. Phys. 18, 765-770 (2022).

23.	Wu, F. et al. Giant correlated gap and possible room-temperature correlated states in twisted bilayer MoS2. Phys. Rev. Lett. 131, 256201 (2023).

24.	Kumar, D. et al. Room-temperature nonlinear Hall effect and wireless radiofrequency rectification in Weyl semimetal TaIrTe4. Nat. Nanotechnol. 16, 421–425 (2021).

25.	Lu, X. F. et al. Nonlinear transport and radio frequency rectification in BiTeBr at room temperature. Nat. Commun. 15, 245 (2024).

26.	Min, L. et al. Strong room-temperature bulk nonlinear Hall effect in a spin-valley locked Dirac material. Nat. Commun. 14, 364 (2023).

27.	Cheng, B. et al. Giant nonlinear Hall and wireless rectification effects at room temperature in the elemental semiconductor tellurium. Nat. Commun. 15, 5513 (2024).

28.	Makushko, P. et al. A tunable room-temperature nonlinear Hall effect in elemental bismuth thin films. Nat. Electron. 7, 207-215 (2024).

29.	Min, L. et al. Colossal room-temperature non-reciprocal Hall effect. Nat. Mater. 23, 1671-1677 (2024).