Silver Nanoparticles from Tabernaemontana Divaricate leaf extract: Mechanism of action and Bio-application for photo degradation of 4-Aminopyridine.

Pratibha Attri1 Sangeeta Garg1*, Jatinder Kumar Ratan1, Ardhendu Sekhar Giri2

1Department of Chemical Engineering, Dr. B.R. Ambedkar National Institute of Technology, Jalandhar, India.

2Department of Chemical Engineering, Indian Institute of Science Education and Research, Bhopal, India.

*E-mail: [gargs@nitj.ac.in]

Availability of data and materials

1.1 Data sheet for XRD of Ag NPs

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 38.1649 | 1164.62 | 0.4408 | 2.35812 | 100.00 |
| 44.4631 | 282.85 | 0.6927 | 2.03763 | 24.29 |
| 64.5272 | 284.26 | 0.3149 | 1.44420 | 24.41 |
| 77.5868 | 268.94 | 0.5668 | 1.23052 | 23.09 |

Name and formula

Reference code:	98-060-4629

Compound name:	Silver

Common name:	Silver

Chemical formula:	Ag1

Peak list

| No. | H | k | l | d [Å] | 2θ [°] | I [%] |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1 | 1 | 1 | 2.35848 | 2.430 | 100.0 |
| 2 | 0 | 0 | 2 | 2.04250 | 2.805 | 47.5 |
| 3 | 0 | 2 | 2 | 1.44427 | 3.968 | 27.8 |
| 4 | 1 | 1 | 3 | 1.23167 | 4.653 | 30.9 |
| 5 | 2 | 2 | 2 | 1.17924 | 4.860 | 8.9 |