Supplementary Materials
Electrocatalytic hydrogen evolution by a novel copper(II) complex: influence of pH and mechanistic insight via DFT
Soumen Rakshit1, Jyotirmoy Mitra1, Jaya Pal1, Ram Chandra Maji1,*
1 Department of Chemistry, Bankura University, Bankura-722155, West Bengal, India.
* Correspondence: rammaji1@gmail.com
Synthesis of 2,2'-(((pyridin-2-ylmethyl)azanediyl)bis(ethane-2,1-diyl))bis(isoindoline-1,3-dione) (c1): 2-picolylamine (2 g, 18.49 mmol), N-(2-Bromoethyl)phthalimide (9.4 g 36.97 mmol), anhydrous K2CO3 (20.44 g, 147.90 mmol), KI (6.137 g, 36.97 mmol) were added to a freshly distilled 300 mL of CH3CN in a 500 mL RB flask under N2 atmosphere. The mixture was refluxed for 24 h and filtrated. The solvent was removed by a rotatory evaporator to yield a brown oil. The oil was dissolved in 200 mL CHCl3 and washed with brine water (200 mL × 3). The organic layer was concentrated to yield a brown solid. The white solid product (4.9 g, 10.78 mmol, 58%) was obtained by a silica-gel chromatography separation using 80% ethyl acetate/hexane. 1H NMR (400 MHz, CDCl3): δ = 8.42 (d, J = 4.8 Hz, 1H), δ = 7.70 (m, 8H), δ = 7.07 (t, J = 4.76 Hz, 3H), δ = 3.86 (s, 2H), δ = 3.77 (d, J = 6.1 Hz, 4H), δ = 2.48 (t, J = 6.3 Hz, 4H), Selected IR frequencies (ATR, cm−1): 3064(w), 2981(w), 2941(w), 2825(w), 1771(m, νC=O), 1703(vs, C=O), 1467(m), 1432(m), 1393(vs), 1240(s), 1082(m), 1042(m), 1009(m), 715(vs), 528(vs).
Synthesis of N1-(2-aminoethyl)-N1-(pyridin-2-ylmethyl)ethane-1,2-diamine (c2): The c1 (3 g, 6.60 mmol) was dissolved in 100 mL ethanol. Then, hydrazine monohydrate (0.825 g, 6.60 mmol) was added to the above solution. After that, the solution was refluxed for 3 h, where a white precipitate was observed. To the mixture, 20 mL 10 M HCl was added and refluxed for another 2 h. The mixture was concentrated under reduced pressure and partitioned by water and chloroform. The aqueous layer was made basic by 20% (w/w) NaOH. A brown oil was separated. It was extracted with CHCl3 (50 mL × 4) and the organic layer was dried over Na2SO4. The organic solvent was removed by a rotatory evaporator to yield the product as a yellow oil (0.840 g, 4.3 mmol, 65%).1H NMR (400 MHz, CDCl3): δ = 8.53 (d, J = 4.05 Hz, 1H), δ = 7.66 (t, J = 7.6 Hz 1H), δ = 7.43 (d, J = 7.8 Hz, 3H), δ = 7.16 (t, J = 6.0 Hz, 3H), δ = 3.76 (s, 2H), δ = 2.77 (t, J = 5.9 Hz, 4H), δ = 2.60 (t, J = 6.6 Hz, 4H), δ = 1.79(s, 4H). Selected IR frequencies (ATR, cm−1): 3362(w, νN-H), 3280(w, νN-H), 3051(w), 3010(w), 2936 (m), 2813(m), 1588(vs), 1568(m), 1472(m), 1361(m), 1045(m), 858(m), 754(m). 
[image: image1.emf] D:\RCM\L102.0          RCM_L102          Instrument type and / or accessory21-12-2023

3064.542981.752941.68 2825.55 1771.511703.031614.231598.161590.181570.681467.011432.111393.061372.081326.401240.161188.531171.441082.721042.161009.63

973.60940.91872.22847.17790.00758.64715.08614.96528.83500.98447.09405.32376.56

500 1000 1500 2000 2500 3000 3500

Wavenumber cm-1

20

40

60

80

100

Transmittance [%]

  Page 1/1


Figure S1: FTIR of spectrum of powder sample of c1 at RT using diamond ATR.
[image: image2.emf] D:\RCM\L105_05-01-24.0          L105          Instrument type and / or accessory05-01-2024

3362.643280.98 3051.613010.042936.57 2813.67 1588.821568.381541.491521.551507.681472.781456.891432.931396.291361.611306.241266.641147.761091.861073.481045.68

993.94858.03754.14730.23635.92613.71566.28517.78457.74404.00375.46355.75

500 1000 1500 2000 2500 3000 3500

Wavenumber cm-1

40

50

60

70

80

90

Transmittance [%]

  Page 1/1


Figure S2: FTIR of spectrum of liquid sample of c2 at RT using diamond ATR.
[image: image3.jpg]L102CDCI3 1D 1H 12/01/23

S
N/

N (0]
NI\—N
o) o

i

%E—

[39625_

[ppm]

[rell




Figure S3: 1H NMR spectrum of c1 in CDCl3 at RT.
[image: image4.jpg]L105CDCI3 1D 1H 12/01/23

hhhhhhhhhhhhhhhhhhh

N TT I

[ppm]

frel





Figure S4: 1H NMR spectrum of c2 in CDCl3 at RT.

[image: image5.emf] D:\RCM\L105+salicyaldehyde_05-01-24.0          L105+salicyaldehyde          Instrument type and / or accessory05-01-2024

3063.303054.463007.912939.892927.692896.412885.992847.952823.03 1631.171586.321495.921460.291433.431417.121370.941339.301278.521208.251150.721116.201045.261028.04

994.04970.79939.92893.85848.78754.30736.48658.60640.39614.17557.15493.58456.91427.21400.81376.30366.08

500 1000 1500 2000 2500 3000 3500

Wavenumber cm-1

50

60

70

80

90

100

110

Transmittance [%]

  Page 1/1


Figure S5: FTIR spectrum of liquid sample of H2L at RT using diamond ATR.
[image: image6.jpg]L106 CDCI3 1D 1H 12001/23

SERTRAREARNEE
EELR TR ]
et »»h»ThThTT»VUlﬁh»hh'{»hL 4 "1
S ey

a c

%iE i

1

5 e

ppm]




Figure S6: 1H NMR spectrum of H2L in CDCl3 at RT.


[image: image7.emf]100 200 300 400 500 600 700

0

100

 

 

%

m/Z

403.2212

425.2076


Figure S7: ESI-Mass spectrum of H2L in MeOH at RT.
[image: image8.emf] C:\Users\Admin\Documents\Bruker\OPUS_8.7.31\DATA\MEAS\L106+Cu(H2O)6(ClO4)2.0          L106+Cu(H2O)6(ClO4)2          Instrument type and / or accessory17-04-2024

3076.33 2962.182940.402920.592873.51 1630.241599.641530.581465.751444.391399.811343.681313.151292.211194.181150.861066.68

975.50927.88898.28861.14758.37 619.55505.94465.81420.42380.33365.79

500 1000 1500 2000 2500 3000 3500

Wavenumber cm-1

65

70

75

80

85

90

Transmittance [%]

  Page 1/1


Figure S8: FTIR spectrum of the powder sample of 1 at RT using diamond ATR.
[image: image9.jpg]



Figure S9: Snapshot of the microcrystalline 1.


[image: image10.emf]200 400 600 800 1000 1200

0

100

464 465 466 467 468 469 470 471

0

100

 

 

%

m/Z

 

Theoritically

 

 

experimental

 

 

 

403.2198

464.1508

%


Figure S10: ESI-Mass spectrum of 1 in methanol solvent at RT. Peak at m/z = 403.2198, and 464.1508 corresponds to [(H2L)+H]+, [Cu(HL)]+, Inset: Isotopic mass distribution, experimental (red trace) and simulated (black trace) of the molecular peak [Cu(HL)]+.

[image: image11.emf]-1.5 -1.0 -0.5 0.0 0.5 1.0 1.5

20

10

0

-10

-20

-30

-40

 

 

I

(



A

)

E(V) vs SHE

0.840 V


Figure S11: Cyclic voltammograms of 1mM solution H2L Ligand in acetonitrile solvent containing 0.1 M [(n-Bu)4N]ClO4 as the supporting electrolyte at 298 K with a 3 mm diameter glassy carbon working electrode using non-aqueous Ag/Ag+ as the reference electrode at a scan rate of 100 mV s−1.

[image: image12.emf]0.00

0.25

0.50

0.75

1.00

200 300 400 500 600 700 800

0

1

2

3

4

 



 X 10

-3 

(

mol

-1

cm

-1

)

 

 

Wavelength(nm)



 X 10

-3 

(

mol

-1

cm

-1

)

 

 

605

374

305

265

245


Figure S12: UV-Vis spectrum of 1 in acetonitrile solvent.

[image: image13.emf]0 20 40 60 80 100 120 140

0

20

40

60

80

time(min)

 

 

 

Charge(C)

----Blank at pH 4.6

---- in presence of complex 1 at pH 4.6


Figure S13: Extended controlled potential electrolysis of 1 (10.0 M) in 0.1 M phosphate buffer at pH 4.6, showing cumulative charge over time for applied potentials of -1.5 V over 130 minutes and the control experiment in the absence of catalyst at -1.5 V (black).

[image: image14.emf]200 300 400 500 600 700 800

0.00

0.25

0.50

0.75

1.00

200 300 400 500 600 700 800

0

1

2

3

4



 × 10

-3 

(

mol

-1

cm

-1

)

 

 

---- pH 7

---- pH 4.6

---- pH 2.5

---- after electrolysis at pH 2.5

Wavelength(nm)



 × 10

-4 

(

mol

-1

cm

-1

)

 

 

280

625

355

325

255

235

220

210


Figure S14. UV-Vis spectra of 1 in different aqueous pH medium: black (pH 7), red (pH 4.6) and green (pH 2.5) traces. Blue trace shows that the reduction of CuII to CuI at a constant potential of -0.430 V at pH 2.5.


[image: image15.emf]2500 2000 1500 1000 500

1593

1599

1625

 

 

% T

Wavenumber(cm

-1

)

1630


Figure S15: FTIR spectrum of the powder sample of 1 and its one-electron reduced species.

[image: image16.emf]4000 3500 3000 2500 2000 1500 1000 500

1340

1293

1429

1531

 

 

 

Wavenumber(cm

-1

)

1635

1595


Figure S16: DFT optimized FTIR spectrum of 1.

[image: image17.emf]4000 3500 3000 2500 2000 1500 1000 500

1433

1527

1590

 

 

Wavenumber(cm

-1

)

1629


Figure S17: DFT optimized FTIR spectrum of one-electron reduced form of 1.

[image: image18.emf]+e

-1

-

6

.

7

8

 

k

c

a

l

 

m

o

l

-

1

[Cu

II

(HL)]

+

[Cu

I

(HL)]

0

[Cu

I

(HLH)]

+

[Cu

I

(HLH)]

0

+

e

-

1

+H

+

+

H

+

+

 

e

-

1

H

2

[Cu

0

(HLH)]

-

[Cu

I

(H)(HLH)]

0

+

e

-

1

+0.20 kc

almol

-1

+

8

.

5

7

k

c

a

l

 

m

o

l

-

1

-

1

3

.

3

1

 

k

c

a

l

 

m

o

l

-

1


Figure S18: Electrocatalytic mechanism of H2 generation by 1 at pH 2.5.
1

_1798387505.bin

_1811069014.bin

_1811080788.bin

_1799232257.cdx

_1799320204.bin

_1798470149.bin

_1777358148.bin

_1777872621.bin

_1777398802.bin

_1776621465.bin

