Supplementary Information for

Observation of quantum phase transition and tunable giant Griffiths phase in twisted trilayer graphene

Phanibhusan S. Mahapatra,1 Haining Pan,2 Kenji Watanabe,3

Takashi Taniguchi,4 J.H. Pixley,2, 5 and Eva Y. Andrei,1∗

1 Department of Physics and Astronomy, Rutgers the State University of New Jersey, 136 Frelinghuysen Rd, Piscataway, New Jersey 08854, USA

​2Center for Materials Theory, Rutgers University, 136 Frelinghuysen Road, Piscataway, NJ 08854, USA

3 Research Center for Functional Materials, National Institute for Materials Science, Namiki 1-1, Tsukuba, Ibaraki 305-0044, Japan

4 International Center for Materials Nanoarchitectonics, National Institute for Materials Science, Namiki 1-1, Tsukuba, Ibaraki 305-0044, Japan

5 Center for Computational Quantum Physics, Flatiron Institute, New York, New York 10010, USA

∗To whom correspondence should be addressed, E-mail: eandrei@physics.rutgers.edu

- Quantum anomalous metal phase

Fig. S1a shows the scanning electron microscope (SEM) image of the superconducting channel, highlighting the high aspect ratio of the channel. Fig. S1b shows the saturation of the sheet resistance Rs at low T at finite magnetic fields (B⊥). The apparent saturation has been a topic of much debate due to the sensitivity of the finite resistance state to the various external measurement conditions. Measurements in superconducting NbSe2 flakes suggests that the magnetoresistance in the anomalous metal phase is strongly sensitive to the circuit impedance due to dissipative coupling1. We verify this by changing the impedance in the circuit, which is series resistor that converts ac voltage (lock-in amplifier) to a constant current source with Iac=VLockinRseries and Rseries≫Rsample. For the two configurations depicted in Fig. S1c, the ac excitation current is the same (=500 pA) but the circuit impedance is varied. As evident, we do not observe any change between the two configurations in magnetoresistance Rs. Fig. S1d shows the comparison of Rs as a function of B⊥ with and without external RC filters with cut-off frequency f~ 1000 Hz at -3 dB attenuation. This suggests that the observed metallic state is not manifested due to coupling of the vortex lattice to external RF radiation2,3. Fig. S1e and S1f show the attenuation (=10logVoutVin) as a function of the excitation frequency f for the internal and externals filters, respectively.

Fig S1: (a) SEM image of the device. (b)  Sheet resistance Rs vs inverse temperature T-1 for different  B⊥ values at ν=2.25. (c) Sheet resistance Rs vs B⊥ for two different series resistors. (d)  Comparison of Rs vs B⊥ with and without external RC filters at ν=1.85. Attenuation vs excitation frequency for (e) internal RLC filters and (f) external RC filters.

- Quantum Interference effects and Weak localization

Fig. S2a shows the sheet resistance Rs as a function of ν for different temperatures. The aperiodic but repeatable oscillations in Rs are signatures of universal conductance fluctuations (UCF) due to quantum interference effects around impurity scattering 4. The oscillations gradually diminish at higher temperature since the phase coherence length Lϕ decrease at high T.  Another manifestation of quantum interference effects can be observed through weak localization (WL) where the Rs (averaged within doping window ν=1-1.25) shows a sharp decrease at low B⊥ (Fig. S1b).

The magnetoresistance correction from the weak localization can be expressed as 5,6

ΔRs=-e2Rs2πℏFBBϕ-FBBϕ+2Biv -2FBBϕ+B*#S1

Where e is the electronic charge, ℏ=h/2π , Bϕ is the phase breaking magnetic field, and Biv and B* are characteristic magnetic field scales for inter valley and intra valley scattering. The phase coherence length can be extracted from Bϕ as Lϕ2=ℏ/eBϕ . A fit to the Eq. S1 suggests Lϕ∼500 nm at 65 mK, which is in the order of the sample dimensions (∼μm). In contrast, Fig. S2c shows a positive magnetoresistance at ν=2.125 and T=2 K, which is a signature of weak antilocalization (WAL). A similar T-dependent transition from WL to WAL has been previously seen in graphene and can be attributed to the different scattering scenarios7.  The fitted Lϕ∼16 nm at 2K, which is substantially reduced from its value at low T.

Fig S2: (a) Sheet resistance Rs vs ν for different T. (b) Change in Rs (averaged over a doping window ν=1-1.25) as a function of B⊥ at T=65 mK. (c) Change in Rs as a function of B⊥ at a fixed ν=2.215 and T=2 K.  The solid lines in (b) and (c) are a fit to theoretic model of the weak localization in graphene.

- Global phase breaking boundary from bias-current dependent transport

To identify the global phase breaking boundary in B-T phase space, we identify the corresponding value of the temperature T for which the sharp central peak (between Idc∼±2 nA) disappears. The procedure is then repeated for several different magnetic fields in the vicinity of the phase transition.

Fig S3: (a) –(g) Dynamic resistance dV/dI vs bias current Idc for different T at ν=2.25 and B⊥=280, 300, 320, 340, 360, 380 and 400 mT, respectively. The curves are offset for better clarity.

- Nonequilibrium effects in the weakly localized state

Increasing Idc increases the bias energy =eIdcR, where R is the total resistance of the channel. For example, at Idc=1 nA, the bias energy is ≈10.7 μeV compared to the thermal energy at base temperature (~ 60 mK), kBT≈5.8 μeV. Such conditions (eV>kBT) broadens the energy of the incoming and outgoing interfering paths thus enhances the dephasing. This suppresses the localization of the wavefunction and reduces the total resistance. Previous experiments in graphene8 suggests that under the dephasing in nonequilibrium condition, the change in resistance (ΔR) should follow a logarithmic decrease, ΔR∝logIdc. In contrast, the expected change resistance in should follow ∝Idc2 for local Joule heating. Our experimental transport data (Fig. S4a and Fig. S4b) corroborates the former, indicating a novel dephasing mechanism from the nonequilibrium measurement conditions.

Fig S4: (a) dV/dI as function of the bias current Idc at T=65 mK, ν=2.25 and B⊥=600 mT. (b) The change in dV/dI as a function of Idc in linear-log scale. The red and blue squares represent the change in dynamic resistance ΔdVdI for positive and negative Idc values, respectively. The black and the green dashed lines show the logIdc and Idc2 dependence as reference, respectively.

- Infinite random fixed point and finite temperature scaling (FTS)

In this section, we first derive the activated dynamical scaling form for the infinite randomness fixed point used in Fig. 3b based on the conventional (for a non-Griffiths continuous phase transition) scaling form used in Fig. 3c within a temperature window and then explain the numerical details to implement this finite temperature scaling using nonlinear least-square minimalizations.

For a typical continuous phase transition induced by the tuning parameter λ, the correlation length ξ diverges algebraically at the critical point λc as ξ∼λ-λc-ν . In the finite system, the IR cutoff restricts the correlation length to be at most the system size L, and therefore leads to a typical finite size scaling of Fλ-λc L1ν, where F is a universal function independent of the system parameters. In a dynamical system, the dynamical exponent z is defined as t~Lz, and therefore leads to a temporal version of the scaling form of Fλ-λc t1νz.

In the finite temperature field theory, we can intuitively relate the temperature T with the inverse of the time t, due to the Wick’s rotation in the Euclidean metrics. Therefore, we can define the following temporal scaling form Fλ-λc T-1νz. With the tuning parameter being the out-of-place magnetic field B⊥, we obtain the scaling of the resistance Rs~B-Bc T-1νz as used in Fig. 3c.

In the Griffiths phase, the spacetime becomes extremely asymmetric, and the temporal varies much slower than the spatial dimension, therefore, we relate the dynamical exponent z with the a so-called activated exponent ψ as z∼Lψ~B-Bc-νψ≡kB-Bc-νψ. Substituting the dynamical exponent z into the previous scaling form and, we obtain the following scaling form

logRs~logB-Bc-kB-BcνψlogT#1

Here, given the estimate of νψ~O(1), the second term is much larger than the first term in Eq. (1), and therefore, we can safely ignore the first term and which, at the same time, also reduces the fitting parameters by one, k, namely, the final activated dynamical scaling form used in Fig. 3b is

logRs~B-BcνψlogT.#2

With the scaling form Eq. (1) or (2), we perform the finite temperature scaling to the experimental data with a magnet field and resistance Bi , Rs,  i under a specific temperature Ti , in order to extract the critical field Bc, and critical exponent zνB.

Based on the finite temperature scaling ansatz in Eq.1, we can define the following loss function,

χ2=i=1NRs,i-Rs,i'2 #3

where N is the total number of data points with different Bi,Ti, and Rs,i' is the linear interpolation between Rs,i  and Rs,i+1 (with Rs,i being sorted in ascending order), i.e.,

Rs,i'=Rs,i-1+Rs,i+1-Rs,i-1Bs,i+1-Bs,i-1 Bs,i-Bs,i-1 #4

We minimize the loss function Eq.2 using the Levenberg-Marquardt algorithm9 10 provided by the Python package  lmfit11 to find the best fit of Bc and zνB.

The error bars of the critical point Bc and the critical exponent zνB are estimated by first choosing a threshold of 1.3 times the minimal loss function χmin2as an operational definition, and then plotting the contour of the loss function Eq.2 as the function of different choices of Bc and zνB near the best fit values, and finally taking the extents of the 1.3χmin2-contour in the parameter space of Bc,zνB on both dimensions as the error bars.

Finally, we present some typical 1.3χmin2-contour (yellow curves) in Fig. S5

Fig.S5: Typical examples of finite temperature scaling following Eq. (1) on the top row, and the spatial profile of the loss function in Eq. (3) with 1.3χmin2-contours on the bottom row (yellow curves). The optimal set of parameters is at argminχ 2 labeled by the red cross. Different columns are for different ranges of temperature (in mK) windows as shown in the legend on the top row.

References:

1	Banerjee, A., Mohapatra, A., Ganesan, R. & Kumar, P. S. A. Restoring Superconductivity in the Quantum Metal Phase of NbSe2 Using Dissipative Coupling. Nano Letters 19 (2019). https://doi.org/10.1021/acs.nanolett.8b04538

2	Dutta, S. et al. Extreme sensitivity of the vortex state in a-MoGe films to radio-frequency electromagnetic perturbation. Physical Review B 100, 214518 (2019). https://doi.org/10.1103/PhysRevB.100.214518

3	Tamir, I. et al. Sensitivity of the superconducting state in thin films. Science Advances 5, eaau3826 (2019).

4	Morozov, S. V. et al. Strong Suppression of Weak Localization in Graphene. Physical Review Letters 97, 016801 (2006). https://doi.org/10.1103/PhysRevLett.97.016801

5	McCann, E. et al. Weak-Localization Magnetoresistance and Valley Symmetry in Graphene. Physical Review Letters 97 (2006). https://doi.org/10.1103/PhysRevLett.97.146805

6	Tikhonenko, F. V., Horsell, D. W., Gorbachev, R. V. & Savchenko, A. K. Weak Localization in Graphene Flakes. Physical Review Letters 100 (2008). https://doi.org/10.1103/PhysRevLett.100.056802

7	Tikhonenko, F. V., Kozikov, A. A., Savchenko, A. K. & Gorbachev, R. V. Transition between Electron Localization and Antilocalization in Graphene. Physical Review Letters 103 (2009). https://doi.org/10.1103/PhysRevLett.103.226801

8	Somphonsane, R. et al. Universal scaling of weak localization in graphene due to bias-induced dispersion decoherence. Scientific Reports 10, 5611 (2020). https://doi.org/10.1038/s41598-020-62313-3

9	Levenberg, K. A Method for the Solution of Certain Non-Linear Problems in Least Squares. Quarterly of applied mathematics 2, 164--168 (1944).

10	Marquardt, D. W. An Algorithm for Least-Squares Estimation of Nonlinear Parameters. Journal of the society for Industrial and Applied Mathematics 11, 431--441 (1963).

11	Newville, M., Stensitzki, T., Allen, D. B. & Ingargiola, A. LMFIT: Non-Linear Least-Square Minimization and Curve-Fitting for Python. Astrophysics Source Code Library, ascl--1606 (2014).