Supplementary Information

Programmable and somatosensory thermoresponsive soft robots

Antonia Georgopoulou1,2, Malena Aguiriano Calvo1,3, Lorenzo Lucherini1, Sudong Lee3, Josie Hughes3, Esther Amstad1,2

1) Soft Materials Laboratory, Institute of Materials (SMaL), École Polytechnique Fédérale de Lausanne, 1015 Lausanne, Switzerland.

2) Swiss National Center for Competence in Research (NCCR) Bio-inspired Materials, University of Fribourg, Chemin des Verdiers 4, 1700 Fribourg, Switzerland.

3) CREATE Lab, Institute of Mechanical Engineering, École Polytechnique Fédérale de Lausanne, 1015 Lausanne, Switzerland.

E-mail: esther.amstad@epfl.ch

Fig. S1. Schematic illustration of the preparation of the actuators based on A. double network bulk and B. DNGH hydrogels.

Fig. S2. Stress-strain curves of the DNGH-A composed of PNIPAM fragments containing 1 wt% (blue), 2 wt% (red) and 4 wt% (green) MBA crosslinker.

Fig. S3. Optical micrographs of A. PNIPAM microgels incubated in a NIPAM containing aqueous solution B. PAMPS microgels incubated in a AAm/PEDOT:PSS containing aqueous solution 
C. PAMPS microgels incubated in an aqueous solution containing AAm, PEDOT:PSS and ZnCl2 (Scale bars 100 µm). D. The average diagonal length derived from A,B,C.

Fig. S4. A. Timelapse of composite strips immersed in 55°C water. The DNGH-S contains 2 wt% (S), 3.5 wt% (M) and 5 wt% (H) MBA crosslinker (scale bar 5 mm). B. Evolution of bending angle with time of composite strips immersed in 55°C water. The DNGH-S contain 2 wt% (blue), 3.5 wt% (red) and 5 wt% (green) MBA crosslinker. C. Stress-strain curves of DNGH-S containing 2 wt% (blue), 3.5 wt% (red) and 5 wt% (green) MBA crosslinker. D. The Young’s modulus as a function of the MBA crosslinker concentration in the microfragments.

Fig. S5. Temperature evolution of single network bulk PAAm gels as a function of the PEDOT: PSS concentration within them if subjected to 5V A. without and B. with 40 wt% ZnCl2.

Fig. S6. A. Volumetric change of PNIPAM strips containing 1 wt% MBA crosslinker as a function of temperature. B. Photographs of PNIPAM strips with (i, ii) 1 wt% and (iii, iv) 4 wt% MBA crosslinker at (i, iii) 25°C and (ii, iv) 50°C.

Fig. S7. Rheological properties of the PAAm precursor solution (orange), PAMPS/PAAm granular ink (purple) A. amplitude sweep and B. shear rate.

Fig. S8. Bode plots featuring the impedance (red) and phase (blue) obtained during impedance spectroscopy of A. PAMPS-PAAm DNGHs B. PAMPS-PAAm DNGHs functionalized with PEDOT:PSS (DNGH-S) C. PAMPS-PAAm DNGHs functionalized with PEDOT:PSS and Zn2+ (DNGH-H).

Fig. S9. Nyquist plots obtained with impedance spectroscopy for double network bulk (DN), bulk DN-H containing 40 wt% ZnCl2 and 0.027 wt% PEDOT:PSS and DN-S containing 0.027 wt% PEDOT:PSS.

Fig. S10. A. UV-VIS Spectra of the supernatant of jammed microgels used to fabricate DNGH-S (blue) and DNGH-A (red). B. Photographs of DNGH-S (left) and DNGH-H (right)-scale bar 1 cm
C. Photograhs of the supernatant jammed microgels used to make DNGH-S (left) and DNGH-H (right)-scale bar 1 cm.

Fig. S11. Piezoresistive sensor signal (blue), mechanical stress (purple) and strain (yellow) during the mechanoelectrical characterization of the DNGH-S with 5 wt% MBA, involving: A. Stress response and B. Relative resistance response during 10 cycles between 0-30% strain. C. Stress response and 
D. Relative resistance response during 10 cycles between 0-100% strain. E. Stress response and 
F. Relative resistance response during 5 cycles between 0-30% strain at maximum and minimum strain.

Movie 1. DNGH bilayers at 55°C with DNGH-S containing contain 2 wt% (S), 3.5 wt% (M) and 5 wt% (H) MBA crosslinker.

Movie 2. DNGH gripper with closed-loop control picking up an orange and a strawberry. The gripper is programmed to pick up the smaller strawberry thanks to its somatosensory feedback.