Supporting Information

A New Fluorescence Probe Based on Self-absorption for Detection of Co2+ and Viscosity

Huizhen WANGa*, Dingxin QIUa, Pengbo WANGb, Pei WUb, Kezhen GOUc, Yan TANGa, Guanjun CHANGd*

1. Experimental method:

1HNMR titration : Accurately weigh 3 portions of 20mg probe HDN and dissolve with 1.0mL DMSO-d6. Co2+ are 0.5, 1.0, and 1.5 equiv. of probe HDN, respectively.

Chitosan cross-linking reaction: 0.3 g of chitosan was dissolved in 90 mL 1.0% acetic acid solution. Then, 900 uL HDN (1.0 × 10-3 mol/L) was added and thoroughly stirred. Next, add 5.0 milliliters of this solution to each of the 9 beakers. Then, add 0.5, 1.0, 1.5, 2.0, 2.5, 3.0, 3.5, 4.0, and 4.5 mL of 10% glutaraldehyde aqueous solution to each beaker, stir until the crosslinking reaction is complete, and perform fluorescence testing separately.

2. The 1H NMR、13C NMR、IR、HR-MS of compound HDN

Fig. S1. 1H NMR spectrum of probe HDN.

Fig. S2. 13C NMR spectrum of probe HDN.

Fig. S3. Infrared spectrum of probe HDN.

Fig. S4. Infrared spectrum of probe HDN+Co2+.

Fig. S5. The mass spectrum of probe HDN

2 Spectroscopic research

Fig. S6. Fluorescence (a) and Uv-vis (b) spectra of probe HDN in different PBS/DMF systems (PBS/DMF=4:6; λex=360 nm).

Fig. S7. The Uv-vis response of probe HDN by adding Co2+ and other anions. (λex = 360 nm, PBS/DMF=4:6)

Fig.S8. Job’s plot of probe HDN-Co2+ (λex = 360 nm, PBS/DMF=4:6)