Electronic supplementary information (ESI)

Basicity Modification of the Yttrium oxide supported ruthenium nanoparticles catalysts to enhance catalytic performance for hydrogen production from ammonia decomposition
Ji Feng,1§ Ningbo Wan,3§ Xiaohua Ju,2 Lin Liu,2,4* Teng He,2,4, Liguang Bai,1 Xiaodong Zhao1
1Liming Chemical Research and Design Institute Co., Ltd, 69, Wangcheng Avenue, Luoyang 471000, China

2Dalian National Laboratory for Clean Energy, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China

3College of Food & Bioengineering, Henan University of Science and Technology, 263, Kaiyuan Avenue, Luoyang 471023, China
4Enter of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China
§These authors contributed equally to this work

E-mail: liulin@dicp.ac.cn

[image: image1.png](a) 160
——Ru/Y,0,
—@—Ru/5% K-Y,0,

—A—Ru/10% K-Y,0,

140+

120+

-1

3

cm g
—
o
o
[]

Volume adsorbed (

0 |} d |}

04 0.6 0.8

Relative pressure (P/P)

0.2

1.0

(b)

Intensity (a.u.)

10%K-Y,0,

Y. O

_—

100 200

300 400 500 600 700 800
Temperature (°C)




Figure S1 (a) Nitrogen sorption isotherms of Ru/Y2O3, Ru/5%K-Y2O3 and Ru/10%K-Y2O3 samples, (b) CO2-TPD profiles of Y2O3, 5%K-Y2O3 and 10%K-Y2O3 supports.

[image: image2.jpg]min'1)

-1

cat

Hydrogen production rate (mmol g

70

604

50 -

404

30-

20-

10-

0

] ——400°C

—€@—450 °C
—4— 500 °C

0

10000 20000 30000 40000 50000 60000

WHSV (mLg_ " h")





Figure S2 NH3 conversion plots at different temperatures as a function of WHSV over Ru/5% K-Y2O3 catalyst.

.

Table S1 The physiochemical properties of Ru/Y2O3, Ru/5%K-Y2O3 and Ru/10%K-Y2O3 samples.

	Samples
	Specific surface area (m2 gcat−1)
	Support weak basic sites (<330 ゜C) (mmol gcat-1)
	Support strong basic sites (>330 ゜C (mmol gcat-1)

	Ru/Y2O3
	52.3
	0.1
	0.27

	Ru/5%K-Y2O3
	49.7
	0.02
	0.46

	Ru/10%K-Y2O3
	49.1
	0.03
	0.42


Table S2 NH3 conversion over different supported Ru catalysts at 450 ºC (WHSV=30000 mL gcat−1 h−1).

	Catalyst
	Method
	Ru loading (wt. %)
	conversion (%)
	H2 formation rate

(mmol gcat−1 min−1)
	H2 formation rate

(mmol gRu−1 min−1)
	References

	Ru/Al2O3
	IMa
	10
	31.5
	9.7
	96.6
	[1]

	Ru/SiO2
	IMa
	10
	34.5
	10.6
	105.8
	[1]

	Ru/CNTs
	IMb
	4.8
	43.3
	13.3
	276.7
	[2]

	K‒Ru/CNTs
	IMb
	4.8
	97.4
	29.9
	622.4
	[2]

	Ru/MgO
	IMb
	4.8
	30.8
	9.4
	196.8
	[2]

	Ru/TiO2
	IMb
	4.8
	27.2
	8.3
	173.8
	[2]

	Ru/Al2O3
	IMb
	4.8
	23.3
	7.1
	148.9
	[2]

	Ru/AC
	IMb
	4.8
	28.7
	8.8
	183.4
	[2]

	Ru/MgO
	Polyol reduction
	2.8
	41.3
	12.7
	452.4
	[3]

	Ru/MgO
	DPc
	3.5
	56.5
	18.9
	545.2
	[4]

	Ru/Y2O3
	precipitation
	5.0
	83.7
	25.7
	513.5
	

[5] ADDIN EN.CITE 

	Ru@La-ZrO2
	IMa
	3.0
	40.0
	13.7
	456.7
	[6]

	K-Ru/Mg2Al-LDO
	IMa
	4.6
	42.7
	14.3
	310.9
	[6]

	Ru/c-MgO
	DPc
	2.9
	75.0
	25.1
	865.5
	[6]

	Ru/La0.33Ce0.67
	IMa
	1.8
	79.3
	26.5
	1472.2
	[6]

	Ru/c-Y2O3
	IMa
	2.8
	74.4
	24.9
	859.0
	[7]

	Ru/c-Y2O3
	IMa
	4.8
	93.9
	31.5
	656.3
	[7]

	Ru/5%K-Y2O3
	DPc
	2.8
	93.5
	31.4
	1072.1
	This work


a Prepared by wetness incipient impregnation with water as solvent.

b Prepared by wetness incipient impregnation with acetone as solvent.

c Prepared by deposition‒precipitation method.

Table S3 Quantitative results of H2-TPR plots of Y2O3, Ru/Y2O3 and Ru/5%K-Y2O3 samples.

	Samples
	H2 consumption quantities/mmol gcat-1

	
	<213 ゜C
	213~472゜C
	>472 ゜C

	Y2O3
	-
	-
	0.05

	Ru/Y2O3
	-
	1.78
	-

	Ru/5%K-Y2O3
	0.30
	1.24
	0.64


References 

[1]
S. F. Yin, B. Q. Xu, C. F. Ng, C. T. Au, Appl. Catal. B-Environ. 2004, 48, 237-241.

[2]
S. F. Yin, B. Q. Xu, W. X. Zhu, C. F. Ng, X. P. Zhou, C. T. Au, Catalysis Today 2004, 93-5, 27-38.

[3]
J. Zhang, H. Y. Xu, Q. J. Ge, W. Z. Li, Catal. Commun. 2006, 7, 148-152.

[4]
X. Ju, L. Liu, P. Yu, J. Guo, X. Zhang, T. He, G. Wu, P. Chen, Applied Catalysis B-Environmental 2017, 211, 167-175.

[5]
J. Feng, L. Liu, X. H. Ju, J. M. Wang, X. L. Zhang, T. He, P. Chen, Chemcatchem 2021, 13, 1552-1558.

[6]
T. A. Le, Y. Kim, H. W. Kim, S.-U. Lee, J.-R. Kim, T.-W. Kim, Y.-J. Lee, H.-J. Chae, Applied Catalysis B: Environmental 2021, 285.

[7]
J. Feng, N. Wan, X. Ju, L. Liu, L. Bai, X. Zhao, T. He, ChemCatChem 2025, 17, e202401314.



