Supporting Information

Folic acid grafted amphiphilic dextran-b-poly(ε-benzyloxycarbonyl- l-lysine) micelles for drug’s pH-responsive release

Ruoxi Huang, Yaxin Yi, Shiyu Zhang, Jiaxin Wang, Haikuan Yuan, Jie Lu*

College of Chemistry and Chemical Engineering, Shanghai University of Engineering Science, Shanghai 201620, China

* Corresponding author: 333 Long Teng Road, Shanghai 201620, China. Tel.: +86 21 67791216; fax: +86 21 67791214. E-mail address: lujie@sues.edu.cn.

Table S1. Molecular weight of block copolymers Dex-b-PZLL.

| block copolymers | Mn | Mw | Mw/Mn |
| --- | --- | --- | --- |
| Dex-b-PZLL10 | 11281 | 13650 | 1.21 |
| Dex-b-PZLL20 | 14217 | 16634 | 1.17 |
| Dex-b-PZLL30 | 17215 | 20309 | 1.18 |

Fig. S1. UV-vis absorption spectra of letrozole at different concentrations (a) and standard curve of letrozole (b).

Fig. S2. Variations of the absorbance of DPH at 350 nm with the copolymer concentration of FDP-1 (a), FDP-2 (b) and FDP-3 (c). The values of CMC denote the critical micelle concentration in aqueous medium.

Fig. S3. Particle size distribution of blank micelles FDP-2 (a), FDP-3 (c) and drug-loaded micelles LTZ/FDP-2 (b), LTZ/FDP-3 (d).