Supplementary

Superior Performance of SIFSIX-3-Cu in Direct Air Capture: A Comparative Study with Mg-MOF-74

| Figure S1. A comparison of GCMC and experimental adsorption of pure components onto SIFSIX-3-Cu at 298 K: (a) pure CO2 and (b) pure N2. |  |
| --- | --- |

Fig. S2 A plot of ln (1-q/q∞) vs. time to calculate MTC for CO2 in SIFSIX-3-Cu;  CO2:N2=10:90 mixture, 1 bar and 298 K

Fig. S3 A plot of ln (1-q/q∞) vs. time to calculate MTC for N2 in SIFSIX-3-Cu at 1 bar and 298 K

took place at 0.01 bar and 398K.

Figure S4. Cycle CO2 uptake curves for CO2 adsorption on SIFSIX-3-Cu. The adsorption was occurred at 1.25 bar, 298K, with a CO2 concentration of 400ppm in N2 and a feed flow rate of 20mL min−1. The subsequent desorption step took place at 0.01 bar and 373K

Figure S. 5 Cycle CO2 uptake curves for CO2 adsorption on Mg-MOF-74. The adsorption was occurred at 1.25 bar, 298K, with a CO2 concentration of 400ppm in N2 and a feed flow rate of 20mL min−1. The subsequent desorption step took place at 0.01 bar and 373K

Tables S1  Packed bed geometry and  characteristics of SIFSIX-3-Cu bed.

| Parameter | Value | Unit | Description |
| --- | --- | --- | --- |
| Hb | 0.027 | m | Height of adsorbent layer |
| Wt | 0.005 | m | Wall thickness used of bed |
| Db | 0.004 | m | Internal diameter of adsorbent layer |
| Ei | 0.25 | m3 void/m3 bed | Inter-particle voidage |
| Ep | 0.4 | m3 void/m3 bead | Intra-particle voidage |
| RHOs | 1400 | kg/m3 | Bulk solid density of adsorbent |
| Rp | 1.00E-04 | m | Adsorbent particle radius |
| SFac | 1 | n/a | Adsorbent shape factor |
| MTC(*) |  |  |  |
| MTC("CO2") | 6.00E-04 | 1/s | Constant mass transfer coefficients |
| MTC("N2") | 4.5E-04 | 1/s | Constant mass transfer coefficients |
| b(*) |  |  |  |
| b(1,"CO2") | 4.19E-09 | n/a | Isotherm parameter |
| b(1,"N2") | 4.83E-07 | n/a | Isotherm parameter |
| b(2,"CO2") | 6338 | n/a | Isotherm parameter |
| b(2,"N2") | 1870 | n/a | Isotherm parameter |
| b(3,"CO2") | 1.54E-06 | n/a | Isotherm parameter |
| b(3,"N2") | 1.61E-04 | n/a | Isotherm parameter |
| b(4,"CO2") | 6339 | n/a | Isotherm parameter |
| b(4,"N2") | 1870 | n/a | Isotherm parameter |
| Direction | 0 | n/a | Specified flow direction (self determined: 0, forward: 1) |
| Cps | 1000 | J/kg/K | Adsorbent specific heat capacity |
| DH(*) |  |  |  |
| DH("CO2") | -54000 | kJ/kmol | Constant for heat of adsorption |
| DH("N2") | -15500 | kJ/kmol | Constant for heat of adsorption |
| Hw | 1.00E-06 | MW/m2/K | Constant heat transfer coefficient between gas and wall |
| Kg | 0.025 | W/m/K | Constant for the gas phase heat conductivity |
| Tamb | 398 | K | Ambient temperature |
| ap | 22500 | 1/m | Specific surface area of adsorbent |
| aHx | 0.2 | 1/m | External specific surface area of heat exchanger |
| UHx | 1.00E-05 | MW/m2/K | Overall (gas to medium) heat transfer coefficient |

Tables S2   Packed bed geometry and  characteristics of Mg-MOF-74 bed.

| Parameter | Value | Units | Description |  |
| --- | --- | --- | --- | --- |
| Hb | 0.027 | m | Height of adsorbent layer |  |
| Wt | 0.005 | m | Wall thickness used of bed |  |
| Db | 0.005 | m | Internal diameter of adsorbent layer |  |
| Ei | 0.25 | m3 void/m3 bed | Inter-particle voidage |  |
| Ep | 0.4 | m3 void/m3 bead | Intra-particle voidage |  |
| RHOs | 1400 | kg/m3 | Bulk solid density of adsorbent |  |
| Rp | 1.00E-04 | m | Adsorbent particle radius |  |
| SFac | 1 | n/a | Adsorbent shape factor |  |
| MTC(*) |  |  |  |  |
| MTC("CO2") | 0.121 | 1/s | Constant mass transfer coefficients |  |
| MTC("N2") | 0.30445 | 1/s | Constant mass transfer coefficients |  |
| b(*) |  |  |  |  |
| b(1,"CO2") | 0.0068 | n/a | Isotherm parameter |  |
| b(1,"N2") | 0.014 | n/a | Isotherm parameter |  |
| b(2,"CO2") | 0 | n/a | Isotherm parameter |  |
| b(2,"N2") | 0 | n/a | Isotherm parameter |  |
| b(3,"CO2") | 2.39E-06 | n/a | Isotherm parameter |  |
| b(3,"N2") | 1.27E-04 | n/a | Isotherm parameter |  |
| b(4,"CO2") | 5051 | n/a | Isotherm parameter |  |
| b(4,"N2") | 2165 | n/a | Isotherm parameter |  |
| b(5,"CO2") | 0.0099 | n/a | Isotherm parameter |  |
| b(5,"N2") | 0 | n/a | Isotherm parameter |  |
| b(6,"CO2") | 0 | n/a | Isotherm parameter |  |
| b(6,"N2") | 0 | n/a | Isotherm parameter |  |
| b(7,"CO2") | 1.70E-05 | n/a | Isotherm parameter |  |
| b(7,"N2") | 0 | n/a | Isotherm parameter |  |
| b(8,"CO2") | 2886.7 | n/a | Isotherm parameter |  |
| b(8,"N2") | 0 | n/a | Isotherm parameter |  |
| Direction | 0 | n/a | Specified flow direction (self determined: 0, forward: 1) |  |
| Cps | 1.00E-03 | MJ/kg/K | Adsorbent specific heat capacity |  |
| DH(*) |  |  |  |  |
| DH("CO2") | -25 | MJ/kmol | Constant for heat of adsorption |  |
| DH("N2") | -15.5 | MJ/kmol | Constant for heat of adsorption |  |
| Hw | 1.00E-06 | MW/m2/K | Constant heat transfer coefficient between gas and wall |  |
| Kg | 1.60E-07 | MW/m/K | Constant for the gas phase heat conductivity |  |
| Tamb | 398 | K | Ambient temperature |  |
| ap | 22500 | 1/m | Specific surface area of adsorbent |  |
| aHx | 0.2 | 1/m | External specific surface area of heat exchanger |  |
| UHx | 1.00E-05 | MW/m2/K | Overall (gas to medium) heat transfer coefficient |  |