Supplementary Information

Generation of continuous-wave 1-11 THz radiation with intersubband polaritonic metasurfaces

J.H. Krakofsky1*, M. Rieder1, S. Stich1, I. Lubianskii1, G. Böhm1, A. Köninger1,                      and M.A. Belkin1*

1 Walter Schottky Institute, Technical University of Munich, 85748 Garching, Germany.

*Corresponding authors. Emails: jonas.krakofsky@wsi.tum.de, mikhail.belkin@wsi.tum.de

- MQW heterostructure design and MQW absorption measurements

The large nonlinear response χzzz2 provided by multiple quantum well (MQW) semiconductor heterostructures originates from transitions between electron states, also known as electron subbands, that are quantized along the growth direction (z-axis). The energies of the corresponding intersubband transitions and their transition dipole moments can be engineered through the MQW heterostructure design.

Two MQW heterostructures were used for the experiments presented in the paper. The first MQW heterostructure, designed to produce maximum nonlinear response for THz DFG at around 8 THz, is described in Fig. 2(b) in the paper. The second MQW heterostructure was designed to have the maximum nonlinear response for THz DFG at around 5 THz. It is made of 23 repetitions of an In0.53Ga0.47As/GaAs0.51Sb0.49 heterostructure with the layer thicknesses of 8.0/4.9/3.0/5.6/5.0/8.0 where the thicknesses are given in nm, the GaAs0.51Sb0.49 ​barriers are shown in bold, and the underlined layer is doped at a nominal electron doping density of 3.31018 cm-3. The conduction band diagram and the computed electron wavefunctions for one period of this second heterostructure are shown in Fig. S1(a).

Both heterostructures were grown on semi-insulating InP substrates. The complete layer structure of the two grown wafers, including sacrificial etch-stop layers for substrate removal and contact layers to mitigate conduction band bending next to metal layers, is given below:

  - 350 µm semi-insulating InP substrate

  - 1500 nm In0.53Ga0.47As (etch stop 1)

  - 200 nm InP (etch stop 2)

  - 15 nm In0.53Ga0.47As nominally doped to 1×1019cm-3 (contact layer)

  - MQW heterostructure

  - 5 nm In0.53Ga0.47As layer nominally doped to 1×1019cm-3 (contact layer)

Following the heterostructure growth, absorption measurements were performed to confirm the designed energy levels spacing and to deduce the mid-infrared intersubband transition linewidths that are used in the calculations of χzzz2. To that end, we cleaved wafer pieces of about 1x1 cm2 in size, deposited metal Ti (5 nm)/Pt (10 nm)/Au (300 nm) on the top layer of the wafer, and mechanically polished the wafer facets into 45° wedges. Absorption spectroscopy of z-polarized intersubband transitions was then performed by coupling s- and p-polarized light through the polished facets at approximately 45° angle to the MQW layers as described, e.g., in Refs. [24,28,29]. The intersubband absorption coefficient αMQW is extracted by relating the transmitted intensities of p- and s-polarized light, Ipand Is using the following expression [24,28,29]:

| αMQW=142hMQWnplnIpIs | (S1) |
| --- | --- |

Here, hMQW ​ is the total height of the MQW stack and np​ is the number of passes of the optical beam through the MQW stack when the light is bouncing through the wafer sample [24,28,29].

The measured absorption spectra are shown in Fig. S1(b), together with the results of the fitting. By fitting the measurement results, we extracted the transition energies and transition linewidths for the mid-infrared transitions 1-0 and 2-0 (cf. Fig. 2(b) or Fig. S1(a)). A summary of the simulated and experimentally-measured transition energies (ℏω10, ℏω20, and ℏω21), transition dipole moments (ez10, ez20, and ez21), and transition linewidths (10 and 20) for the transitions between the ground and the first two excited electron states in the two MQW heterostructures are provided in Table S1. Also included in the table are the estimated transition linewidths for THz transitions between states 1 and 2 (21), the estimated γii values (γii=ℏTi, where Ti is the electron lifetime in state i) and the computed differences in the permanent dipole moments (ez00, ez11, and ez22) of the three electron subbands.

Figure S1. Design and characterization of the MQW structure. (a) Conduction band diagram and computed electron wavefunctions for one period of an In0.53Ga0.47As/GaAs0.51Sb0.49 multi-quantum-well heterostructure designed for giant nonlinear response maximized for 5 THz DFG. (b) 45° wedged absorption measurements of the intersubband transitions in the MQW samples designed for the maximum DFG nonlinearity for 8 THz generation and 5 THz generation. The energies of mid-infrared transitions and transition linewidths obtained from the fit are given in Table S1. (c) Computed absolute value of the intersubband nonlinear susceptibility |χzzz2| of the heterostructure shown in panel (a) as a function of THz difference frequency. Calculations assume a fixed pump 2 frequency 2=28 THz and a tunable pump 1 frequency 1=28-40 THz.

| Transition parameters | Sample 5 THz | Sample 9 THz |
| --- | --- | --- |
| ℏω10 ℏω20 ℏω21 | 116 meV (e), 116.1 meV (c) 128 meV (e), 128.0 meV (c) 12 meV(e), 11.9 meV (c) | 117.5 meV (e), 117.6 meV (c) 150.5 meV (e), 150.3 meV (c) 43 meV (e), 35.7 meV (c) |
| z10 z20 z21 | 1.45 nm (e), 1.52 nm (c) 1.5 nm (e), 1.65 nm (c) 4.7 nm (c) | 1.73 nm (e), 1.72 nm (c) 1.69 nm (e),1.70 nm (c) 4.9 nm (c) |
| γ10 γ20 γ21 | 9.5 meV (e) 8.5 meV (e) 5 meV (estimate) | 9 meV (e) 10 meV (e) 5 meV (estimate) |
| z00-z11 z00-z22 z11-z22 | 6.38 nm (c) 5.35 nm (c) 1.03 nm (c) | 4.71 nm (c) 4.55 nm (c) 0.16 nm (c) |
| γ11,γ22 | 2 meV (estimate) | 2 meV (estimate) |

Table S1. Intersubband parameters. The parameters marked with (e) are the experimentally measured values, the parameters marked with (c) are the values obtained from our 8-band k⋅p bandstructure computations; the parameters marked with (estimate) are estimates taken from literature values reporting similar MQW systems, particularly from Ref. [29].

- Calcination of χzzz2

The nonlinear susceptibility for difference-frequency generation (DFG) associated with intersubband transitions under z-polarized excitation is given by the sum-over-states expression [29,32]:

| χzzz2ωTHz=ω1-ω2 ,ω1,ω2=Ne2ε0ℏ lmnρllzln znm zml1Enl-ℏωTHz-iγnlEml-ℏω1-iγml +1Enl-ℏωTHz-iγnlEml+ℏω2-iγml+1Emn-ℏωTHz-iγmnEnl+ℏω1+iγnl+1Emn-ℏωTHz-iγmnEnl-ℏω2+iγnl+1Enm+ℏωTHz+iγnmEml-ℏω1-iγml+1Enm+ℏωTHz+iγnmEml+ℏω2-iγml+1Eml+ℏωTHz+iγmlEnl+ℏω1+iγnl+1Eml+ℏωTHz+iγmlEnl-ℏω2+iγnl | Almn Blmn Clmn Dlmn Elmn Flmn Glmn Hlmn |  | (S2) |
| --- | --- | --- | --- |

Here, Ne is the average MQW bulk doping density, ρll is the occupation probability of state l, ezij are the dipole matrix elements,Eij≡ℏωij=Ei-Ej are the transition energies, and γij are the corresponding dephasing rates. The eight terms in Eq. (S2) represent eight distinct resonance pathways contributing to the second-order nonlinear susceptibility obtained through second-order perturbation theory [32].

When applying Eq. (S2) to our system, the terms in Eq. (S2) can be grouped into a doubly resonant (DR) part and an optical rectification (OR) part [29]: χzzz2=χzzz,DR2+χzzz,OR2 [30]. The DR term is maximized when the pump frequencies ω1 and ω2  are tuned to match the transitions 0→1 and 0 →2, respictively,leading to a peak in nonlinear response at  ℏωTHz=E21.

| χzzz,DR2ωTHz,ω1,ω2=(D021+A102)+E021+G210=z02z21z102ε0ℏNeρ00-ρ11E21-ℏωTHz-iγ21E10-ℏω2-iγ10+ρ00-ρ22ℏωTHz-E21-iγ21E20-ℏω1-iγ20 | (S3) |
| --- | --- |

In addition to the DR term, the nonlinear susceptibility for difference-frequency generation also includes the OR term, which becomes significant in the low-frequency limit, i.e., as ω1-ω2→0.

| χzzz,OR2ωTHz,ω1,ω2=D011+E011+B101+ G110)+(H001+A020+C100+F100+(D022+E022+B202+G220)+(H002+A020+C200+F200) =12ε0ℏNeρ00-ρ11⋅ z012z00-z11ℏωTHz+2iγ20ℏωTHz+iγE10-ℏω2-iγ10ℏω1-E10-iγ20 +ρ00-ρ22 z022z00-z22ℏωTHz+2iγ20ℏωTHz+iγE20-ℏω1-iγ20ℏω2-E20-iγ20 | (S4) |
| --- | --- |

Here, zii=izi denotes the position expectation value of an electron in state i and γii=1Ti≈γ is a common average intersubband relaxation time [30]. While χzzz,OR2 dominates around ℏωTHz≪ E21  the doubly resonant χzzz,DR2 maximizes for ℏωTHz=E12.

Our two MQW systems are designed to maximize the value of |χzzz2| for THz DFG at 8 THz and 5 THz for the mid-infrared pump frequencies tunable between 28 and 40 THz as described in the paper. The computed value of  χzzz2=|χzzz,DR2+χzzz,OR2|  for the MQW structure shown in Fig. 2(b) is given in Fig. 2(c). The value of  |χzzz2| for THz DFG for the MQW structure shown in Fig. S1(b) is given in Fig. S1(c).

- Linear permittivity of the MQW

The values of MQW dielectric permittivity tensor εijω at mid-infrared and THz frequencies are required for the metasurface nanoresonator design and for the calculations of the overlap integral (Eq. (1) in the main text). We model the MQW permittivity as a diagonal tensor, with each principal component expressed as the sum of three distinct physical contributions as outlined below.

For the diagonal components of the εijω tensor in the plane of MQW layers (εxx=εyy), we write:

| εxxω=εyyω=ε∞+εFCω+εphω, | (S5) |
| --- | --- |

where ε∞≈11.8 is a constant value corresponding to the dielectric permittivity of the MQW sample excluding free electron and optical phonon contributions,  εFC is the free carrier contribution (FC), εphω is the optical phonon contribution.

We describe εFC with the Drude model:

| εFCω=-ε∞⋅ωp2ω2+iωγp, | (S6) |
| --- | --- |

where ωp​ is the plasma frequency of the semiconductor material, given by: ωp=Nee2ε0ε∞m* , where Ne is the charge carrier density, m*=0.044×me is the reduced effective electron mass, and the average charge carrier scattering rate is taken as γp= 5 THz.

The phonon-photon interaction is described by the sum over all binary combinations GaAs, GaSb, and InAs as given by Ref. [30,31,34]:

| εphω=-bεΔ,b⋅ωTO,b2ω2-ωTO,b2+iωγb | (S7) |
| --- | --- |

Here, ωTO,b, is the transverse optical phonon resonance frequency of the binary compound b, εΔ,b=εb∞-εb(0) is the phonon strength, and γbis the linewidth of the phonon absorption peak. The corresponding material parameters were obtained from Ref. [30,31,34]. All the linewidths γbwere set to 0.45×1012 rad/s to produce the best match to the experimental results.

The intersubband contribution εisbω is only present in the z direction and it replaces the FC contribution: εzzω=ε∞+εisbω+εphω, where

| εisbω=Neε0i,j(ρii-ρjj)e2zij2Eji-ℏω-iγji. | (S8) |
| --- | --- |

Here, Ne denotes the average volume-doping density, ρii is the diagonal element of the density matrix corresponding to state |i⟩. The values of zij,  Eij and γij are given in Table S1.

- Nanoresonator design of the metasurface optimized for 5 THz DFG

Our metasurface nanoresonators are engineered to maximize the nonlinear overlap integral defined in Eq. (1). Because the intersubband transitions in MQW heterostructures are polarized in the z-direction fields, the resonator must convert the incident x- or y- polarized pump light into a strong, localized Ez field (see, e.g., Fig. 3(a)). The H-shaped nanoresonator design described in the paper achieves this by supporting three distinct resonator modes – two modes resonant with each of the two pump wavelengths and a third mode resonant at the output THz frequency. The two mid-infrared resonator modes have a relative π-phase reversal of Ez in one end of the nanoresonator as shown in Fig. 3(a). This sign flip boosts the overlap integral because it produces a corresponding sign change in the induced THz nonlinear polarization along the THz nanoresonator antenna. At lower THz frequencies, the two mid-infrared pump wavelengths move closer together, making it increasingly difficult to implement a nanoresonator with separate resonances at the two pump frequencies. Therefore, for the metasurface optimized for THz DFG in the 4-6 THz spectral range, we use a Y-shaped nanoresonator that employs a single resonant mode to couple both mid-infrared pumps to the intersubband transitions in the MQW heterostructure.

The Y-shaped nanoresonator design details are given in Fig. S2(a,b,c) and details are given in the figure captions. To obtain the broad tunability, the resonator was designed with an internal angle at the top of the “Y” of 160°, which broadens its mid-infrared resonance.

Figure S2. Metasurface optimized for DFG at 4-6 THz. (a) Measured and simulated mid-infrared reflection spectra of the metasurface, displaying a broad mid-infrared resonance peak centered at around 10 m. (b) Schematic of the Y-shaped resonator design used for the metasurface, indicating the pump polarization along the y-axis and the THz polarization along the x-axis. The coordinate system is given in the figure. (c) Simulated electric field distribution at half the MQW height for the pump mode (the image is for vpump= 32 THz) and the resulting THz mode (the image is for vTHz=4.5 THz). The nanoresonator dimensions are ly=2442 nm, w=1100 nm, lTHz=9901 nm.                  (d) Scanning electron microscope image of the fabricated metasurface.

The Y-shape metasurface was patterned into 81 individual patterns, each measuring 350µm by 350 µm. Within this matrix we systematically varied both lTHz and ly (cf. Fig.S2(c)). The highest conversion efficiency was achieved for lTHz=9900 nm and ly=2440 µm which is in excellent agreement with our COMSOL Multiphysics simulation-based optimization predictions.

- Metasurface fabrication

Following the wafer growth, a metallic tri-layer made of Ti (5 nm) / Pt (80 nm) / Au (500 nm) is evaporated on both the grown MQW wafer and the host InP wafer. The sample and the host wafers are then placed on top of one another with metallized surfaces facing each other and thermocompressively bonded together at 320o C.  Following the thermocompressive bonding, the substrate of the bonded MQW wafer is selectively removed in concentrated HCl. The first etch-stop layer is then stripped in an H₃PO₄ / H₂O₂ solution, and the second etch-stop layer is removed in a 1:1 HCl:H₂O bath.

Nanoresonators are then patterned by electron-beam lithography (Elionix ELS-BODEN 100). A SiN hard mask is defined by fluorine/oxygen ICP-RIE (Oxford PlasmaPro 100), and the MQW nanoresonators are then etched with a Cl₂/Ar/H₂ ICP-RIE. The hard mask is subsequently stripped in a second F/O₂ ICP-RIE step.

Finally, the top metal is deposited on top of the nanoresonators by electron-beam evaporation of a Ti (5 nm) / Pt (10 nm) / Au (35 nm) tri-layer. A large source-to-sample distance is used to minimize sidewall metallization. Scanning electron pictures (SEM) of processed metasurfaces are shown in Fig. 4(a) and Fig S2(d).

- Collection efficiency of the presented setup configuration.

The details of the measurement setup are shown in Fig. S3(a). To relate the THz power measured at the detector to the power generated at the metasurface, we used an analytical model that treats the metasurface as an infinitesimally thin nonlinear layer. This approximation yields closed-form expressions for the THz far field, enabling us to calculate the mirror-system collection efficiency ηcoll and thus recover the THz power at the sample.

| ηcoll=WTHzDetector/WTHzSample | (S9) |
| --- | --- |

The far-field profile of the THz radiation is determined by the focal-spot sizes of the two mid-infrared pump beams, which are treated as Gaussian. Knife-edge measurements yielded the 1/e² radii w1  ​ and w2 ​ for the two mid-infrared pump lasers. Because the nonlinear signal is proportional to the product of the two optical fields, the generated THz beam can also be approximated as Gaussian, with a waist

| wTHz =w1 -2+w2 -2-1/2. | (10) |
| --- | --- |

In our setup, w1=45 µm and w2=60 µm, giving wTHz ≈36  μm.

We then treat the metasurface output as Fraunhofer diffraction from a Gaussian aperture of 1/e² radius of wTHz ​. In this formalism, the polar angle dependence of the intensity of the emitted THz radiation is given as

| Iθ∝Eθ2∝exp-2π2w02λ2sin2θ | (S11) |
| --- | --- |

The collection efficiency η  of a 90° off-axis parabolic mirror (OAP) used for THz radiation collimation is obtained as:

| η=0βIθsinθ dθ0π/2Iθsinθ dθ | (12) |
| --- | --- |

Our setup uses a 1.5-inch-diameter 0.8-inch focal length OAP, with the sample placed in the mirror focus (see fig. S3(a)). The mirror has a central through hole of 3 mm in diameter for focus in the mid-infrared pump beams. The power lost through the aperture of the hole is evaluated with a similar expression using Eq. (S11).

The net collection efficiency is calculated with the measured Gaussian-beam focal radii of our pump lasers is plotted in Fig. S3(b). For comparison, the collection efficiency corresponding to the use of the same OAP without a central through hole is also shown to highlight the fraction of power lost through the central hole.

Figure S3. Experimental setup and estimates of THz collection efficiency. (a) Laser 1 (Daylight Solutions MIRcat) and Laser 2 (Access Lasers L4-GL) are combined with a dichroic mirror (Spectrogon LP 10000) and expanded five-fold by a custom ZnSe Galilean beam expander (f₁ = 15 mm, f₂ = 75 mm). The expanded beam is focused onto the metasurface with an achromatic doublet lens through the 3 mm central bore in a 1.5-inch-diameter off-axis parabolic mirror (OAP, f = 0.8 in). The emitted THz radiation is collimated by the same OAP and is then refocused with another OAP without a hole onto a THz detector. (b) Calculated collection efficiency of the OAP next to the sample as a function of THz frequency. The solid curve describes our experimental conditions, the dashed curve shows the collection efficiency of the OAP with the same numerical aperture but without the central hole. A comparison of the two curves highlights the amount of THz power lost through the mirror center hole.