SUPPLEMENTARY INFORMATION

Geometry effect on the photocatalytic properties of LCD 3D-printed TiO2-based nanocomposites

Libera Vitiello1,†,*, Giuseppe Proietto Salanitri2,†, Paolo Maria Riccobene1, Maria Grazia Pia Musumeci3, Roberto Fiorenza3, Sabrina Carola Carroccio1

1CNR-IPCB Institute for Polymers, Composites and Biomaterials CNR-IPCB, Via Paolo Gaifami 18, Catania 95126, Italy

2Department of Industrial Chemistry “Toso Montanari”, University of Bologna, Via Piero Gobetti 85, 40129 Bologna, Italy

3Department of Chemical Sciences, University of Catania, V.le A. Doria 6, Catania 95125, Italy

*Corresponding author: libera.vitiello

@cnr.it (L. Vitiello)

† These authors contributed equally

Table of contents:

- Figures S1 – 5

- Tables S1 – 3

Fig. S1. Schematic representation of the 3D-printed model designed for the optimization of printing parameters. All dimensions are in millimetres.

Fig. S2. Dimensions of the three-dimensional macroscopic structures: wheel, gyroid and lattice.

Fig. S3. Clear UV resin loaded with different TiO2 NPs contents after 60 hours after preparation.

Fig. S4. Methylene blue concentration variation in dark conditions for samples containing 0%, 2.5%, 5%, and 10% TiO₂: (a) gyroid, (b) wheel, and (c) lattice. The dashed lines are guides for the eye.

Fig. S5. Photocatalytic degradation of methylene blue over time for the lattice (a) and wheel (c) samples with 0%, 2.5%, 5%, and 10% TiO₂; linear fit of the concentration variation during the first 6 hours of testing for the lattice (b) and wheel (d) samples. The dashed lines are guides for the eye.

Table S1. Temperature at 5% weight loss (T₅%), principal degradation peak temperature (Tₚₑₐₖ), and residue at 800 °C of the 3D-printed nanocomposites with different TiO₂ content.

| TiO2 [wt.%] | T5% [°C] | Tpeak [°C] | Residue [%] |
| --- | --- | --- | --- |
| 0 | 212 | 431 | 0.0 |
| 2.5 | 273 | 437 | 2.7 |
| 5 | 271 | 438 | 5.3 |
| 10 | 240 | 444 | 10.5 |

Table S2. EDX elemental mapping data for C, O and Ti in 3D-printed model sample loaded with different TiO2 contents.

| TiO2 [wt.%] | Weight Concentration [%] |  |  |
| --- | --- | --- | --- |
|  | C [%] | O [%] | Ti [%] |
| 0 | 90 | 10 |  |
| 2.5 | 49 | 36 | 15 |
| 5 | 43 | 39 | 18 |
| 10 | 32 | 37 | 31 |

Table S3. Printing parameters on Sonic Mini 8K for Phrozen Aqua 3D Printer Resin.

| Printing parameters |  |
| --- | --- |
| Layer height [mm] | 0.05 |
| Bottom layer count | 15 |
| Bottom exposure time [s] | 100 |
| Transition layer count | 5 |
| Transition type | Linear |
| Waiting mode during printing | Resting time |
| Rest time after retraction [s] | 3 |
| Bottom lift distance [mm] | 6 |
| Lifting distance [mm] | 6 |
| Bottom lift speed [mm/min] | 60 |
| Lifting speed [mm/min] | 60 |
| Bottom retract speed [mm/min] | 150 |
| Retract speed [mm/min] | 150 |