Supplementary Materials

Rectal Nanoparticulate-Hydrogel Delivery of Corticosteroid Altering Enterohepatic Metabolism and Clearance for Improved Drug Disposition

Rui Xue Zhang1, 2, *#, Weijia Lu2,#, Xu Yan2, Xudong Deng3, Runrun Wan2, Zhejun Song1, Xue-Ting Wang3, Tingting Cao2, Yan Chen1, Paul K.H. Tam1,*

1 Precision Regenerative Medicine Research Centre, and School of Pharmacy, Medical Sciences Division, Macau University of Science and Technology, Macau 999078, China

2 Institute of Medical Research, Northwestern Polytechnical University, 127 West Youyi Road, Xi’an, Shaanxi 710072, China

3 School of Life Sciences, Northwestern Polytechnical University, 127 West Youyi Road, Xi’an, Shaanxi 710072, China

# the authors contributing equally to this work

* Corresponding authors: zhangruixue@must.edu.mo;  pkhtam@must.edu.mo

S1. Materials

Budensonide-d8 (an internal standard) was purchased from GlpBio Technology Inc, USA. N-(3-Dimethylaminopropyl)-N-ethylcarbodiimide (EDC, 98%) were bought from Aladdin, China. Hydrochloric acid (HCl, 36.0~38.0 %) was from Sinopharm Chemical ReagentCo., China. Sodium hydroxide (NaOH, 97%) and D2O (99.9 atom %) was obtained from Macklin, China. 4% paraformaldehyde was purchased from HAT (Xi’an, China). Triton X-100 were bought from Solarbio (Beijing, China). For LC-MS analysis of drug plasma concentration, LiChrosolv® formic acid (FA), methanol (MeOH) and water were purchased from Merck (Darmstadt, Germany).

S2. Preparation and characterization of BD-LNP

S2.1 Preparation of BD-LNP. BD-LNP nanoparticles were prepared by ultrasonic emulsification based on the following the methods described by Miao, R. et al., [1]. To prepare the nanoparticles, the following steps were taken: First, 5 mg of BD drug, 20 mg of palmityl palmitate, and 30 mg of Compritol-ATO888 were weighed into a 15 mL test tube, followed by the addition of 20 μL of oleic acid at room temperature. After adding a magnetic stirrer, the sample was stirred at 85°C in a recirculating water bath (SC100, Thermo Scientific, USA) for 5 minutes. Subsequently, 400 μL of preheated ultrapure water (85°C) was added dropwise, and the mixture was stirred for an additional 5 minutes. Next, the magnetic stirrer was removed, and a handheld ultrasonic processor (Hielscher, Germany) was used to sonicate the nanosuspension at 85% power for 5 minutes. Then, 375 μL of a 10% (w/v) Poroxamer-188 solution was added dropwise, and the mixture was sonicated at the same power for another 5 minutes. Finally, the completed nanosuspension was quickly transferred to a test tube containing 4 mL of ice-cold ultrapure water. The mixture was briefly vortexed and then stored at 4°C for future use. For the preparation of Nile Red (NR)-labeled BD-LNP (NR-BD-LNP), 0.82 mg of NR was pre-spiked at the bottom of a 15 mL test tube, and the same procedure described above was followed.

S2.2 Characterization of BD-LNP. The prepared LNP was diluted 10-fold with ultrapure water. The particle size, polydispersity index (PDI), and ζ-potential of the LNP were measured using Zetasizer Nano ZS (Malvern Panalytical, UK). To determine the encapsulation efficiency (EE%) and drug loading (DL%) of BD-LNP, an indirect method was employed. Specifically, 500 μL of the LNP solution was added to an ultrafiltration centrifuge tube (3 kDa, Millipore, USA) and centrifuged at 14,000 ×g for 30 minutes. The filtrate was then mixed with acetonitrile at a ratio of 1:1 (v/v). The concentration of BD was calculated by measuring the absorbance at 254 nm using a multifunctional microplate detector (Spark, Tecan, Switzerland). The encapsulation efficiency (EE%) and drug loading (DL%) were calculated using the following equations.

EE%=1-BD Amount  in filtrateTotal  added BD amount×100%

DL%=BD mass loadedTotal excipient mass ×100%

S3. Synthesis and characterization of HA-2APBA

S3.1 Synthesis of HA-2APBA. 2APBA-modified HA (HA-2APBA) was obtained via a carbodiimide-mediated conjugation reaction between HA and 2APBA based on a reported method by Deng, X. et al., [2]. HA (600 mg) was dissolved in 300 mL of acidified water (pH 4.5-5). An aqueous solution of EDC·HCl (2 g) was added into the solution, and the pH was adjusted to 4.5-5 by the addition of 0.1 M HCl or NaOH solution. 2APBA·HCl (2 g) was added into the solution, and the pH of mixture was maintained at 4.75 by the addition of 0.1 M HCl or NaOH solution overnight. The reaction was stopped by the addition of 0.1 M NaOH solution to adjust the pH to 7.0. The modified HA was centrifuged at 12,000 rpm for 10 min, and purified by dialysis in a large excess of ultra-pure water using a prewashed dialysis bag (MWCO = 8,500 - 14,000 Da). The dialysis was stopped after 48 h, and the samples obtained from dialysis at different time points were freeze-dried.

S3.2 1H NMR characterization of HA-2APBA. HA-2APBA graft density in D2O (98 %) as the solvent was performed by 1H-NMR using a Bruker ADVANCE NEO 500 MHz spectrometer. Integration of the NMR signals arising from the anomeric protons of the PBA group (δ = 7.0 – 7.6) and protons of CH3 group (δ = 1.7 – 2.3) indicated a degree of substitution of 0.33 ± 0.07 moles of 2APBA per disaccharide repeat unit (Figure S1). The method for grafting 2APBA onto FITC-HA was the same as above.

Figure S1. 1H NMR spectra of HA-2APBA. The characteristic peak of methyl hydrogen was between 1.8 ppm and 2.2 ppm chemistry shift, and characteristic peak of benzene hydrogen on HA-2APBA was between 7.0 ppm and 7.6 ppm chemistry shift.

S4. Drug release of BD-LNP@Hydrogel

S4.1 HPLC-UV method for BD Quantification. concentrations in drug release study of BD-LNP@Hydrogel was assayed according to our previously established methods of HPLC-UV instruments (Alliance HPLC, Waters, USA) [3, 4]. The chromatographic conditions were as follows: a C18 column (5 μm, 4.6×250 mm, XAuqa C18, Beijing Xinchuang Science and Technology Co., Ltd.) was used, with a mobile phase consisting of 60% HPLC-graded acetonitrile and 40% of water (v/v) at a flow rate of 1.0 mL/min. The injection volume was 10 μL, and the detection wavelength was set at λ = 244 nm. A BD stock solution was prepared at a concentration of 32 μg/mL using the same mobile solvent. The stock solution was then diluted to concentrations of 16 μg/mL, 8 μg/mL, 4 μg/mL, 2 μg/mL, 1 μg/mL, and 0.5 μg/mL to create a standard curve. Linear regression analysis was performed using the concentration of BD as the horizontal axis and the area under the curve (AUC) of the response signal as the vertical axis. The resulting linear equation was y = 17400x - 4310, with a correlation coefficient squared (R²) of 0.999061. The standard curve ranged from 0.5 μg/mL to 32 μg/mL (Figure S2).

Figure S2. The standard curve of budesonide determined by HPLC-UV method.

S4.2 fitting drug release profile. Obtained drug release profile of BD-LNP@Hydrogel in PBS and SCF was fitted by Korsmeyer-Peppas model using DDSolver 1.0 [5]. Characteristic parameters were shown in Table S1, and fitted parameters in SCF were further substituted into Korsmeyer-Peppas equation, obtaining the following equation:

where F(t) was the amount of drug release, 9.866 (Kkp) was the release rate constant, and 0.35 (n) was the diffusion exponent in function of time (t).

Table S1. Characteristic parameters for fitting the drug release curve of BD-LNP@Hydrogel.

S5. Immunofluorescence staining of mice colon

Swiss rolling as well as tissue immunohistochemical staining were performed based on the methods described by Miao, R. et al., [1]. Healthy 8-week-old female C57BL/6N mice were sacrificed by cervical dislocation. The entire colon was carefully isolated, incised longitudinally along the mesenteric line, rinsed with 1×PBS (pH 7.4) and fixed with 4% paraformaldehyde. The colon was then rolled from the distal to the proximal end using the Swiss rolling technique. The colon rolls were fixed in 4% paraformaldehyde at 4 ℃ for 24 h and subsequently embedded in optimal cutting temperature (OCT) compound for the preparation of 5-μm frozen sections (SYD-K2080, Shenyang Yude Electronic Technology Co., Ltd.). The colon sections were placed on glass slides and rinsed twice with PBS. They were then fixed with 4% paraformaldehyde for 15 min at room temperature to prepare for immunohistochemical staining.

For immunohistochemical staining, colonic tissue sections were stained with fluorescein isothiocyanate (FITC) to label actin filaments and DAPI for nuclei. Briefly, the fixed colon sections were treated with 0.1% (v/v) Triton X-100 for 20 min to permeabilize the cell membranes. The sections were then incubated with FITC-conjugated phalloidin (diluted 1:100 in PBS containing 1% BSA and 0.1% Triton X-100) for 60 min at room temperature. After several rinses with 0.1% (v/v) Triton X-100, the sections were incubated with DAPI (diluted 1:1000 in distilled water) for 15 min at room temperature. The sections were rinsed twice with PBS and then visualized using confocal laser scanning microscopy (FV3000, Olympus, Japan).

S6. Analysis of BD and HP concentrations in biological matrix

S6.1 Drug extraction from plasma, urine and tissues. Briefly, 400 μL of pre-cooled methanol was added to 100 μL of plasma containing an internal standard (I.S.) Budensonide-d8. The solution was vortexed for 3 minutes to ensure complete protein precipitation. After centrifugation at 12,000×g for 2 min, the supernatant was transferred to a new tube and dried at room temperature using a vacuum concentrator (SpeedVac SPD1030, Thermo Fisher, USA). The dried sample was reconstituted by adding 50 μL of 75% methanol solution and vortexed thoroughly. Similarly, BD and HP in urine were detected using a direct dilution method. Briefly, 50 µL of urine was collected and dried at room temperature using the vacuum concentrator. Prior to analysis, the samples were reconstituted by adding 100 µL of 75% methanol solution.

To extract BD and its metabolite HP from tissues (liver and intestine), approximately 100 mg of tissue was fully homogenized in 1 mL ethanol using a tissue homogenizer (KZ-III, ServiceBio, China) at 70 Hz for 90 s, with the process repeated three times. One hundred μL of the homogenized tissue was transferred to a new tube, followed by spiking 50 μL of I.S. budensonide-d8. Subsequently, 1.6 mL of pre-cooled ethanol was added and the sample was shaken vigorously for 5 h at 4 °C. After centrifugation, the supernatant was transferred to a new tube, and dried using the vacuum concentrator at room temperature. For analysis, 100 µL of 75% methanol solution was added to reconstitute the samples, followed by vortex. To ensure the purity of the samples and the normal operation of the instrument, all the samples were centrifuged at 15,000 ×g for 10 min at 4 °C prior to analysis. The sample was then transferred to HPLC sample insert for drug concentration determination by LC-MS.

S6.2 LC-MS analysis of budesonide in plasma, urine and tissues. The concentrations of BD and HP in plasma, urine, and tissues were determined at predefined time points using liquid chromatography-mass spectrometry (LC-MS). The LC-MS system was coupled to an ultra-high performance liquid chromatography (UPLC) system (Vanquish™, Thermo Scientific, USA) and a mass spectrometry (MS) system (TSQ Altis™, Thermo Scientific, USA). The separation of BD and HP was performed on a Zorbax SB-C18 column (1.8 μm, 4.6 × 50 mm, Agilent, USA) using a gradient elution mode. The column temperature was maintained at 25 °C, with a flow rate of 0.3 mL/min and an injection volume of 5 μL. The mobile phases consisted of 1% (v/v) formic acid in water (A) and methanol (B), with the gradient profile detailed in Figure S3. The MS system was operated in negative ion mode using an electrospray ionization (ESI) source. The drugs BD, HP, and the internal standard BD-d8 were quantified in Selective Reaction Monitoring (SRM) mode, with the following mass transitions: m/z 437/323 for BD, m/z 377/323 for HP, and m/z 439/323 for BD-d8. The area under the curve (AUC) of the peaks for BD, HP, and BD-d8 was analyzed by Xcalibur (version 5.1, Thermo Scientific, USA).

Figure S3. A) Mobile phase composition in the programmed gradient elution; B) Representative extracted ion chromatogram of BD and HP; C) Calibration curve of the drug BD and HP in plasma; D) Calibration curve of the drug BD and HP in liver. The standard curves of BD and HP were prepared in the mice plasma and tissue, ranging from 2.5 ng/mL to 1000 ng/mL for BD and 2 ng/mL to 800 ng/mL for HP, respectively. These calibration curves were used to validate the quantification method, ensuring accurate determination of drug concentrations in different matrices. The extracted ion chromatograms (EIC) were used to monitor the specific mass-to-charge ratios (m/z) of BD and HP, providing a targeted approach for detecting these compounds.

S7. PBPK model fitting and simulation

S7.1 PK of a single bolus intravenously injected and gastric gavage Free-BD. All animal work were performed in line with the Animal Care Guidelines at the Institute of Medical Research (Xi’an, China), and approval was granted by the Institutional Animal Ethics Committee at Northwestern Polytechnical University (Date December 20, 2022/ No. 202201176). Healthy 8-week-old female C57BL/6N mice were fasted for 24 h with free access to water before experiment. For intravenous (i.v.) administration, free budesonide solution (Free-BD, 0.6 mg/ml in 10% DMSO solution) was injected as a single bolus into the jugular vein. For oral gavage, Free-BD was orally administered at BD dose of 3 mg/kg per mouse. The volume of dose injected was 100 μL. At designated time points, mice were anesthetized prior to withdrawal of whole blood and retrieval of organs (the entire gastrointestinal tract and liver) after perfusion with ice-cold 1×PBS. For the mice in the 24 h group of i.v. and oral administration, entire urinary content was collected in a metabolic cage. Blood was collected by cardiac puncture at the designed time points post administration, centrifuged at 3000×g at 4 ℃ for 10 min to obtain plasma (Heraeus Fresco 17 centrifuge, Thermo Scientific, USA). The tissues were weighed, frozen immediately in liquid nitrogen, and transferred to polypropylene tubes. All samples were stored at − 80 ℃ until analysis. After extraction from the blood and tissues matrix, the concentrations of the drug BD, the metabolite 16α-hydroxy-prednisolone (HP), and the internal standard budesonide-d8 were quantified by liquid chromatography-mass spectroscopy (LC-MS) (TSQ Altis™, Thermo Scientific, USA). Non-compartmental analysis of AUC∞ (area under the concentration-time curve to infinity) was estimated as sum of AUC0-t, calculated by using the trapezoidal rule, and AUCextrap derived by dividing the blood concentration of the last sampling point (Clast) by β, the terminal slope. The total body (blood) clearance (CLtotal) was calculated as Dose/AUC0-∞. Additionally, the systemic bioavailability (Fsys) was determined from the Dose-normalized ratio of AUC∞,oral/AUC∞,IV. All data were expressed mean ± SEM.

S7.2 Model fitting and simulation. Both fitting and simulation were performed by using ADAPT5 Systems Analysis Software (BMSR Biomedical Simulations Resource, USC, Version 5.0.53, Los Angeles, CA). PBPK model was applied to fit the concentration data of BD and HP in the plasma, liver and small intestine as well as cumulative secretion of BD and HP in the urine of mice following intravenous (i.v.) and oral (per os, p.o.) administration of Free-BD, with used literature parameters including the plasma and tissue volume (V in mL), organ blood flow rate (Q in mL/mim), intrinsic clearance for metabolite formation (CLintBD→HPin mL/min), unbound fraction of BD and HP in plasma (fup), and partition coefficient (KOT/BBD and KOT/BHP) [6, 29-34] summarized in table S2. Fitted drug release kinetics of BD-LNP@Hydrogel in SCF was incorporated into PKPB model for BD nanoparticulate (i.e., p.o. BD-LNP and rectal BD-LNP@Hydrogel). PBPK model simulation was performed by incorporating optimal fitted parameters into the model compartment to estimate intrinsic metabolism and various clearance at hepatic and intestinal sites of BD in Free- versus nanoparticulate forms. The accuracy of model simulation was by average folding error (AFE)  and absolute average folding error (AAFE) with the following equations [6]:

Cobs was the experimental measured concentration values, Cpre was the concentration values predicted by the model, and N was the number of time points.

Table S2. Literature data of PK parameters used for PBPK model fitting.

| Parameters |  | Definition | Value | References |
| --- | --- | --- | --- | --- |
| Bioavailability | Fsys | Fraction of dose absorbed in gut lumen | 0.11 | [7, 8] |
| Volume (mL) | VP | Total plasma volume | 1 | [9] |
|  | VOT | Total other tissue volume | 13.32 | [10] |
|  | VIP | Intestinal plasma volume | 0.03 | [11] |
|  | VIT | Intestinal tissue volume | 1.5 | [10] |
|  | VLP | Liver plasma volume | 0.51 | [11] |
|  | VLT | Liver tissue volume | 1.3 | [10] |
| Blood flow (mL/min) | QCO | Cardiac output | 8 | [9] |
|  | QOT | Other tissue blood flow | 4.85 | [9, 10] |
|  | QHA | Hepatic artery | 0.35 | [10] |
|  | QPV | Portal vein | 1.5 | [10] |
| Partition coefficient |  | BD Partition coefficient for other tissue | 0.1 | Assumed |
|  |  | HP Partition coefficient for other tissue | 1 | Assumed |
| Unbound fraction |  | Plasma unbound fraction for BD | 0.32 | [12] |
|  |  | Plasma unbound fraction for HP | 0.1 | Assumed |
| Intrinsic Clearance (mL/min) |  | Hepatic intrinsic clearance forming HP | 4.42 | [13] |
|  |  | Intestinal intrinsic clearance forming HP | 4.42 | [13] |

S7.3 Mathematical equations.

In the plasma (P) compartment:

In other tissue compartments:

In the kidney blood compartment:

In the urine compartment:

In the urine compartment:

In the liver plasma compartment zone 1, with segregated flows returning from the intestine:

In the liver plasma compartment zone 2:

In the liver plasma compartment zone 3:

In the liver tissue compartment zone 1:

In the liver tissue compartment zone 2:

In the liver tissue compartment zone 3:

In the bile compartment:

In the intestinal plasma compartment:

In the intestinal tissue compartment:

In the fecal compartment:

S8. Characterization of BD-LNP@Hydrogel

Figure S4. A) Representative nanoparticle size distribution of BD-LNP determined by DLS; B) Scheme of hydrogel synthesis and nanoparticles entrapment. Grafted 2APBA groups of HA-2APBA covalently interact with cis- 1,3-diol containing PVA, facilitating the formation of dynamic phenylborate ester cross-linking hydrogel; C) Macroscopic appearance and rapid recovery of BD-LNP@Hydrogel.

Table S3. Mesh size of different concentration hydrogels prepared by mixing HA-2APBA @PVA (n = 3).

S9. PBPK model validation

S9.1 Pharmacokinetics of Free-BD after a single i.v. and p.o. dose to mice. The plasma concentrations of BD and its metabolite HP in mice administered by gastric gavage and intravenous injection were shown in figure S4, and non-compartmental analysis was applied to calculate PK parameters. To calculate the excretion rates, the cumulative excretion of BD and HP in mice urine was divided by the administered dose of 60 μg of BD (assuming a body weight of 20 g for the mice). The excretion rates of BD in urine, expressed as a percentage of the administered dose, were found to be 0.013% for oral gavage and 0.017% for intravenous injection. For the metabolite HP, the excretion rates were 9.62% and 8.77% for oral gavage and intravenous injection, respectively. These results were consistent with the urinary excretion profile of BD, where the parent drug BD was almost absent from the urine, and the metabolite HP was one of the main metabolites present in the urine. This pattern was typical for drugs that undergo significant metabolism before excretion, with metabolites often being more readily excreted than the parent compound [7].

Figure S5. PK of BD and its major metabolite HP monitored by LC-MS after i.v. or p.o. administration of Free-BD via different ingestion routes in mice. A) Plasma BD concentration-time profiles; B) Plasma HP concentration-time profiles; C) Urinary secretion amount of BD and HP during 24 hours; D) PK parameters of BD. The blood was collected at 0.25, 0.5, 1, 2, 4,6, 8, 12 and 24 h post gastric gavage or i.v. injection and the urine was collected over a 24 h period after oral gavage or intravenous administration. A single dose of BD was administered at 3mg/kg.

9.2 Fitting of Free BD pharmacokinetic data. The PBPK model was constructed and used to fit the measured plasma concentrations of BD and HP, as well as the cumulative urinary excretion of BD and HP, in mice from pharmacokinetic experiments. The measured results were then compared with simulation results from the model. As shown in figure S6, in the intravenous group, the predicted values of the PBPK model were in good agreement with the experimentally determined HP plasma concentrations and cumulative urinary excretion of BD and HP, but the fitting results for BD plasma concentrations were less specific. The simulation results for the oral gavage group showed that the predicted values of the PBPK model were more consistent with the experimentally determined plasma concentrations of BD and HP, as well as the cumulative urinary excretion of BD and HP in mice. The AFE and AAFE for BD plasma concentrations in the oral gavage group were 1.42 and 3.05, respectively; those for HP were 0.17 and 3.64, respectively. This further confirms that the model fits the oral BD data well.

As the simulation results of the oral free BD group data show, the established mouse PBPK model can accurately predict BD's pharmacokinetic behavior in mice. Therefore, the values obtained for the model fitting parameters were used to simulate BD and HP's concentration-time profiles in the livers and intestines of mice, which were then compared with the measured values. Based on data from previous experiments, the mouse liver weight was assumed to be 0.8 g and the small intestine weight to be approximately 0.7 g. The simulation results showed that the constructed PBPK model can accurately predict the concentrations of the drug BD and its metabolite HP, as well as their trends.

Figure S6. BD and 16α-hydroxy-prednisolone (HP) concentration-time profiles in plasma, intestine and liver as well as the cumulative amounts of BD and HP in urine after 3mg/kg IV A) or PO B) administration of Free BD in mice. Solid triangles are BD and open triangles are HP (IV, red; PO, blue). Fitting was performed according to PBPK models. The fit of the model to drug concentrations in plasma and tissues of BD and cumulative amounts of BD in urine following intravenous and oral administration of BD are solid lines, HP are dashed lines.

S10. Comparison of BD metabolism between p.o. and rectal administration

S10.1 Comparison of fitted PK parameters of p.o. Free-BD and p.o. BD-LNP (Table S4). Compared with p.o. Free-BD group, the model fitting of blood, liver, and small intestinal concentrations in the oral BD-LNP group showed three key results: Firstly, the influx transporter clearance () and efflux transporter clearance () of BD at the intestinal site increased by 1.75 and 1.87 times, respectively, but the ratio of the two (7.70) did not change significantly compared with the Free BD group (7.22), indicating that the absorption and transport of BD-LNP at the intestinal site were similar to those of Free BD, that is, there was no significant change in the absorption of BD. The influx transporter clearance () of BD at the liver site increased by 1.2 times, while the efflux transporter clearance () decreased by 5.71 times, and the ratio of the two increased by 6.93 times, indicating that the absorption and transport process of BD at the liver site was stronger than the efflux transport process, that is, a large amount of BD was absorbed into the liver tissue. The intrinsic clearance of CYP3A4-generated HP ( and ) in the intestine and liver increased by 1.70 and 5.46 times, respectively, and the excretion clearance of HP ( and ) in the intestine and liver increased by 23.75 and 17.5 times, respectively. This metabolic shift may be due to the sustained low-dose drug release characteristics of BD-LNP, which kept the CYP3A4 enzyme in an unsaturated state, thereby promoting the preferential biotransformation of the major metabolite HP.

Table S4. Fitted PK parameters for BD delivered by p.o. Free-BD, p.o. BD-LNP or rectal BD-LNP@Hydrogel. A single dose of BD was given at 3 mg/kg (total dose 60 µg).

| Parameters a |  |  | Definition |  | Fitted Value (PO Free BD) | Fitted Value (PO BD-LNP) | Fitted Value (Rectal BD-LNP@Hydrogel) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Unbound fraction | Intestine |  |  | Intestinal tissue unbound fraction for BD | - | - | - |
|  |  |  |  | Intestinal tissue unbound fraction for HP | - | - | - |
|  | Liver |  |  | Hepatic tissue unbound fraction for BD | - | - | - |
|  |  |  |  | Hepatic tissue unbound fraction for HP | - | - | - |
| Transport clearance (mL/min) | Intestine |  |  | Influx clearance of BD in the intestine | 3.94 | 6.90 | 11.12 |
|  |  |  |  | Efflux clearance of BD in the intestine | 28.45 | 53.13 | 4.12 |
|  |  |  |  | Efflux clearance of HP in the intestine | 8.35 | 1.23×10-2 | 1.95 |
|  | Liver |  |  | Influx clearance of BD in the liver | 15.71 | 19.08 | 124.30 |
|  |  |  |  | Influx clearance of HP in the liver | 0.93 | 1.40 | 5.55 |
|  |  |  |  | Efflux clearance of BD in the liver | 2.05 | 0.36 | 65.20 |
|  |  |  |  | Efflux clearance of HP in the liver | 34.41 | 10.96 | 36.71 |
| Secretion clearance (mL/min) | Intestine |  |  | Intestinal secretion clearance for BD | 1.43×10-2 | 5.14×10-2 | 1.41×10-2 |
|  |  |  |  | Intestinal secretion clearance for HP | 0.20 | 4.75 | 0.33 |
|  | Liver |  |  | Biliary clearance of BD | 0.86×10-3 | 1.68×10-2 | 1.72 |
|  |  |  |  | Biliary clearance of HP | 0.14 | 2.45 | 8.29×10-3 |
|  | Kidney |  |  | Renal clearance of BD | 0.32 | - | - |
|  |  |  |  | Renal clearance of HP | 5,90 | - | - |
| Intrinsic clearance (mL/min) | Intestine |  |  | Intestinal intrinsic clearance forming HP | 1.27 | 2.16 | 0.07 |
|  |  |  |  | Intestinal intrinsic clearance forming other metabolites | 2.12 | 0.09 | 77.25 |
|  | Liver |  |  | Hepatic intrinsic clearance forming HP | 4.45 | 24.31 | 1.21 |
|  |  |  |  | Hepatic intrinsic clearance forming other metabolites | 3.27 | 124.10 | 1.69 |
| Absorbance fraction (min-1) |  | (min-1) |  | Absorption rate constant of BD | 0.26 | 0.20 | 1.46 |

a Intestine for p.o. Free-BD and BD-LNP was the small intestine, and for rectal BD-LNP@Hydrogel was the colon.

Figure S7. Hepatic and intestinal biodistribution of the drug BD and its metabolite HP in the form of p.o. Free-BD, p.o. BD-LNP and rectal BD-LNP@Hydrogel as determined by LC-MS after drug extraction by liquid-liquid extraction method. A) Total BD and HP concentration in liver and B) Total BD and HP concentration in intestinal tissues. Free BD and BD-LNP group mice were orally gavage at a BD dose of 3 mg/kg. Data were presented as means ± SEM (n=6).

References

[1] R. Miao, F. Jin, Z. Wang, W. Lu, J. Liu, X. Li, R.X. Zhang, Oral delivery of decanoic acid conjugated plant protein shell incorporating hybrid nanosystem leverage intestinal absorption of polyphenols, Biomaterials, 281 (2022) 121373.10.1016/j.biomaterials.2022.121373

[2] X. Deng, R. Attalla, L.P. Sadowski, M. Chen, M.J. Majcher, I. Urosev, D.C. Yin, P.R. Selvaganapathy, C.D.M. Filipe, T. Hoare, Autonomously self-adhesive hydrogels as building blocks for additive manufacturing, Biomacromolecules, 19 (2018) 62–70.10.1021/acs.biomac.7b01243

[3] X. Yan, Synthesis, characterization and mechanistic study of phenylborate ester dynamic cross-linking hydrogel for rectal controlled drug delivery, in:  Institute of Medical Research, Northwestern Polytechnical University, Northwestern Polytechnical University, Xi'an, China, 2024, pp. 128.

[4] T. Cao, Permeability study of budesonide loaded nanostructured lipid carriers across intestinal epithelial cells, in:  School of Life Sciences, Northwestern University, Northwestern University, Xi'an, China, 2023, pp. 43.

[5] Y. Zhang, M. Huo, J. Zhou, A. Zou, W. Li, C. Yao, S. Xie, Ddsolver: An add-in program for modeling and comparison of drug dissolution profiles, Aaps j, 12 (2010) 263–271.10.1208/s12248-010-9185-1

[6] L. Sun, C. Wang, Y. Zhang, A physiologically based pharmacokinetic model for valacyclovir established based on absolute expression quantity of hpept1 and its application, European Journal of Pharmaceutical Sciences, 123 (2018) 560–568.https://doi.org/10.1016/j.ejps.2018.07.057

[7] S. Edsbacker, T. Andersson, Pharmacokinetics of budesonide (entocort ec) capsules for crohn's disease, Clin Pharmacokinet, 43 (2004) 803–821.10.2165/00003088-200443120-00003

[8] K. McKeage, K.L. Goa, Budesonide (entocort ec capsules): A review of its therapeutic use in the management of active crohn's disease in adults, Drugs, 62 (2002) 2263–2282.10.2165/00003495-200262150-00015

[9] B. Davies, T. Morris, Physiological parameters in laboratory animals and humans, Pharm Res, 10 (1993) 1093–1095.10.1023/a:1018943613122

[10] E.C. Chow, M.R. Durk, C.L. Cummins, K.S. Pang, 1alpha,25-dihydroxyvitamin d3 up-regulates p-glycoprotein via the vitamin d receptor and not farnesoid x receptor in both fxr(-/-) and fxr(+/+) mice and increased renal and brain efflux of digoxin in mice in vivo, J Pharmacol Exp Ther, 337 (2011) 846–859.10.1124/jpet.111.179101

[11] C. Hall, E. Lueshen, A. Mošat, A.A. Linninger, Interspecies scaling in pharmacokinetics: A novel whole-body physiologically based modeling framework to discover drug biodistribution mechanisms in vivo, J Pharm Sci, 101 (2012) 1221–1241.10.1002/jps.22811

[12] K. Yamazaki, M. Kanaoka, Computational prediction of the plasma protein-binding percent of diverse pharmaceutical compounds, J Pharm Sci, 93 (2004) 1480–1494.10.1002/jps.20059

[13] A. Effinger, C.M. O'Driscoll, M. McAllister, N. Fotaki, Predicting budesonide performance in healthy subjects and patients with crohn's disease using biorelevant in vitro dissolution testing and pbpk modeling, Eur J Pharm Sci, 157 (2021) 105617.10.1016/j.ejps.2020.105617