Supporting Information

Emergent Superparamagnetism and Anomalous Hall Effect in Two-Dimensional Magnet CrxPt1-xTe2

Xue Yang1,2†, Ruihuan Duan3†, Xin Zhou4†, Yuqiao Zhou5†, Lei Xu1,2, Sicheng Zhou1,2, Xinyi Zheng1,2, Siyuan Zhou1,2, Lihong Hu1,2, Hua Ke6, Bingbing Tong1,7, Jie Shen1,2,7, Zhaozheng Lyu1,2,7, Xiunian Jing1, Fanming Qu1,2,7, Peiling Li1,2,7*, Zheng Liu3,8*, Guangtong Liu1,2,7*, and Li Lu1,2,7

1 Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China.

2 School of Physical Sciences, University of Chinese Academy of Sciences, Beijing 100049, China.

3 School of Materials Science and Engineering, Nanyang Technological University, 639798 Singapore.

4 Institute for Functional Intelligent Materials, National University of Singapore, 117544, Singapore.

5 Key Laboratory of Green Chemistry & Technology, Ministry of Education, College of Chemistry, Sichuan University, Chengdu 610064, China.

6 School of Materials Science and Engineering, Harbin Institute of Technology, Harbin 150001, China.

7 Hefei National Laboratory, Hefei, Anhui 230088, China.

8 CINTRA CNRS/NTU/THALES, Research Techno Plaza, Singapore, Singapore.

* Corresponding authors E-mail: cioran@iphy.ac.cn; z.liu@ntu.edu.sg; gtliu@iphy.ac.cn

†These authors contributed equally.

X-ray photoelectron spectroscopy (XPS)

X-ray photoelectron spectroscopy (XPS) measurements were conducted to investigate the chemical composition and valence states of the synthesized CrxPt1−xTe2 single crystals. The XPS spectra for these crystals are presented in Fig. 1e and 1f. Energy calibration was carried out using the C 1s peak (284.6 eV) to eliminate the effects of charge accumulation and surface contamination during the analysis. The binding energy of Cr0.35Pt0.65Te2 has been discussed in the main text, while those of other samples are listed in Table S1. However, relying only on XPS results presents challenges in accurately determining the stoichiometric ratio of the sample, as noted in previous report1. Additionally, with the increasing Cr content, the observed shifts in peak positions can be attributed to the differences in electronegativity among Cr (1.66), Pt (2.28), and Te (2.1). When an atom with lower electronegativity replaces a bonded atom, the binding energy tends to decrease2. Hence, it is inferred that the Cr elements in CrxPt1−xTe2 are likely substituting for either Pt or Te, leading to the formation of Cr-Pt and Cr-Te bonds, which indicates a significant change of the local chemical environment surrounding the Pt and Te atoms.

Table S1: Specific binding energies of Pt 4f7/2(Pt 4f5/2), Cr 2p3/2(Cr 2p1/2) and Te 3d5/2(Te 3d3/2) in various oxidation states for the CrxPt1−xTe2 (x=0.25, 0.3, and 0.35), together with values obtained from deconvoluted XPS spectra.

|  | Pt 4f7/2(Pt 4f5/2) | Cr 2p3/2(Cr 2p1/2) | Te 3d5/2(Te 3d3/2) |
| --- | --- | --- | --- |
| Cr0.25Pt0.75Te2 | 72.61(75.96) eV | 576.46(586.66) eV | 573.41(583.76) eV |
| Cr0.3Pt0.7Te2 | 72.55(75.85) eV | 576.23(586.53) eV | 573.28(583.63) eV |
| Cr0.35Pt0.65Te2 | 72.58(75.93) eV | 576.18(586.40) eV | 573.15(583.50) eV |

Fig. S1. (a) Optical images and EDX spectra of as-grown Cr0.6Pt0.4Te2 single crystals. (b) Left: XRD patterns for CrxPt1−xTe2 samples with varying Cr concentration of (x=0, 0.25, 0.3, 0.35 and 0.6) alongside calculated patterns for PtTe2 and CrTe2. Right: Enlarged XRD patterns in the 12.5º to 20º range. (c) Changes in c-axis lattice constant with Cr concentration.

Fig. S2. STEM investigation of pristine PtTe2. Left: HAADF image of the PtTe2 material. Top-right: Fourier transform pattern of the STEM image. Bottom-right: Zoomed-in STEM image overlaid with the atomic model of PtTe2, where pink spheres represent Pt atoms and yellow spheres represent Te atoms.

The STEM image of pristine PtTe2 reveals the characteristic atomic arrangement displaying a honeycomb structure, which is further evidenced by the Fourier transform pattern. The metal-chalcogenide spacing, measured from the calibrated STEM image, is observed to be 2.32 Å. This measurement aligns precisely with the typical value for PtTe23.

Fig. S3. Temperature-dependent magnetization of Cr0.35Pt0.65Te2. (a) Out-of-plane (H∥c) magnetization of Cr0.35Pt0.65Te2 measured under different magnetic fields. (b) In-plane magnetization of Cr0.35Pt0.65Te2 under different magnetic fields. The green arrows in (a) and (b) indicate the shift in the blocking temperature TB as the external applied magnetic field increases. For clarity, the zero-field-cooling (ZFC) and field-cooling (FC) curves for different fields have been shifted vertically. As the external magnetic field decreases, the blocking temperature TB systematically shifts to higher temperatures for both H∥c and H∥ab directions, which aligns with the theoretical expectation of the superparamagnetism (SPM), confirming that Cr0.35Pt0.65Te2 exhibits superparamagnetic properties in the intermediate temperature range.

Fig. S4. Plots of reduced magnetization M/Ms versus H/T under out-of-plane (H∥c) (a) and in-plane (H∥ab) (b) magnetic fields of Cr0.35Pt0.65Te2.

Analysis of the M(H) Curve with Modified Langevin Functions

We analyzed the magnetization data M(H) of CrxPt1−xTe2 using the modified-Langevin function, expressed as,

MH,T=N0∞μLxfμdμ+χH#1

where N=M0(T)/μ represents the number density of clusters, μ=M0(T)ρV is the mean cluster magnetic moment, M0(T) is the saturated magnetization, and V is the mean cluster volume. The Langevin function is given by Lx=cothx-1x, with x=μHkBT. The function fμ=1μs2πexp-ln⁡(μμd)22s2 represents the log-normal distribution of the cluster magnetic moment, where s and µd are the median and the standard deviation of the log-normal distribution, respectively. We used Python to fit the data below 120 K with Eq. (1), adjusting the parameters N, µd, s and χ. According to refs.4 and 5, several factors can complicate parameter fitting, and the correlation among parameters may lead to over- or underestimation4,5. To enhance the accuracy of our fitting, we selected the data below 120 K that exhibited a good overlap with the results presented in Fig. S4. The fitting parameters and the calculated mean volume diameter D are summarized in Table S2. Notably, the mean magnetic moment μ decreases with increasing temperature, indicating a reduction in the magnetic contributions from superparamagnetic clusters. Interestingly, the estimated average diameter at 120 K is larger than those at 80 K and 100 K, which could be attributed to factors such as anisotropy and reduced saturation magnetization, potentially leading to deviations in the Langevin fitting from the experimental data.

Next, we show how to derive the mean volume diameter D. The mean cluster volume V is proportional to the cube of the mean diameter, V∝D3. The magnetic cluster moment is given by,

μ=M0m=M0ρV#2

where M0=Nμ is the saturation magnetization, ρ = 7.16 g/cm3 is the density of Cr, m is the mass of magnetic cluster, and V is the volume of magnetic cluster. Thus, mean cluster volume can be written as,

V=0∞Vμfμdμ=0∞μM0ρfμdμ=1M0ρ0∞μfμdμ#3

From this, we can derive the mean volume diameter D,

D~3V~31M0ρ0∞μfμdμ~31M0ρμ~3μNμρ~31Nρ#4

Table S2: Values of the fitting parameters N, s, μd, χ, and the mean volume diameter ⟨D⟩ for Cr0.35Pt0.65Te2 at various temperatures.

| T (K) | N (1017/g) | μd(μB) | s | χ (10-4emugOe) | D (nm) | μ(μB) |
| --- | --- | --- | --- | --- | --- | --- |
| 80 K | 0.95 | 5070 | 0.52 | 2.46 | 8.79 | 5803 |
| 100 K | 0.82 | 4430 | 0.71 | 2.44 | 8.37 | 5700 |
| 120 K | 1.85 | 832 | 1.38 | 2.30 | 10.98 | 2156 |

Note:
To calculate the mean magnetic moment μ=0∞μf(μ)dμ, we let x=μ. Thus,

I=0∞μfμdμ=1s2π0∞exp-lnxμd22s2dx#5

Next, we perform a change of variables by setting y=ln⁡(xμd)2s. Then

x=μde2sy, dx=2sμde2sydy=2sxdy#6

Substituting this into the integral yields:

I=12πs-∞∞e-y22sxdy
=1π-∞∞xe-y2dy=1π-∞∞μ0e2sye-y2dy#7
=μdπ-∞∞e-(y-22s)2es22dy
Letting t=y-22s gives dt=dy, and we can express the integral as,

I=3μdes22-∞∞1πe-t2dt#8

Since -∞∞e-t2dt=π, we find,

I=μdes22#9

Fig. S5. In-plane superparamagnetism in Cr0.35Pt0.65Te2. (a) Temperature dependence of the in-plane magnetization curves M(T) for Cr0.35Pt0.65Te2 under an in-plane magnetic field (H∥ab) of 500 Oe. (b) In-plane isothermal magnetization M(H) curves at different temperatures. (c) Evolution of the temperature-dependent coercive field Hab along with the magnetic phase diagram of Cr0.35Pt0.65Te2. Schematic representations illustrate the orientation of the magnetic moment of superparamagnetic particles in ferromagnetic (FM), superparamagnetic (SPM), and paramagnetic states (PM).

The results of the in-plane magnetization measurements are presented in Fig. S5. As shown in Fig. S5a, the MZFC(T) and MFC(T) exhibit a discernible difference up to 125 K, with MZFC(T) displaying a cusp at 23 K, indicating the presence of superparamagnetism (SPM). According the Curie–Weiss law (1χ=T-TCWC), Tcw = 247 K can be obtained. Fig. S5b presents the in-plane magnetization M(H) curves collected at various temperatures. In contrast to the out-plane M(H) curves, the in-plane M(H) exhibits smaller coercivities and a sharper transition at zero magnetization, suggesting a strong magnetic anisotropy in Cr0.35Pt0.65Te2, with the ab-plane being the easy magnetization plane. When T ≤ 20 K, small hysteresis loops are observed, and the coercive field drops to zero above 40 K, confirming the presence of in-plane SPM. The temperature-dependent coercivity Hc(T) is plotted in Fig. S5c. The pronounced decrease of Hc from 2 K to 40 K implies a transition from a ferromagnetic state to a superparamagnetic state. Similarly, we also establish the magnetic phase diagram of in-plane magnetization transition, as superimposed on Fig. S5c.

Fig. S6. (a) Inverse magnetic susceptibility (1χ=HM) of the out-of-plane magnetization of CrxPt1−xTe2 (x=0.25, 0.3 and 0.35) under an external perpendicular magnetic field (Hc) of 500 Oe. The red dashed line represents the best fit to the experimental data with Curie-Weiss law (1χ=T-TCWC). The mass values for the samples are as follows: Cr0.25Pt0.75Te2 is 1.37 mg, Cr0.3Pt0.7Te2 is 32.1 mg, and Cr0.35Pt0.65Te2 is 7.3 mg. (b) Temperature dependence curves M(T). For clarity, the data for Cr0.25Pt0.75Te2 is multiplied by 100. (c) Inverse magnetic susceptibility of the in-plane magnetization under a magnetic field (H∥ab) of 500 Oe. For clarity, the data for Cr0.3Pt0.7Te2 and Cr0.35Pt0.65Te2 are multiplied by 10 in (a) and (c). (d) Phase diagram of CrxPt1−xTe2 as a function of Cr doping concentration x and temperature for the in-plane magnetization.

To verify the Cuire-Weiss temperature Tcw of these samples, we compare the temperature dependence of magnetic susceptibility χ−1(T ) for the magnetic fields oriented parallel to the c-axis and the ab-plane, as shown in Fig. S6a and S6c. A linear relationship between χ−1 and T is observed, consistent with the Curie–Weiss law, allowing for the determination of the corresponding Curie temperature Tcw and Curie constant C. Fig. S6b shows the ZFC and FC magnetization curves under an external field (µ0H=500 Oe) parallel to the ab-plane for CrxPt1−xTe2 samples with x= 0, 0.25, 0.3 and 0.35. Notably, the ZFC and FC curves diverge at the irreversible temperature Tirr, and the ZFC curve displays a peak at the temperature TB. Further, Fig. S6d presents the magnetic phase diagrams for various Cr doping concentrations across different temperature ranges, incorporating Tcw, TB, and Tirr. The corresponding values for the out-plane and in-plane magnetization are summarized in Tables S3 and Table S4.

Table S3: Curie constant C, Curie-Weiss temperature Tcw, Blocking temperature TB, and Irreversible temperature Tirr for H∥c in CrxPt1−xTe2 (x = 0.25, 0.3, and 0.35).

|  | C (10-4 Oe· K·g/emu) | Tcw(K) | TB(K) | Tirr(K) |
| --- | --- | --- | --- | --- |
| Cr0.25Pt0.75Te2 | 6.92 | 114 | 15 | 33 |
| Cr0.3Pt0.7Te2 | 22.78 | 220 | 53 | 194 |
| Cr0.35Pt0.65Te2 | 23.28 | 220 | 60 | 200 |

Table S4: Curie constant C, Curie-Weiss temperature Tcw, Blocking temperature TB, and Irreversible temperature Tirr for H∥ab in CrxPt1−xTe2 (x = 0.25, 0.3, and 0.35).

|  | C (10-4 Oe· K·g/emu) | Tcw(K) | TB (K) | Tirr(K) |
| --- | --- | --- | --- | --- |
| Cr0.25Pt0.75Te2 | 9.01 | 85 | 8 | 20 |
| Cr0.3Pt0.7Te2 | 20.63 | 239 | 17 | 120 |
| Cr0.35Pt0.65Te2 | 28.28 | 247 | 23 | 125 |

Fig. S7. Temperature-dependent in-plane magnetization (H∥ab) (a) and out-of-plane (H∥c) (c) of Cr0.25Pt0.75Te2 sample under different magnetic fields. The solid and dashed lines represent the magnetization curves measured under the FC and ZFC conditions, respectively. Isothermal magnetization curves M(H) for in-plane (H∥ab) (b) and out-of-plane (H∥c) (d) taken at different temperatures.

Fig. S8. Temperature-dependent in-plane magnetization (H∥ab) (a) and out-of-plane (H∥c) (c) of Cr0.3Pt0.7Te2 sample under different magnetic fields. The solid and dashed lines represent magnetization curves measured under the FC and ZFC conditions, respectively. Isothermal magnetization curves M(H) for in-plane (H∥ab) (b) and out-of-plane (H∥c) (d) taken at different temperatures.

Fig. S9. (a) Hall measurement results at different temperatures ranging from 2 K to 300 K of Cr0.35Pt0.65Te2. (b) High-temperature (T >100 K) magneto-resistance MR=(Rxx(µ0H) − Rxx(0T))/Rxx(0T) of Cr0.35Pt0.65Te2.

Fig. S9a plots the total Hall resistance Rxy as a function of the external perpendicular magnetic field µ0H collected at various temperatures ranging from 2 K to 300 K. The total Hall resistance can be expressed as follows,

Rxy=RxyO+RxyA#10

Where RxyO represents the ordinary Hall resistance and and RxyA is the anomalous Hall resistance. Based on the positive slope of RxyO, the type of the charge carrier is determined to be p-type.

When T ≥ 200 K, the Hall traces exhibit a linear dependence on µ0H, accompanied by negative magneto-resistance (MR=(Rxx(µ0H) − Rxx(0T))/ Rxx(0T)) in the Rxx curve (Fig. S9b). The observed negative MR above 200 K may be associated with the spin fluctuations of the local electron6,7. Below 200 K, the MR displays a remarkable increase from -1.62% at 200 K to -4.29% at 150 K, indicating that an external magnetic field can easily orient more magnetic moments. As T decreases, RxyA gradually deviates from linearity at ∼ 200 K and develops into a well-defined S−shaped curve with zero coercivity until reaching 80 K. These behaviors further confirm the presence of superparamagnetism8,9.

Fig. S10. Plot of ΘH vs σxx  for Cr0.25Pt0.75Te2, Cr0.35Pt0.65Te2, and other reported anomalous Hall materials10-12. For most anomalous Hall materials, the increase of ΘH is typically accompanied by a decrease of σxx . The green dashed line guides the eye to illustrate the increasing tendency of ΘH for Cr0.25Pt0.75Te2, Cr0.35Pt0.65Te2, and other reported anomalous Hall materials.

Fig. S11. The anomalous Hall conductivity σxyA as a function of the longitudinal conductivity σxx  (a) and the square of the longitudinal conductivity σxx2 (b). The red dashed lines are linear fits to the experimental data.

Fig. S10 shows the anomalous Hall conductivity σxyA as a function of the longitudinal conductivity σxx  and its square σxx2 from 2 K to 220 K. Clearly, the experimental data cannot be adequately fitted with either σxyA ∝ σxx  (red dashed line in Fig. S10a) or σxyA ∝σxx2 (red dashed line in Fig. S10b). These observations suggest that conventional scaling approaches, which typically consider only extrinsic or intrinsic mechanisms, are insufficient to interpret the experimental results.

Fig. S12. (a) Temperature-dependent zero-field longitudinal resistance Rxx (left axis) and coercive field Hc (right axis) extracted from (b) of Cr0.25Pt0.75Te2 single crystals. (b) Anomalous Hall resistance RxyA measured at different temperatures ranging from 2 K to 300 K. The RxyA hysteresis is highlighted by the shaded red region. Low-temperature longitudinal resistance Rxx (T < 40 K) (c) and high-temperature (T > 60 K) magneto-resistance MR=(Rxx(µ0H) − Rxx(0T))/Rxx(0T) of Cr0.25Pt0.75Te2. For clarity, each trace in (b) and (c) is vertically offset.

Fig. S13. The anomalous Hall conductivity σxyA as a function of σxx  of Cr0.25Pt0.75Te2. The red line is the best fit to the experimental data with the equation σxyA=α+βσxx +γσxx2 for the SPM data from 15 K to 120 K.

Fig. S14. (a) Carrier density n and mobility µ at different temperatures for Cr0.25Pt0.75Te2 and Cr0.35Pt0.65Te2. (b) Temperature-dependent curves of longitudinal conductivity (c) Anomalous Hall conductivity, and (d) Anomalous Hall angle for Cr0.25Pt0.75Te2 and Cr0.35Pt0.65Te2.

Accordingly, the density n and mobility µ can be calculated using the fundamental single- carrier Drude model, with the relations n = 1/eR0d and µ=σxx /ne at different temperatures (Fig. S13a), where e is the elementary charge, d is the sample thickness, and R0 is the ordinary Hall coefficient. The extracted n and µ are plotted as a function of temperature in Fig. S13. All the samples show p-type conducting behavior, with n (µ) found to be monotonically increasing (decreasing) upon cooling. In Fig. S13b and c, both σxx  and σxyA for Cr0.25Pt0.75Te2 and Cr0.35Pt0.65Te2 exhibit similar temperature-dependent trends, with σxyA saturating at low temperatures. This observation further confirms the presence of the AHE in the superparamagnetic system CrxPt1−xTe2. The temperature dependence of the anomalous Hall angle, shown in Fig. S13d, reveals pronounced peaks around 15 K and 60 K for Cr0.25Pt0.75Te2 and Cr0.35Pt0.65Te2, respectively, corresponding to their blocking temperatures, as evidenced by magnetic measurements.

Fig. S15. Plot of σxyA vs σxx  for a variety of materials spanning the various AHE regimes, ranging from the impurity scattering to the intrinsic and skew scattering regimes13-18. Compared to other anomalous Hall materials, the smaller anomalous Hall conductivity of Cr0.25Pt0.75Te2 (green symbol) and Cr0.35Pt0.65Te2 (yellow symbol) may suggest the presence of disorder introduced by Cr doping.

References

1.	Roy, A. et al. Perpendicular Magnetic Anisotropy and Spin Glass-like Behavior in Molecular Beam Epitaxy Grown Chromium Telluride Thin Films. ACS Nano 9, 3772-3779 (2015).

2.	Hu, J. et al. Co-doping: An effective strategy for developing stable and high-speed Sb2Te-based phase-change memory. Applied Physics Letters 122 (2023).

3.	Furuseth, S. et al. Redetermined Crystal Structures of NiTe2, PdTe2, PtS2, PtSe2, and PtTe2. Acta Chemica Scandinavica 19, 257-258 (1965).

4.	Respaud, M. Magnetization process of noninteracting ferromagnetic cobalt nanoparticles in the superparamagnetic regime: Deviation from Langevin law. Journal of Applied Physics 86, 556-561 (1999).

5.	Henrard, D. et al. Monitoring of Superparamagnetic Particle Sizes in the Langevin Law Regime. Journal of Nanomaterials 2019, 1-9 (2019).

6.	Moriya, T. Spin fluctuations in itinerant electron magnetism. Vol. 56 (Springer Science & Business Media, 2012).

7.	Tsujii, N., Nishide, A., Hayakawa, J. & Mori, T. Observation of enhanced thermopower due to spin fluctuation in weak itinerant ferromagnet. Science Advances 5, eaat5935 (2019).

8.	Allia, P., Knobel, M., Tiberto, P. & Vinai, F. Magnetic properties and giant magnetoresistance of melt-spun granular Cu100-x-Cox alloys. Physical Review B 52, 15398-15411 (1995).

9.	Zhang, H. et al. Itinerant ferromagnetism in van der Waals Fe5-xGeTe2 crystals above room temperature. Physical Review B 102, 064417 (2020).

10.	Huang, M. et al. Significant perpendicular magnetic anisotropy in room-temperature layered ferromagnet of Cr-intercalated CrTe2. 2D Materials 8, 031003 (2021).

11.	Li, P. et al. Giant room temperature anomalous Hall effect and tunable topology in a ferromagnetic topological semimetal Co2MnAl. Nature Communications 11, 3476 (2020).

12.	Huang, M. et al. Colossal Anomalous Hall Effect in Ferromagnetic van der Waals CrTe2. ACS Nano 15, 9759-9763 (2021).

13.	Miyasato, T. et al. Crossover Behavior of the Anomalous Hall Effect and Anomalous Nernst Effect in Itinerant Ferromagnets. Physical Review Letters 99, 086602 (2007).

14.	Nakatsuji, S., Kiyohara, N. & Higo, T. Large anomalous Hall effect in a non-collinear antiferromagnet at room temperature. Nature 527, 212-215 (2015).

15.	Yang, S.-Y. et al. Giant, unconventional anomalous Hall effect in the metallic frustrated magnet candidate, KV3Sb5. Science Advances 6, eabb6003 (2020).

16.	Iguchi, S., Hanasaki, N. & Tokura, Y. Scaling of Anomalous Hall Resistivity in Nd2(Mo1-xNbx)2O7 with Spin Chirality. Physical Review Letters 99, 077202 (2007).

17.	Nayak, A. K. et al. Large anomalous Hall effect driven by a nonvanishing Berry curvature in the noncolinear antiferromagnet Mn3Ge. Science Advances 2, e1501870 (2016).

18.	Liu, E. et al. Giant anomalous Hall effect in a ferromagnetic kagome-lattice semimetal. Nature Physics 14, 1125-1131 (2018).