Table 1. The results of application of the electrodes to estimate their ability in repeated and reproduced measurements under the optimal conditions

| Electrode | Added (mM) | Found* (mM) | Recovery* | Repeatability (RSD) |
| --- | --- | --- | --- | --- |
| 1 | 20 | 19.86 | 99.30 | ± 2.11 |
| 2 | 25 | 24.91 | 99.64 | ± 2.03 |
| 3 | 30 | 29.92 | 99.73 | ± 2.01 |
|  |  |  | Reproducibility (RSD) | ± 3.55 |

*The average of 5 repeated measurements values (n= 5).

Table 2. Impact of foreign species on the determination of 0.1 µM T4 at EPHC@CP/GE

| Foreign species | Conc. (µM) | RE (%) |
| --- | --- | --- |
| Fe3+ Cu2+ Mg2+ I–, Cl– | 800 580 840 1200 | -3.3 -4.3 -3.0 +3.1 |
| Propylthiouracil | 700 | -3.7 |
| Liothyronine (T3) | 170 | 4.4 |

| Sample | Added (µM) | Found (µM) |  | Recovery (%) |  |  |  | F-test (p= 0.05) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Electrode | HPLC |  | Electrode | HPLC |  |  |
| Tablet (10.0 µM) | 0.00 | 10.11 ± 1.06 | 10.53 ± 2.62 |  | 101.10 ± 3.12 | 105.30 ± 3.94 |  | 0.63 |
|  | 15.00 | 25.37 ± 1.13 | 25.81 ± 2.86 |  | 101.48 ± 2.41 | 103.24 ± 3.27 |  | 0.54 |
|  | 30.00 | 40.02 ± 1.08 | 40.76 ± 2.55 |  | 100.05 ± 2.20 | 101.90 ± 3.80 |  | 0.34 |
| Human serum | 0.00 | -- | -- |  | -- | -- |  | -- |
|  | 25.00 | 25.34 ± 2.00 | 25.43 ± 3.13 |  | 101.36 ± 2.79 | 101.72 ± 3.10 |  | 0.81 |
|  | 40.00 | 40.39 ± 1.95 | 39.35 ± 2.91 |  | 100.98 ± 2.62 | 98.38 ± 3.41 |  | 0.59 |

Table 3. The assessment of effectiveness of EPHC@CP/GE for quantifying T4 in both human serum and tablet samples, with results compared to those obtained using the standard HPLC method. Measurements were conducted in five replicates (n= 5)

Table 4. Comparing the electrochemical performance of EPHC@CP/GE sensor with some other reported potential sensors

| Sensing element | Technique | LDR (mM) | LOD (mM) | Ref. |
| --- | --- | --- | --- | --- |
| HGR | IMS-MS/HPLC | 1.0 × 10-3 - 0.13 | 1.0 × 10-3 | [68] |
| Fluorophore | HPLC | 3.2 × 10-1 - 3.22 | 2.6 × 10-1 | [69] |
| MIP-MO | Fluorescence | 1.0 × 10-3 - 0.50 | 5.0 × 10-4 | [70] |
| CuMOF@PANI | DPV | 8.0 × 10-3 - 1.55 | 3.0 × 10-3 | [71] |
| CLE | CL | 6.0 × 10-3 - 6.00 | 2.0 × 10-3 | [72] |
| Mass spectrometry | LC-MS/MS | 1.0 × 10-3 - 6.44 | 9.0 × 10-4 | [73] |
| CdO-ZnO NPs | cc-PSA | 2.0 × 10-4 - 0.19 | 8.0 × 10-5 | [74] |
| EPHC@CP/GE | DPV | 8.7 × 10-3 - 80.00 | 8.0 × 10-3 | This work |

PANI: polyaniline; MOF: metal-organic-framework; MIP-MO: molecular imprinted mesoporous organosilica; CE: chemiluminescence enhancement; HGR: Host-guest recognition; LC: Liquid chromatography; cc-PSA: constant-current potentiometric stripping analysis