Supporting Information

ZIF-8-inspired cascading nanoreactors for photodynamic/starvation synergistic therapy of breast cancer

Fenglan Li1, Yuanyuan Zhang2, Chenliu Ye3, Junyang Zhuang2*

1 Department of Forensic Science, Fujian Police College, Fuzhou 350007, China

2 The Higher Educational Key Laboratory for Nano Biomedical Technology of Fujian Province, School of Pharmacy, Fujian Medical University, Fuzhou 350122, China

3 Department of Pharmacy, Longyan First Hospital, Affiliated to Fujian Medical University, Longyan 364000, China.

mail: lfl010484@fjpsc.edu.cn (Fenglan Li)
[image: image1.jpg]



Figure S1. TEM image for ZIF-8. 

[image: image2.jpg]>

Absorbance (a.u.)

Absorbance (a.u.)

4 ———ZIF-8
——Ce6
——CGH@ZIF
3
2
1
0
200 300 400 500 600 700
Wavelength (nm)
4 ———ZIF-8
—GOx
Hemin
3 ——CGH@ZIF

200 300 400 500 600
Wavelength (nm)

700

800




Figure S2. (A) UV-Vis absorption spectrum of ZIF-8, Ce6, CGH@ZIF. (B) UV-Vis absorption spectrum of ZIF-8, GOx, hemin and CGH@ZIF.
[image: image3.jpg]~ ZIF8

204 - G@ZIF
= gl C@ZIF
) ——H@ZIF
£ 12] — CGH@ZIF
g — mCGH@ZIF
= 8-
=

4

0 :

1000





Figure S3. Size distributions of ZIF-8, C@ZIF, G@ZIF, H@ZIF, CGH@ZIF and mCGH@ZIF from DLS measurements.
[image: image4.jpg]e

e

\\ra*e‘ ¢ (e N
l N0\

ﬁmm\‘a\ s‘b"‘“e l
‘;?N\\A ¥ l
5 M




Figure S4. DLS measured size of mCGH@ZIF in different media for 24 h.

[image: image5.jpg]Time (d)




Figure S5. Hydrodynamic size distribution and PDI changes of mCGH@ZIF in 7 days.
[image: image6.jpg]Absorbance (a.u.) >

Absorbance (a.u.) w

s
&

Ce6+ ABDA+L

B~ -
o b & > &

=
S

=
>

w
3
3

400 500 600 700 800
‘Wavelength (nm)

28

24

2.0

1.6

12

04

0.0 v T
300 400 500 600 700 800
‘Wavelength (nm)





Figure S6. (A) UV-vis absorption spectrum of Ce6 and ABDA mixed solution after laser irradiation at different time intervals. (B) UV-vis absorption spectrum of CGH@ZIF and ABDA mixed solution after laser irradiation at different time intervals.
[image: image7.jpg]ABDA A /A,

ek
(]

o
(=]

=
%

=
=)

=
F

=
)

g Control == Ce6 + GOx + Glu
——Ceb e Ce6 + Hemin + H202

0 2 4 6 8 10
Time (min)




Figure S7. ROS production abilities of Ce6, Ce6+GOx+Glu and Ce6+hemin+H2O2 with illumination. ABDA was used as the ROS probe.
