Tab.1: Band gap and Urbach energy values ​​relating to chromites NixCd1-xCr2O4.

| X | sample | Directe bande gap (eV) | Eu(eV) | ref |
| --- | --- | --- | --- | --- |
| 0.0 | CdCr2O4 | 3.44 | - | [35] |
| 0.3 | Ni0.3Cd0.7Cr2O4 | 2.20 | 0.21 | [1] |
| 0,5 | Ni0.5Cd0.5Cr2O4 | 2.24 | 0.40 | this study |
| 0.7 | Ni0.7Cd0.3Cr2O4 | 2.21 | 0.58 | [8] |
| 1 | NiCr2O4 | 1.72 | - | [39] |

Tab.2: Computed values of optical parameters for the chromite compound Ni0.5Cd0.5Cr2O4.

| Sample | τs | ε∞ | ωp (rad s-1) | Nme*x1050 (g-1cm-3) |
| --- | --- | --- | --- | --- |
| Ni0.5Cd0.5Cr2O4 | 4.30 | 3,26.106 | 1.42 | 0.33 |

Tab.3: Photocatalytic properties of spinel chromite ACr2O4 such as A{Fe, Ni, NxMg₁₋ₓ, Cu, Zn and Cd}

| Sample | Poluant/s | C. time (min) | L. source | R. capcity % | Dg(nm) | Eg(eV) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cr2O3 | MB | 240 | UV-Vis | 88 | 30 | 3.16 | [56] |
| CdCr2O4/Ag | MB | 70 | UV | 37 | 32 | 3.35 | [57] |
| FeCr2O4/Ag | MB | 70 | UV | 56 | 57 | 3.2 | [60] |
| NiCr2O4 | MB | 90 | Vis | 40 | 20.23 | 2,1 | [58] |
| Ni0.6Mg0.4Cr2O4 | MB | 90 | UV-Vis | 65 | 15.16 | 2.36 | [58] |
| MgCr2O4 | MB | 90 | UV-Vis | 50 | 7.39 | 2.73 | [58] |
| (NiCd)0.5Cr2O4 | MB | 180 | UV-Vis | 73 | 38.5 | 2.2 | This study |
| CuCr2O4 | MB | - | Vis | 80.6 | 5-35 | 1.4 | [59] |
| ZnCr2O4 | MB | 70 | UV-Vis | 96.5 | 35 | 2.8 | [61] |

Tab.4: Rate constants for MB degradation using Ni0.5Cd0.5Cr2O4

|  | Ni0.5Cd0.5Cr2O4 |
| --- | --- |
| K-1(min-1) | 0.00741 |
| R2 | 0.99765 |