Supporting Information

Removal of U (VI) from aqueous solution by effective bio-adsorbent from walnut shell and cellulose composites stabilized iron sulfide nanoparticle

Huifang Wang, Renrong Liu, Li Han, Baowei Hu, Muqing Qiu*

School of Life Science, Shaoxing University, Huancheng West Road 508, Shaoxing, 312000, P. R. China

*Corresponding Author: Muqing Qiu, qiumuqing@usx.edu.cn

Preparation of biochar derived from walnut shell, FeS nanoparticles and CFeS-WS

The preparation of biochar derived from walnut shell and FeS nanoparticle were synthesized by the modified method (Lyu et al. 2018). In a word, the peanut shell was rinsed with distilled water, and dried for 24 h at 110 ℃. After cooling down, the dried walnut shell was ground into 1-2 cm pieces and carbonized for 2 h at 250 ℃ in a muffle furnace under oxygen-limited conditions. Then biochar was pulverized and sieved through a 60 meshes sieve. The biochar derived from walnut shell was gained.

The iron sulfide nanoparticles (FeS) were prepared according to the reaction of FeSO4 with Na2S. That is, 50 mL FeSO4 solution (0.05 mol/L) was added into 250 mL Erlenmeyer flask. Then, 50 mL Na2S solution (0.05 mol/L) was also added and mixed for 30 min under continuous aerating N2 and magnetic stirring condition. Then suspensions were sealed with rubber stopper and aged for 48 h. It could ensure the full growth of iron sulfide nanoparticles. Finally, the iron sulfide nanoparticles were obtained for experiments.

CFeS-WS was prepared with the composites of biochar, cellulose and FeS nanoparticles. According to the previous experimental results, it can be found that the mass ratio of ferrous sulfate, Na2S, cellulose and biochar is 2:2:1:4, which is optimum value. That is, under the magnetic stirring condition and continuous aerating nitrogen, the 5 g FeSO4 and 100 mL of anaerobic deionized water were mixed into the 250 mL Erlenmeyer flask. Then, added 10 g biochar from walnut shell to the Erlenmeyer flask and stirred them for 30 min under magnetic stirring condition. Next, added 2.5 g cellulose into the Erlenmeyer flask again, and stirred them for 30 min under magnetic stirring condition. Then, 5 g Na2S was added into the mixture solution, which was stirred them for 30 min under magnetic stirring condition. In the process of preparation, they were conducted under magnetic stirring condition and continuous aerating nitrogen in order to avoid oxidation of Fe2+ ions in solution. Then, the mixture solution was sealed with rubber stopper, which was placed in a constant temperature of 25℃ for 48 h. Then, they were freeze-dried for 12 h, which were washed with anaerobic deionized water for three times. Subsequently, they were freeze-dried for 12 h again. The efficient bio-adsorbent of CFeS-WS was obtained. The obtained materials (biochar, FeS nanoparticle, FeS-WS and CFeS-WS were prepared for tests.

Calculation of the removal rate and uptake capacity

The Eq.1-2 was used for the calculation of the removal rate ((%)) and uptake capacity ((mg/g)).

(1)

(2)

Where, (L) and (g) were the solution volume and the weight of adsorbent, respectively. (mg/L) and (mg/L) were equilibrium concentration and initial concentration, respectively.

Pseudo first-order kinetic model and Pseudo second-order kinetic model

Their mathematical expressions of pseudo first-order kinetic model and pseudo second-order kinetic model were shown as Eq.3-4 (Hummers ＆ Offeman 1958, Lagergren 1898).

(3)

(4)

Where (mg/g) and  (mg/g) are adsorption capacity of U(VI) ions solution by CFeS-WS at adsorption time  and adsorption equilibrium respectively.  (min-1) and  (min-1) are the adsorption rate constant.

Langmuir isotherm model and Freundlich isotherm model

Their mathematical expressions of Langmuir isotherm model and Freundlich isotherm model were displayed as Eq.5-6 (Langmuir 1918, Freundlich 1906).

(5)

Where (mg/g) was concentration of adsorbed U(VI) ions at equilibrium. (mg/g) was the maximum uptake capacity of U(VI) ions. (mg/L) was concentration of U(VI) ion at equilibrium and (L/mg) was constant.

(6)

Where (mg/g) was the amount of adsorbed U(VI) ions per unit mass of the adsorbent at equilibrium. (mg/L) was concentration of U(VI) ion at equilibrium.  and  were constant.

Calculation of thermodynamic parameters

They are Gibbs free energy ((kJ/mol)), enthalpy ((kJ/mol)) and entropy ((J/mol/K)) respectively. They can be calculated using the following Eq.7-9:

(7)

(8)

(9)

Where,  was the solution temperature (K), and  was the adsorption equilibrium constant. The value of  was the gas constant (8.314 J.mol-1.K-1), and  was the amount of adsorbate adsorbed per unit mass of adsorbate at equilibrium (mg/g). The value of  is the equilibrium concentration of the adsorbate (mg/L).

The species distribution of U(VI) ions at different pH

Fig.7 The species distribution of U(VI) ions using Visual MINTEQ (Version 3.0).

Reference

Freundlich, H.M.F. 1906. Uber die adsorption in lasungen. J. Phys. Chem., 57: 385-470.

Hummers, W.S. and Offeman, R.E. 1958. Preparation of graphitic oxide. J. Am. Chem. Soc., 80: 1339-1339.

Lagergren, S. 1898. Zur theorie der sogenannten adsorption geloster stoffe. Pseudo-second order model for sorption processes. Handlingar, 24:1-39.

Langmuir, I. 1918. The adsorption of gases on plane surface of glass, mica and platinum. J. Am. Chem. Soc., 40: 1361-1403.

Lyu, H.H., Zhao, H., Tang, J.C., Gong, Y.Y., Huang, Y., Wu, Q.H., Gao, B., Immobilization of hexavalent chromium in contaminated soils using biochar supported nanoscale iron sulfide composite, Chemosphere, 2018, 194, 360-369.