# Esterification of Bleached Kraft Pulp using Itaconic Anhydride – Supplementary information

Jelka Feldhusen1,2, Kent Malmgren3 Tomas Larsson4,5, Gunnar Westman1,2

- Department of Chemistry and Chemical Engineering, Chalmers University of Technology, Kemivägen 10, SE-41296, Gothenburg, Sweden

- Wallenberg Wood Science Center, Chalmers University of Technology, Kemivägen 10, SE-41296, Gothenburg, Sweden

- Senior R&D specialist, SCA, Sundvall, Sweden

- Department of Fibre and Polymer Technology, School of Chemical Science and Engineering, KTH Royal Institute of Technology, Teknikringen 56, SE-10044, Stockholm, Sweden

- Wallenberg Wood Science Center, KTH Royal Institute of Technology, Teknikringen 56, SE-10044, Stockholm, Sweden

## FTIR of all:

The following section displays the FTIR spectra for the different esterification methods.

BKPLE Kn – Varying time at 70 °C

Figure S1. Left: Complete FTIR spectra of BKPLE Kn reaction with varying reaction times at 70 °C. Right: Close-up of the carbonyl region.

BKPLE Kn – Varying molar ratios of AGU:ITA

Figure S2. Left: Complete FTIR spectra of BKPLE Kn reaction with varying equvalience of AGU:ITA. Right: Close-up of the carbonyl region.

BKPLE Gas

Figure S3. Left: Complete FTIR spectra of BKPLE Gas reaction with varying reaction times and temperatures. Right: Close-up of the carbonyl region.

BKPLE Kn – MCC reference reaction

Figure S4. FTIR of kneading reaction with MCC.

## Example of polyelectrolyte isotherm: BKPND

Figure S5. Adsorption isotherm for fibers titrated with poly(BRENE) for assessment of total fiber charge. Adsorbed polymer is plotted against equilibrium polymer concentration.

| Sample | Sample weight (g) | Filter | Filter + Klason lignin | Klason lignin (g) | K. Lignin content (%) | Absorbance | Soluble Lignin Conc. (g/dm3) | Soluble Lignin (g) | Sol. Lignin content (%) | TOTAL LIGNIN (%) | Arabinose | Galactose | Glucose | Xylose | Mannose | Arabinose | Galactose | Glucose | Xylose | Mannose | TOTAL sugars % | Total detected |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BKP1 | 0,20 | 818 | 832 | 0,0014 | 0,70% | 2430 | 0,002 | 0,0022 | 1,1% | 1,80% | 1,2786 | 0,4662 | 161,4744 | 15,569 | 12,4833 | 0,603 | 0,225 | 79,036 | 8,702 | 6,218 | 94,79% | 96,59% |
| BKP2 | 0,20 | 726 | 732 | 0,0006 | 0,30% | 2448 | 0,002 | 0,0022 | 1,1% | 1,40% | 1,3247 | 0,4835 | 168,1702 | 16,118 | 12,9590 | 0,621 | 0,232 | 81,742 | 8,947 | 6,411 | 97,95% | 99,35% |
| BKPLE1 | 0,13 | 1410 | 1412 | 0,0002 | 0,15% | 2256 | 0,002 | 0,0021 | 1,5% | 1,69% | 1,1917 | 0,4535 | 165,1041 | 13,475 | 12,2383 | 0,585 | 0,228 | 84,093 | 7,838 | 6,344 | 99,09% | 100,78% |
| BKPLE2 | 0,14 | 1492 | 1495 | 0,0003 | 0,21% | 2445 | 0,002 | 0,0022 | 1,5% | 1,76% | 1,3884 | 0,5247 | 189,6902 | 15,538 | 14,0848 | 0,633 | 0,245 | 89,686 | 8,389 | 6,777 | 105,73% | 107,49% |

## Carbohydrate analysis

Klason analysis was performed on BKP and BKPLE, as presented in the Table S1.