Supporting information

ZnO microsphere decorated with Au nanoparticles for SERS detection and removal of trace 2-Mercaptobenzothiazole in environmental water

Jiangli Shi1, Boran Zhang1, Li Zhang, Xinling Liu, Yiping Wu, Ying Wen, Haifeng Yang*, Xiaoyu Guo*

The Education Ministry Key Lab of Resource Chemistry, Joint International Research Laboratory of Resource Chemistry, Ministry of Education, Shanghai Key Laboratory of Rare Earth Functional Materials, Shanghai Municipal Education Committee Key Laboratory of Molecular Imaging Probes and Sensors, Shanghai Frontiers Science Center of Biomimetic Catalysis and College of Chemistry and Materials Science. Shanghai Normal University, Shanghai, 200234, China

*Corresponding author

Xiaoyu Guo

Address correspondence to gxy2012@shnu.edu.cn

Haifeng Yang

Address correspondence to hfyang@shnu.edu.cn

1These authors contributed equally to this work.

Calculation of the size of AuNPs

The diameter of the AuNPs was calculated according to the following equation [1]:

d(nm) = 2.511 λmax(nm) - 1294.8

λmax is the maximum absorption wavelength of Au NPs. In this work, λmax is 533 nm. d is the diameter of the Au NPs, and the value of 43.6 nm was obtained through calculation.

Calculation of the band gap energy of F-ZnO MPs and S-ZnO MPs

The band gap energy of the semiconductor was determined based on the UV–Vis absorption spectra and calculated using the Tauc equation:

αhν1n=Αhν-Εg

α is the absorption constant, h is the Planck constant, ν is the frequency, Α is the constant, Εg is the semiconductor band gap width, ZnO is a direct bandgap semiconductor n = 1/2.

Determination of the energy level diagram of F-ZnO MPs and S-ZnO MPs

Based on the Mott–Schottky plot (Figure 4B), The flat-band potential (Efb) was determined from the intercept of the linear portion of the curve on the voltage axis, yielding Efb (vs. Ag/AgCl) = -1.17 V. This value was subsequently converted to the normal hydrogen electrode scale, resulting in Efb (vs. NHE) = -0.97 V. Further calculations provided the conduction band (ECB) and valence band (EVB) potentials, with ECB = -1.07 V and EVB = 2.03 V. When referenced to the vacuum energy level (0 eV), the prepared S-ZnO exhibits ECB = -3.783 eV and EVB = -6.883 eV.

Fig. S1 XRD patterns of (A) F-ZnO MPs and F-ZnO-Au MPs, (B) S-ZnO MPs and S-ZnO-Au MPs

Fig. S2 XPS spectra of ZnO (a), Zn 2p (b), O1s(c), and ZnO-Au (d), Zn 2p (e), Au (f)

Fig. S3 SERS spectra of 4-MPy on substrates fabricated through adding different volume of reducing agent (1% trisodium citrate) (A, C) and reaction with different time (C, D). (A, B) are for F-ZnO MPs and (C, D) are for S-ZnO MPs

Fig. S4 SERS spectra of 4-MPy on F-ZnO-Au MPs (A) and S-ZnO-Au MPs (B) collected by using different laser

Fig. S5 SERS spectra of 4-MPy with different concentrations on (A) F-ZnO-Au MPs and (B) S-ZnO-Au MPs

Calculation of EF

The enhancement factor (EF) of S-ZnO-Au MPs for 4-MPy was calculated according to the follow formula:

EF = (CRaman ISERS) / (CSERS IRaman )

Where CRaman (here is 1×10-1 mol/L) is the concentration of 4-MPy could generate normal Raman signal and CSERS (here is 1×10-8 mol/L) is the concentration of 4-MPy on S-ZnO-Au MPs. ISERS  (ISERS = 6567, reading from SERS spectrum in Figure S6) and IRaman (IRaman=1195, reading from Raman spectrum in Figure S6) are the SERS intensity of 4-MPy on S-ZnO-Au MPs and the normal Raman intensity of 4-MPy at 1105 cm−1, respectively. Raman spectrum of 4-MPy and SERS spectrum of 4-MPy on S-ZnO-Au MPs are shown in Figure S6. Put the above values into the formula, EF of 5.5×107 is obtained:

EF=10-1×656710-8 ×1195 =5.5×107

Fig. S6 (a) Raman spectrum of 4-MPy (1×10-1 mol/L) and (b) SERS spectrum of 4-MPy (1×10-8 mol/L) on the substrate of S-ZnO-Au MPs

Fig. S7 3D Raman spectra of 4-MPy on S-ZnO-Au MPs and corresponding histogram at 1105 cm-1: (A, B) Raman response from randomly selected 20 points on the same substrate; (C, D) Raman response with the change of storage time; (E, F) Raman response among different batches substrates

Fig. S8 Raman spectrum of MBT and its SERS spectrum on S-ZnO-Au MPs

Table S1. The assignments of bands in SERS spectrum of 4-MPy on S-ZnO-Au MPs substrates.

| Wavenumber/cm-1 | Assignments |
| --- | --- |
| 1031 | ring breathing |
| 1064 | β (CH) b2 |
| 1107 | ν (ring breathing) / ν (C-S) |
| 1219 | β (CH) |
| 1320 | ν (C-H) b2 |
| 1588 | ν (C-C) with deprotonated nitrogen |
| 1602 | ν (C-C) with protonated nitrogen |

Table S2. The assignments of bands in a SERS spectrum of MBT on S-ZnO-Au MPs substrates.

| Wavenumber/cm-1 | Assignments |
| --- | --- |
| 397, 609, 637, 716 | ν(C-S) |
| 496, 1112 | β (C-H) in plane |
| 893 | β (C-H) out plane |
| 1127 | β (C-H) |
| 1242, 1323, 1395, 1506 | ν (C-C) |
| 1372 | ν(C=N) |
| 1593 | ν (C-H) in plane |

The limit of detection of the S-ZnO-Au MPs for the detection of MBT by confocal Raman systems:

According to the stand of IUPAC, the limit of detection (LOD) was calculated following the formula:

LOD=3×RSD×BEC

The RSD value is the relative standard deviation for repeating the same experiment.

The BEC value is the absolute value of the intercept between the linear regression equation and the x-axis.

The specific formula is as follows:

LOD = 3×2.54%×10-8.73 mol/L= 1.42×10-10 mol/L

[1] Muhammad Iqbal, Gisele Usanase, Kafia Oulmi, Fairouz Aberkane, Tahar Bendaikha, Hatem Fessi, Nadia Zine, Géraldine Agusti, El-Salhi Errachid, Abdelhamid Elaissari. Preparation of gold nanoparticles and determination of their particles size via different methods. Materials Research Bulletin 79 (2016) 97–104.