A co-delivery strategy of abemaciclib combined with vitamin E succinate based on hyaluronic acid- modified calcium phosphate to enhance anti-cancer effect

Yuanyuan Liu, Na Gan, Shuangshuang Zhang, Qiaomei Sun*, Xin Wei, Xiuyun Ren, Xi Xiang, , and Hui Li*

School of Chemical Engineering, Sichuan University, Chengdu 610065, China

*Correspondence author: Hui Li. Tel: +86-28-85405220. E-mail: lihuilab@sina.com (Hui Li)

 *Corresponding author. E-mail address: qiaomeisun@163.com (Qiaomei Sun).

EDS analysis results show that the carbon content increases after CaP coated with HA layer, which is related to the high proportion of carbon in the HA framework (Fig. S1 B). The Ca/P ratio 1.5 further indicates that the synthesized CaP is a kind of calcium-deficient hydroxyapatite with poor crystallinity[36]. Similar to CaP/ABE-VES, after HA/CaP is loaded with drugs, the content of carbon and oxygen increases (Fig. S1 D). This obvious element change is attributed to the addition of two drug molecules. In addition, the increased fluorine element in the EDS diagram of HA/CaP/ABE-VES can be found, which shows the presence of ABE in the nanomaterial. In general, EDS confirmed the presence of HA in the outer layer of CaP, and compared with CaP/ABE-VES, the content of C, O, and F elements in HA/CaP/ABE-VES also increased, indicating that the incorporation of HA can increase the drug loading of nanomaterials. This may be due to the carboxyl group of HA can provide more sites for drug molecules, which is consistent with the XRD results.

Fig. S1 EDS spectra of CaP (A), HA/CaP (B), CaP/ABE-VES (C), and HA/CaP/ABE-VES (D)