Supplementary Information

Syntheses of microcrystalline cellulose-graft bottlebrush copolymer elastomers with hydrogen bonding interactions to endow applicable mechanical property

Wanyu Wang, Rou Chen, Xuehui Wang, Huanjuan Sun*, Zhigang Wang*

Shared first authorship: Wanyu Wang and Rou Chen contributed equally to this manuscript.

WY Wang, R Chen, XH Wang, HJ Sun

State Key Laboratory of Precision and Intelligent Chemistry, Department of Polymer Science and Engineering, University of Science and Technology of China, Hefei, Anhui 230026, P. R. China

Corresponding author: Huanjuan Sun, E-mail: shjjj@mail.ustc.edu.cn (HJ Sun)

ZG Wang

College of Materials Engineering, Fujian Agriculture and Forestry University, Fuzhou 350002, P. R. China

Corresponding author: Zhigang Wang, E-mail: zgwang@fafu.edu.cn (ZG Wang)

Table S1. Synthetic formulae and characteristics for MCC-g-P(nBA-co-tBA) graft copolymers.

| sample codeᵅ | feed molar ratioᵇ | feed molar ratio of nBA to tBA | measured molar ratio of nBA to tBAᶜ | Tgd (oC) |
| --- | --- | --- | --- | --- |
| tBA350-MCC0.9 | 1/650/350 | 1.86/1 | 1.76/1 | -22.2 |
| tBA320-MCC0.9 | 1/680/320 | 2.13/1 | 1.98/1 | -24.7 |
| tBA300-MCC0.8 | 1/700/300 | 2.33/1 | 2.12/1 | -26.5 |
| tBA250-MCC0.9 | 1/750/250 | 3.0/1 | 2.79/1 | -30.3 |
| tBA220-MCC1.1 | 1/780/220 | 3.55/1 | 3.06/1 | -33.1 |

ᵅSample codes are defined as follows: the numbers behind “tBA”, and “MCC” stand for the molar numbers of tBA and MCC contents (percentage), respectively. ᵇMolar ratio: MCC-BiB/nBA/tBA. ᶜMeasured by 1H NMR spectroscopy. dMeasured by DSC.

Fig. S1. Photos of tBA250-MCC0.9 (a) and dumbbell-shaped AA250-MCC0.9 (b) at room temperature.

Fig. S2. 1H NMR spectrum for MCC-BiB in DMSO-d6.

Fig. S3. 1H NMR spectra for MCC-g-P(nBA-co-tBA) in CDCl3, (a) tBA350-MCC0.9 and tBA320-MCC0.9 and (b) tBA300-MCC0.8 and tBA220-MCC1.1.

Fig. S4. 1H NMR spectra for MCC-g-P(nBA-co-AA) in DMSO-d6, (a) AA350-MCC0.9 and AA320-MCC0.9 and (b) AA300-MCC0.8 and AA220-MCC1.1.

Fig. S5. Mass loss (a) and derivative mass loss curves (b) for MCC and MCC-BiB from TGA measurement.