Tables

| Table 1 Pd@h-Fe2O3@C catalyzed Suzuki-Miyaura reaction of various halides with terminal alkynesa |  |  |  |  |
| --- | --- | --- | --- | --- |
| Product | X | R1 | Time (min) | Yieldb (%) |
| 3a | I | H | 60 | 95 |
| 3b | I | 4-Me | 80 | 80 |
| 3c | I | 4-OMe | 55 | 90 |
| 3d | I | 4-COMe | 70 | 85 |
| 3e | I | 4-NO2 | 60 | 80 |
| 3f | Br | H | 125 | 70 |
| 3g | Br | 4-Me | 105 | 77 |
| 3h | Br | 4-NH2 | 140 | 80 |
| 3i | Cl | H | 165 | 63 |
| 3j | Cl | 4-NH2 | 150 | 80 |
| 3l | Cl | 2-NO2 | 130 | 82 |
| 3m | Cl | 4-Me | 170 | 75 |
| a Reaction condition: aryl halide (1 mmol), boronic acid (1.2 mmol), Pd@h-Fe2O3@C (0.5 mol%), Na2CO3 (2 mmol) in water:EtOH (6 mL) at 75 °C. b Isolated yields. |  |  |  |  |

| Table 2 Pd@h-Fe2O3@C catalyzed Sonogashira reaction of various halides with terminal alkynesa |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Product | X | R1 | R2 | Time (h:min) | Yieldb (%) |
| 5a | I | H | C6H5 | 00:35 | 93 |
| 5b | I | 4-Me | C6H5 | 00:45 | 98 |
| 5c | I | 4-OMe | C6H5 | 00:25 | 95 |
| 5d | I | 4-COMe | C6H5 | 00:40 | 90 |
| 5e | I | H | CH2OH | 01:00 | 88 |
| 5f | I | 4-Me | CH2OH | 01:15 | 85 |
| 5g | Br | H | C6H5 | 01:20 | 98 |
| 5h | Br | H | CH2OH | 01:50 | 78 |
| 5i | Br | 4-Me | C6H5 | 02:10 | 65 |
| 5j | Br | 4-NH2 | C6H5 | 02:45 | 72 |
| 5k | Cl | H | C6H5 | 03:00 | 80 |
| 5l | Cl | H | CH2OH | 03:45 | 70 |
| 5m | Cl | 4-NH2 | C6H5 | 05:10 | 55 |
| 5n | Cl | 2-NO2 | C6H5 | 04:55 | 55 |
| 5o | Cl | 4-Me | C6H5 | 05:15 | 58 |
| a Reaction condition: aryl halides (1.0 mmol), terminal alkynes (1.2 mmol), Pd@h-Fe2O3@C (0.35 mol%), Na2CO3 (2.0 mmol) in H2O (5.0 mL) at 50 ˚C b Isolated yields. |  |  |  |  |  |

| Table 3 The study of loading and leaching of Pd element by ICP-AES analysis on the catalytic activity of the prepared catalysts in Sonogashira model reactiona |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Loading Pd (mmol.g-1) | Leaching Pd (mmol.g-1) | Catalytic activity |  |
|  |  |  |  | Time (h:min) | Yieldb (%) |
| 1 | Pd@h-Fe2O3 | 0.019 | 0.010 | 1:20 | 35 |
| 2 | Pd@h-Fe2O3@MRF | 0.030 | 0.019 | 1:20 | 70 |
| 3 | Pd@h-Fe2O3@MRF-C | 0.045 | 0.0079 | 1:20 | 88 |
| 4 | Pd@h-Fe2O3@glu | 0.023 | 0.020 | 1:20 | 50 |
| 5 | Pd@h-Fe2O3@glu-MRF | 0.039 | 0.013 | 1:20 | 80 |
| 6 | Pd@h-Fe2O3@glu-RF | 0.034 | 0.014 | 1:20 | 80 |
| 7 | Pd@h-Fe2O3@glu-RF-C | 0.066 | 0.0052 | 1:20 | 92 |
| 8 | Pd@h-Fe2O3@C | 0.075 | 0.0031 | 1:20 | 95 |
| a Reaction condition: aryl halides (1.0 mmol), terminal alkynes (1.2 mmol), catalyst (0.35 mol%), Na2CO3 (2.0 mmol) in H2O (5.0 mL) at 50 ˚C b Isolated yields. |  |  |  |  |  |