Supporting Information

Terminal Groups Dependent Near-Field Enhancement Effect of Ti3C2Tx Nanosheets

Ying-Ying Yang1, Wen-Tao Zhou1, Wei-Long Song1, Qing-Quan Zhu1, Hao-Jiang Xiong1, Jue Zhang1, Sheng Cheng2, Pai-Feng Luo1, Ying-Wei Lu1, 3,

1School of Materials Science and Engineering, Hefei University of Technology, Hefei 230009, P. R. China

2Instrumental Analysis Center, Hefei University of Technology, Hefei 230009, P. R. China

3Engineering Research Center of High Performance Copper Alloy Materials and Processing, Ministry of Education, Hefei University of Technology, Hefei 230009, P. R. China

Figure S1. Zeta potentials of ML-Ti3C2Tx and FL-Ti3C2Tx

Figure S2. (a) Optical photographs of ML-Ti3C2Tx and FL-Ti3C2Tx. (b) Optical photographs of ML-Ti3C2Tx and FL-Ti3C2Tx soaking in R6G solutions.

Table S1. Surface states and corresponding relative contents extracted from the XPS Ti 2p, C 1s and O 1s spectra of ML-Ti3C2Tx and FL-Ti3C2Tx

| Sample IDs |  |  | ML-Ti3C2Tx | FL-Ti3C2Tx |
| --- | --- | --- | --- | --- |
| Region | BE (eV) | Assigned to | Fraction (%) | Fraction (%) |
| Ti 2p* | 455.0/461.2 | Ti-C1-3 | 17.31 | 9.80 |
|  | 455.8/461.8 | Ti(II) 1,3 | 41.47 | 46.35 |
|  | 457.2/462.9 | Ti-O1,2 | 28.10 | 28.02 |
|  | 459.0/464.7 | TiO21 | 6.15 | 8.37 |
|  | 460.2/466.5 | C-Ti-Fx(III) 1 | 6.90 | 7.46 |
| C 1s | 281.8 | C-Ti-Tx1 | 17.23 | 21.27 |
|  | 284.6 | C-C1,2 | 26.17 | 44.62 |
|  | 285.4 | C-O1,2 | 53.00 | 28.58 |
|  | 287.8 | O-C=O/C-F2,3 | 3.60 | 5.53 |
| O 1s | 529.4 | Adsorbed Oxygen4 | 11.54 | - |
|  | 529.9 | TiO21 | 13.98 | 19.60 |
|  | 531.2 | C-Ti-Ox1 | 19.91 | 11.64 |
|  | 532.2 | C-Ti-OHx1,5 | 54.57 | 33.21 |
|  | 533.1 | H2Oads or C-OH1 | - | 35.55 |

* XPS Ti 2p spectra presents Ti 2p3/2 (lower BE) and Ti 2p1/2 (higher BE) components

Figure S3. TEM images of (a) Ag/ML-Ti3C2Tx and (b) Ag/FL-Ti3C2Tx. The insets are the size distributions of Ag NPs in the corresponding samples.

References

- Halim J, Cook K M, Naguib M, Eklund P, Gogotsi Y, Resen J, Barsoum MW (2016) X-ray photoelectron spectroscopy of select multi-layered transition metal carbides (MXenes). Appl. Surf. Sci. 362: 406-417.

- Han M, Yin X, Li X, Anasori B, Zhang L, Cheng L, Gogotsi Y (2017) Laminated and two-dimensional carbon-supported microwave absorbers derived from MXenes. ACS Appl. Mater. Interfaces 9: 20038-20045.

- Tong Y, He M, Zhou Y, Zhong X, Fan L, Huang T, Liao Q, Wang Y (2018) Electromagnetic wave absorption properties in the centimetre-band of  Ti3C2Tx MXenes with diverse etching time. J. Mater. Sci.-Mater. El. 29: 8078-8088.

- Peng C, Yang X, Li Y, Yu H, Wang H, Peng F (2016) Hybrids of two-dimensional Ti3C2 and TiO2 exposing {001} facets toward enhanced photocatalytic activity. ACS Appl. Mater. Interfaces 8: 6051-6060.

- Mashtalir O, Naguib M, Mochalin VN, Dall’Agnese Y, Heon M, Barsoum MW, Gogotsi Y (2013) Intercalation and delamination of layered carbides and carbonitrides. Nat.Commum. 4: 1-7.

Correspondence: luyw@hfut.edu.cn

1School of Materials Science and Engineering, Hefei University of Technology, Hefei 230009, P. R. China

3Engineering Research Center of High Performance Copper Alloy Materials and Processing, Ministry of Education, Hefei University of Technology, Hefei 230009, P. R. China