Supporting Information

MOCVD Growth of Covalent and 2D Ga–Se: A Raman Microscopy-Based Phase Validation

Nils Fritjof Langlotz1,2, Robin Günkel1,2, Dominik Muth1,2, Imad Limame3, Naghmeh Ghadghooni1,2, Max Bergmann1,2, Marcel Kröner1,2, Jürgen Belz1,2, Andreas Beyer1,2, Stephan Reizenstein3, Marina Gerhard1,2, Kerstin Volz1,2*

1mar.quest | Marburg Center for Quantum Materials and Sustainable and Technologies, Philipps-Universität Marburg, 35032 Marburg, Germany

2Department of Physics, Philipps-Universität Marburg, Hans Meerwein Str. 6, 35032 Marburg, Germany

3Institute of Physics and Astronomy, Technical University of, Hardenbergstraße 36, 10623 Berlin, Germany

*kerstin.volz@physik.uni-marburg.de

Table of contents:

S1.		Evaluation of GaSe on Sapphire Substrates at 450 °C
S2.		Evaluation of GaSe on Sapphire Substrates at 500–550 °C
S3.		Evaluation of Ga2Se3 on Sapphire Substrates
S4.		Evaluation of Ga2Se3 on GaP/Si Substrates
S5.		Comparison of GaP/Si and Sapphire Substrates
S6.		EDX Analysis of the Ga2Se3 Layer on GaP/Si (Figure 2e)
S7.		EDX Analysis of GaSe on GaP/Si (Figure 3a,c)
S8. 		MOCVD Reactor Setup

Figure S1: Morphology and spectroscopic characterization of GaSe grown at 450 °C on sapphire: (a) AFM image of a cluster consisting of a central grain with layered flakes growing outward. (b) AFM image showing a grain from which an in-plane layered structure grows, featuring visible screw dislocations, with a 3.0× magnified inset of an individual screw dislocation. (c) AFM image of hexagonal flakes that are still not coalesced. (d) Raman spectra corresponding to (a–c), showing only GaSe- and substrate-related Raman modes.[1–7]

Figure S2: Morphology and spectroscopic characterization of GaSe grown at 500 and 550 °C on sapphire: (a) AFM image of out-of-plane flakes. (b) AFM image of non-coalesced hexagonal and trigonal flakes showing screw dislocations, with a 2.3× magnified inset of an individual screw dislocation. (c) AFM image of hexagonal flakes that are still not coalesced. (d) AFM image of screw dislocations in hexagonal and trigonal flakes with a fully coalesced underlying layer. (e) Raman spectra corresponding to (a–d), showing only GaSe- and substrate-related Raman modes.[1–7]

Figure S3: Morphology and spectroscopic characterization of Ga₂Se₃ grown at 450 and 550 °C on sapphire: (a) AFM image of Ga2Se3 clusters. (b) AFM image of a coalesced layer with clusters and rod-like structures on it. (c) AFM image of Ga2Se3 clusters. (d) AFM image of Ga2Se3 clusters. (e) AFM image of layered Ga2Se3 and rod-like structures. (f) AFM image of layered and clustered Ga2Se3 structures. (g) Raman spectra corresponding to (a) and (b), showing only Ga2Se3- and substrate-related Raman modes.[2,3,8–11] (h) Raman spectra corresponding to (c–f), showing only Ga2Se3- and substrate-related Raman modes.[2,3,8–11]

Figure S4. Morphology and spectroscopic characterization of Ga2Se3 grown at 600 °C on GaP/Si: (a) AFM image of Ga2Se3 clusters with rod-like features. (b) AFM image of Ga2Se3 clusters with rod-like features oriented in two perpendicular directions. (c) AFM image of coalesced Ga2Se3 layers and clusters. (d) AFM of small Ga2Se3 patches. (e) Raman spectra corresponding to (a–d), showing only Ga2Se3- and substrate-related Raman modes.[8–15]

Figure S5: Morphology and spectroscopic characterization of GaP/Si and sapphire substrates: (a) AFM image of GaP steps on the GaP/Si substrate. (b) AFM image of the sapphire substrate showing polishing lines and a localized surface contamination. (c) Raman spectra of the GaP/Si substrate, showing GaP peaks (marked) and additional signals from Si.[12–15] (d) Raman spectra of sapphire, showing four characteristic sapphire-related Raman peaks (marked).[2,3]

Figure S6: EDX Analysis of the Covalently bonded Ga2Se3 Layer on GaP/Si: (a) Zoomed-out HAADF image of the Ga2Se3 layer from Figure 2(e) of thin Ga2Se3 layer. (b) EDX map corresponding to (a). (c) Averaged EDX line profile across the Ga2Se3, GaP, and Si interface extracted from the EDX map shown in (b), illustrating the 2:3 ratio of Ga and Se in the covalently bonded layer.

Figure S7: EDX Analysis of the 2D GaSe on GaP/Si: (a) HAADF image of GaSe on GaP/Si from Figure 3(a,c) (b) EDX map corresponding to (a). (c) Averaged EDX line profile across the GaSe and GaP interface extracted from the EDX map shown in (b), illustrating a 1:1 ratio of Ga and Se in the van der Waals bonded layeres.

Figure S8: MOCVD reactor setup

References

1.	Rodriguez, R. D. et al. Selective Raman modes and strong photoluminescence of gallium selenide flakes on sp2 carbon. Journal of Vacuum Science & Technology B, Nanotechnology and Microelectronics: Materials, Processing, Measurement, and Phenomena 32; 10.1116/1.4881995 (2014).

2.	Vural, S. & Sari, Ö. Synthesis and characterization of SDS assistant α-alumina structures and investigation of the effect of the calcination time on the morphology. Colloid Polym Sci 297, 107–114; 10.1007/s00396-018-4442-4 (2019).

3.	Kadleı́ková, M., Breza, J. & Veselý, M. Raman spectra of synthetic sapphire. Microelectronics Journal 32, 955–958; 10.1016/S0026-2692(01)00087-8 (2001).

4.	Grzonka, J., Claro, M. S., Molina‐Sánchez, A., Sadewasser, S. & Ferreira, P. J. Novel Polymorph of GaSe. Adv Funct Materials 31; 10.1002/adfm.202104965 (2021).

5.	Diep, N. Q. et al. Growth Mode Transition in Two-Dimensional GaSe on Three-Dimensional GaN/Sapphire Platform: Implication for Self-Powered Photodetection. ACS Appl. Nano Mater. 7, 3042–3049; 10.1021/acsanm.3c05343 (2024).

6.	Avdienko, P. et al. Structural and Optical Properties of GaSe/GaAs(001) Layers Grown by Molecular Beam Epitaxy. Acta Phys. Pol. A 136, 608–612; 10.12693/APhysPolA.136.608 (2019).

7.	Diep, N. Q. et al. Screw-Dislocation-Driven Growth Mode in Two Dimensional GaSe on GaAs(001) Substrates Grown by Molecular Beam Epitaxy. Scientific reports 9, 17781; 10.1038/s41598-019-54406-5 (2019).

8.	Bletskan, D. I., Kabatsii, V. N. & Kranjčec, M. Photoelectric properties of ordered-vacancy Ga2Se3 single crystals. Inorg Mater 46, 1290–1295; 10.1134/S0020168510120034 (2010).

9.	Emde, M. von der et al. MOCVD growth of Ga2Se3 on GaAs(100) and GaP(100): a Raman study. Applied Surface Science 104-105, 575–579; 10.1016/S0169-4332(96)00205-X (1996).

10.	Märkl, A., Emde, M. von der, Nowak, C., Richter, W. & Zahn, D. Investigation of Se capping of epitaxial Ga 2 Se 3 layers. Surface Science 331-333, 631–635; 10.1016/0039-6028(95)00356-8 (1995).

11.	Finkman, E., Tauc, J., Kershaw, R. & Wold, A. Lattice dynamics of tetrahedrally bonded semiconductors containing ordered vacant sites. Phys. Rev. B 11, 3785–3794; 10.1103/PhysRevB.11.3785 (1975).

12.	Seo, H. W., Bae, S. Y., Park, J., Yang, H. & Kim, S. Synthesis of gallium phosphide nanowires via sublimation method. Chem. Commun., 2564–2565; 10.1039/B207995J (2002).

13.	Dubey, R. L., Dubey, S. K., Yadav, A. D., Sulania, I. & Kanjilal, D. Raman scattering and FTIR studies of 100 MeV Fe 9+ ion-irradiated gallium phosphide. Radiation Effects and Defects in Solids 166, 743–748; 10.1080/10420150.2011.578633 (2011).

14.	Abdullayeva, S. H. et al. GaInPN/Si heterostructure growth by metal-organic vapour phase epitaxy. Fizika (Baku) 15, 18–23 (2009).

15.	Lee, W.-J. & Chang, Y.-H. Growth without Postannealing of Monoclinic VO2 Thin Film by Atomic Layer Deposition Using VCl4 as Precursor. Coatings 8, 431; 10.3390/coatings8120431 (2018).