Appendix-A: Estimation of volumetric electrical-resistivity and coating resistance

Insulation resistance of an electrical-cable is given by the following relation:

Ri = (ϱ2Πl) ln Rr  ……………………………….Eq. (A.1)

Where, Ri = Insulation resistance of the cable (Ω), ϱ = Volumetric electrical-resistivity of insulation material (Ω-m), l = Length of the insulation over the cable (m), R = Outer radius of the cable with insulation (m) and r = Outer radius of the conductor (m).

Using data from Table-I, II, III, IV and V and taking the enveloping IR values at each temperature:

| Test Campaign | Probe | Insulation Resistance (Ω) | Average coating thickness (mm) | Coated length (m) | Temperature (ºC) | Resistivity (Ω-cm) | Coating resistance (Ω-m2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | P1 | 6 x 109 | 0.495 | 0.085 | 300 | 6.65 x 1011 | 3.29 x 106 |
|  |  | 6.18 x 109 | 0.495 | 0.085 | 300 | 6.85 x 1011 | 3.39 x 106 |
|  |  | 0.822 x 109 | 0.495 | 0.085 | 350 | 9.12 x 1010 | 4.51 x 105 |
|  |  | 1 x 109 | 0.495 | 0.085 | 350 | 1.11 x 1011 | 5.49 x 105 |
|  | P2 | 1 x 108 | 0.212 | 0.065 | 300 | 1.74 x 1010 | 3.68 x 104 |
|  |  | 3.15 x 108 | 0.212 | 0.065 | 300 | 5.47 x 1010 | 1.16 x 105 |
|  |  | 0.835 x 108 | 0.212 | 0.065 | 350 | 1.45 x 1010 | 3.08 x 104 |
|  |  | 1 x 108 | 0.212 | 0.065 | 350 | 1.74 x 1010 | 3.68 x 104 |
| 2 | P3 | 2.90 x 108 | 0.429 | 0.060 | 300 | 2.55 x 1010 | 1.09 x 105 |
|  |  | 4.57 x 108 | 0.429 | 0.060 | 300 | 4.01 x 1010 | 1.72 x 105 |
|  |  | 1.29 x 108 | 0.429 | 0.060 | 350 | 1.13 x 1010 | 4.86 x 104 |
|  |  | 2.99 x 108 | 0.429 | 0.060 | 350 | 2.63 x 1010 | 1.13 x 105 |
|  |  | 0.583 x 108 | 0.429 | 0.060 | 400 | 5.12 x 109 | 2.20 x 104 |
|  |  | 0.768 x 108 | 0.429 | 0.060 | 400 | 6.74 x 109 | 2.89 x 104 |