Table 1. Basic properties of the soil studied.

| Index properties | As-received | Passing 2 mm |
| --- | --- | --- |
| Standard compaction test Maximum dry density: g/cm3 | 1920 |  |
| Optimum water content (%) | 11 |  |
| Cement content by mass (%) | 8 |  |
| Grains size distribution |  |  |
| Gravel content: % | -- |  |
| Sand content: % | 95 | 88 |
| Silt content: % | 5 | 12 |
| Specific gravity (soil + cement) |  | 2.82 |
| Grain characteristics |  |  |
| Cc | 1.5 | 2.3 |
| Cu | 2.4 | 9.0 |
| Soil classification based on USCS. (ASTM, 2011) | Poorly graded sand with silt (SP – SM) | Well-graded sand with silt (SW – SM) |

Table 2. Test setup and locations of cracks characterization.

| Sample ID | Observable cracks after cycle 3 |
| --- | --- |
| OH-100 |  |
| SH-80 |  |
| SH-60 | Direction of crack travel A large crack that appears to split the sample into an upper and lower portions |

152.4 mm

Table 3. Physical observation of samples after three wetting-drying cycles.

| Sample ID | Images of Samples |
| --- | --- |
| Samples in setup condition | SH-80 OH-100 SH-60 |
| OH-100 |  |
| SH-80 |  |
| SH-60 | 762 mm |

NB: White arrows indicate a hypothesized development, concentration, and direction of travel of tensile stresses.

Table 4. Samples of images used for cracks characterization.

| Sample ID | Original Image | Cycle -1 | Cycle - 2 | Cycle - 3 |
| --- | --- | --- | --- | --- |
|  |  | Isolated Cracks and Pores (Scale: 500µm) |  |  |
| OH-100-Loc 1 |  |  |  |  |
| OH-100-Loc 3 |  |  |  |  |
| SH-80-Loc 1 |  |  |  |  |
| SH-80-Loc 3 |  |  |  |  |
| SH-60-Loc 1 |  |  |  |  |
| SH-60-Loc 3 |  |  |  |  |

Table 5. Pore area fraction and size variation with cycles for different treatment.

| Pore Area Fraction (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Test ID | OH-100 |  |  |  |  |  | SH-80 |  |  |  |  |  | SH-60 |  |  |  |  |  |
| Location | 1 | 2 | 3 | 4 | 5 | 6 | 1 | 2 | 3 | 4 | 5 | 6 | 1 | 2 | 3 | 4 | 5 | 6 |
| Cycle 1 | 33 | 33 | 35 | 34 | 30 | 34 | 32 | 30 | 39 | 38 | 32 | 11 | 37 | 30 | 26 | 42 | 37 | 38 |
| Cycle 2 | 33 | 25 | 27 | 31 | 27 | 34 | 26 | 25 | 25 | 35 | 35 | 6 | 22 | 26 | 22 | 26 | 38 | 29 |
| Cycle 3 | 24 | 27 | 22 | 19 | 28 | 21 | 21 | 18 | 25 | 25 | 18 | 23 | 12 | 21 | 12 | 19 | 17 | 24 |
| Mean | 30 | 28 | 27 | 27 | 28 | 29 | 26 | 24 | 29 | 32 | 27 | 11 | 22 | 26 | 19 | 28 | 29 | 30 |
| ± SD | 5 | 4 | 6 | 8 | 2 | 7 | 5 | 6 | 8 | 7 | 9 | 9 | 13 | 5 | 7 | 12 | 12 | 7 |
| Pore Size Variation (μm) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Cycle 1 | 421 | 354 | 376 | 366 | 347 | 208 | 374 | 369 | 375 | 430 | 326 | 185 | 323 | 311 | 297 | 342 | 320 | 319 |
| Cycle 2 | 353 | 319 | 333 | 341 | 319 | 347 | 293 | 292 | 280 | 341 | 335 | 176 | 262 | 282 | 270 | 290 | 327 | 303 |
| Cycle 3 | 311 | 341 | 326 | 306 | 345 | 328 | 275 | 279 | 308 | 302 | 269 | 306 | 241 | 265 | 243 | 265 | 251 | 280 |
| Mean | 359 | 338 | 344 | 337 | 337 | 287 | 312 | 311 | 318 | 354 | 309 | 215 | 273 | 285 | 269 | 297 | 297 | 300 |
| ± SD | 56 | 18 | 27 | 30 | 16 | 75 | 53 | 49 | 49 | 66 | 36 | 72 | 43 | 23 | 27 | 40 | 42 | 19 |

Table 6. Heatmap of mean and standard deviation values.

| Pore Area Fraction (%) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parameter | Mean |  |  | SD |  |  |
| Test ID | OH-100 | SH-80 | SH-60 | OH-100 | SH-80 | SH-60 |
| Cycle 1 | 33 | 28 | 35 | 2 | 10 | 6 |
| Cycle 2 | 29 | 22 | 27 | 4 | 11 | 6 |
| Cycle 3 | 23 | 21 | 17 | 3 | 3 | 5 |
| Pore Size Variation (μm) |  |  |  |  |  |  |
| Cycle 1 | 338 | 332 | 318 | 72 | 84 | 15 |
| Cycle 2 | 335 | 280 | 288 | 14 | 59 | 23 |
| Cycle 3 | 326 | 289 | 257 | 16 | 17 | 15 |