Supplementary Material

1. Methodology

1.1 X-ray diffraction (XRD).

X-ray diffraction (XRD) analyses of the potassium mineral samples were performed using a LabX XRD-6000 diffractometer (Shimadzu, Japan) operated with Cu Kα radiation (λ = 1.54056 Å), voltage of 30 kV, and current of 30 mA. The diffractograms were recorded for 2θ from 4° to 90°, using a scanning speed of 1° min-1.

1.2. Energy Dispersive X-Ray Analysis (EDX)

Semi-quantitative atomic compositions were evaluated by energy-dispersive X-ray (EDX) spectroscopy using a JEOL microscope (JSM-6510) operated at an acceleration voltage of 15 kV with a distance of 10 mm and a secondary electron detector.

2. Table and figure

Table S1. Chemical analysis (by X-ray fluorescence), surface area, and particle size for KRfeldspar and KRpolyhalite.

| Oxide species | KRfeldspar (wt.%) | KRpolyhalite (wt.%) |
| --- | --- | --- |
| K2O | 8.35 | 12.00 |
| Na2O | 7.44 | 1.74 |
| MgO | 0.35 | 6.79 |
| Al2O3 | 20.4 | <0.1 |
| SiO2 | 55.1 | 0.36 |
| P2O5 | 0.06 | 0.02 |
| CaO | 1.7 | 16.2 |
| TiO2 | 0.6 | <0.01 |
| MnO | 0.25 | <0.01 |
| Fe2O3 | 3.88 | 0.01 |
| SO3 | <0.01 | 47.5 |
| Others | 1.86 | 15.27 |
| Total | 100 | 100 |
| C | 0.62 | 0.86 |
| N | 0.62 | 0.66 |
| H | 0.19 | 1.43 |
| Particle size | 561.60 nm | 385.10 nm |
| Surface area | 2.75 m² g-1 | 0.38 m² g-1 |

Fig. S1. Energy dispersive X-ray analysis (EDX) of residual: A) KRpolyhalite natural, B) KRpolyhalite in water, C) KRpolyhalite in gluconic acid, D) KRpolyhalite in oxalic acid, E) KRpolyhalite in citric acid, F) KRfeldspar natural, G) KRfeldspar in water, H) KRfeldspar in gluconic acid, I) KRfeldspar in oxalic acid, J) KRfeldspar in citric acid, K) KRfeldspar in HCl (0.1 M) and KRfeldspar in HCl (1 M).