Online Resource 1 (electronic supplementary material). Electrospinning solution compositions and process parameters.
Detailed polymer solutions (solvent systems, final concentrations) and Nanospider process settings (electrode distance, voltages, cartridge movement speed, substrate rewinding speed, orifice size, controlled temperature and relative humidity) used to fabricate PCL and PVDF membranes.
Note: Please harmonize the reported PVDF final concentration throughout the manuscript (24 wt% vs 26 wt%) to a single value consistent with the experimental batch used for in vivo testing.

| Parameter | PCL | PVDF |
| --- | --- | --- |
| Molecular weight | 45.000 | 180.000 |
| Solvent system | Chloroform / ethanol / acetic acid (8/1/1) | Dimethylacetamide / acetone (8/2) |
| Final concentration [wt%] | 16 | 24 |
| Distance between electrodes [mm] | 170 | 170 |
| Voltage [kV] | -10 / +40 | -10 / +50 |
| Cartridge movement speed [mm/s] | 400 | 380 |
| Substrate rewinding speed [mm/min] | 45 | 12 |
| Orifice size [mm] | 0.6 | 0.7 |
| Temperature [°C] | 22 | 22 |
| Relative humidity [%] | 50 | 15 |