Supporting Information

Enaminone-Linked Quasi-One-Dimensional Covalent Organic Frameworks for CO2 Photoreduction with Water

Junxian Bai, Yuxin Hu, Fangyuan Si, Yan Li, Guijie Liang, Tingting Hou*, Yingwei Li*

Results and discussion

Figure S1. The 1H NMR spectrum of PDP.

Figure S2. The 13C NMR spectrum of PDP.

Figure S3. The 1H NMR spectrum of BDP.

Figure S4. The 13C NMR spectrum of BDP.

=

Figure S5. Synthesis of En-Q1DCOF.

Figure S6. Synthesis of Mix-Q1DCOF.

Figure S7. Synthesis of Im-Q1DCOF.

Figure S8. Experimental and Pawley refined PXRD of Mix-Q1DCOF crystal structure on the basis of the AA stacking models.

Figure S9. Mix-Q1DCOF top view and side view of the AA stacking structure based on PXRD and modeling.

Figure S10. Experimental and Pawley refined PXRD of Im-Q1DCOF crystal structure on the basis of the AA stacking models.

Figure S11. Im-Q1DCOF top view and side view of the AA stacking structure based on PXRD and modeling.

Figure S12. (a) Experimental and simulated powder X-ray diffraction patterns (AB stacking) and (b) ideal structure of En-Q1DCOF.

Figure S13. (a) Experimental and simulated powder X-ray diffraction patterns (AB stacking) and (b) ideal structure of Mix-Q1DCOF.

Figure S14. (a) Experimental and simulated powder X-ray diffraction patterns (AB stacking) and (b) ideal structure of Im-Q1DCOF.

Figure S15. Comparison of the FTIR spectra of Mix-Q1DCOF.

Figure S16. Comparison of the FTIR spectra of Im-Q1DCOF.

Figure S17. Comparison of the FTIR spectra of Q1DCOFs.

Figure S18. The 13C CP/MAS spectra of Mix-Q1DCOF.

Figure S19. The 13C CP/MAS spectra of Im-Q1DCOF.

Figure S20. High-resolution XPS spectra of (a) C 1s and (b) O 1s.

Figure S21. The pore-size distribution of Q1D-COFs.

Figure S22. SEM images of En-Q1DCOF.

Figure S23. TEM images of En-Q1DCOF.

Figure S24. SEM images of Mix-Q1DCOF.

Figure S25. TEM images of Mix-Q1DCOF.

Figure S26. Elemental mapping images of Mix-Q1DCOF.

Figure S27. SEM images of Im-Q1DCOF.

Figure S28. TEM images of Im-Q1DCOF.

Figure S29. Elemental mapping images of Im-Q1DCOF.

Figure S30. Mott-Schottky plots of (a) En-Q1DCOF, (b) Mix-Q1DCOF and (c) Im-Q1DCOF.

Figure S31. Valence band XPS spectra of (a) En-Q1DCOF, (b) Mix-Q1DCOF and (c) Im-Q1DCOF.

Figure S32. CO and O2 evolution rates of En-Q1DCOF, Mix-Q1DCOF and Im-Q1DCOF.

Figure S33. Dependence of the CO evolution rate for En-Q1DCOF with different masses.

Figure S34. Mass‐dependent AQY of photocatalytic CO evolution for En-Q1DCOF.

Figure S35. (a) PXRD patterns of En-Q1DCOF before and after photocatalytic reaction. (b) FTIR spectra of En-Q1DCOF before and after photocatalytic reaction.

Figure S36. Chemical stability of En-Q1DCOF. (a) PXRD patterns and (b) FTIR spectra of En-Q1DCOF after treatment in 1M NaOH, 1M HCl or 1M DMF for 7 days.

Figure S37. (a) En-COF and (b) Im-COF used for the calculation of the minimal fragment (Grey for C atoms, white for H atoms, red for O atoms and blue for N atoms).

Figure S38. Charge of CO2 adsorption sites in (a O-site) En-COF and (b N-site) Im-COF.

Figure S39. EIS Nyquist plots, with an inset showing the electrical equivalent circuit of the Nyquist plots.

Figure S40. Polarization curves.

Figure S41. Electron paramagnetic resonance spectra of DMPO‐•O2- of the samples in dark.

Figure S42. In situ ATR FTIR spectra of dry CO2 interactions with En-Q1DCOF under dark.

Figure S43. Gibbs free energy at different OH adsorption sites of Q1DCOFs.

Table S1. Fractional atomic coordinates for the unit cell of En-Q1DCOF with AA stacking.

| Space group PMA2 |  |  |  |
| --- | --- | --- | --- |
| Calculated cell parameters |  |  |  |
|  | a=29.4992Å | b= 27.3954Å | c= 6.0908Å |
|  | α= 90.0000° | β= 90.0000° | γ= 90.0000° |
|  | Rp= 2.96% | Rwp=3.83% |  |
| Atom | x | y | z |
| C1 | -0.97577 | 0.1005 | 0.25335 |
| O2 | -0.96888 | 0.07597 | 0.42419 |
| C3 | -0.96696 | 0.07988 | 0.04508 |
| C4 | -0.94802 | 0.0338 | 0.00095 |
| N5 | -0.93293 | 0.00294 | 0.15887 |
| C6 | -0.91403 | -0.04187 | 0.1328 |
| C7 | -0.88857 | -0.06064 | 0.30983 |
| C8 | -0.86675 | -0.10622 | 0.29411 |
| C9 | -0.87018 | -0.135 | 0.10166 |
| C10 | -0.89686 | -0.11643 | -0.07248 |
| C11 | -0.9183 | -0.07076 | -0.05824 |
| C12 | -0.84737 | -0.18034 | 0.08054 |
| C13 | -0.84483 | -0.21418 | 0.25598 |
| C14 | -0.82122 | -0.25857 | 0.2338 |
| C15 | -0.79954 | -0.27068 | 0.03456 |
| C16 | -0.80355 | -0.23815 | -0.14373 |
| C17 | -0.82606 | -0.19335 | -0.11948 |
| C18 | -1.3 | -0.64262 | -0.00566 |
| C19 | -1.32267 | -0.63127 | -0.20352 |
| C20 | -1.34743 | -0.58758 | -0.22483 |
| C21 | -1.34979 | -0.55379 | -0.04952 |
| C22 | -1.3282 | -0.56611 | 0.15042 |
| C23 | -1.30424 | -0.61012 | 0.17285 |
| C24 | -1.37294 | -0.50883 | -0.06954 |
| C25 | -1.41785 | -0.50627 | -0.15044 |
| C26 | -1.44151 | -0.4616 | -0.15447 |
| C27 | -1.42085 | -0.41826 | -0.07736 |
| C28 | -1.37528 | -0.42037 | -0.00798 |
| C29 | -1.35168 | -0.46489 | -0.00378 |
| N30 | -1.4414 | -0.37419 | -0.0565 |
| C31 | -1.48614 | -0.36323 | -0.06197 |
| C32 | -1.50284 | -0.31724 | 0.00181 |
| C33 | -1.47683 | -0.27588 | 0.06059 |
| O34 | -1.4356 | -0.27381 | 0.01058 |
| C35 | -1.49458 | -0.23622 | 0.18213 |
| C36 | -0.77421 | -0.31419 | 0.01422 |
| C37 | 1.47866 | 1.18793 | 0.1478 |
| C38 | 1.4929 | 1.14836 | 0.28115 |
| C39 | 1.52426 | 1.1582 | 0.45105 |
| C40 | 1.54102 | 1.2055 | 0.48619 |
| C41 | 1.52649 | 1.2441 | 0.35226 |
| H42 | -0.97544 | 0.10005 | -0.09029 |
| H43 | -0.94512 | 0.02418 | -0.16064 |
| H44 | -0.93501 | 0.01488 | 0.30759 |
| H45 | -0.8852 | -0.04084 | 0.45142 |
| H46 | -0.84775 | -0.1178 | 0.42437 |
| H47 | -0.90093 | -0.13616 | -0.21303 |
| H48 | -0.93723 | -0.05915 | -0.18848 |
| H49 | -0.86027 | -0.20693 | 0.40233 |
| H50 | -0.81985 | -0.28197 | 0.36428 |
| H51 | -0.78968 | -0.24657 | -0.29252 |
| H52 | -0.82628 | -0.17008 | -0.25051 |
| H53 | -1.32119 | -0.65472 | -0.33381 |
| H54 | -1.36338 | -0.58044 | -0.37038 |
| H55 | -1.32986 | -0.54313 | 0.28267 |
| H56 | -1.28985 | -0.61815 | 0.32094 |
| H57 | -1.43403 | -0.5371 | -0.20376 |
| H58 | -1.47396 | -0.46122 | -0.2124 |
| H59 | -1.35896 | -0.38945 | 0.04389 |
| H60 | -1.31876 | -0.4649 | 0.04959 |
| H61 | -1.4217 | -0.34718 | -0.02172 |
| H62 | -1.50934 | -0.38947 | -0.10181 |
| H63 | -1.53738 | -0.31438 | 0.01242 |
| H64 | 1.45551 | 1.18172 | 0.02569 |
| H65 | 1.53519 | 1.13075 | 0.55123 |
| H66 | 1.56354 | 1.21196 | 0.61043 |
| H67 | 1.53883 | 1.27827 | 0.38442 |

Table S2. Fractional atomic coordinates for the unit cell of Mix-Q1DCOF with AA stacking.

| Space group PMA2 |  |  |  |
| --- | --- | --- | --- |
| Calculated cell parameters |  |  |  |
|  | a=28.7365Å | b= 24.7115Å | c= 6.2289Å |
|  | α= 90.0000° | β= 90.0000° | γ= 90.0000° |
|  | Rp= 2.72% | Rwp=3.58% |  |
| Atom | x | y | z |
| C1 | -0.99388 | 0.17817 | 0.13628 |
| O2 | -0.97559 | 0.16765 | -0.0418 |
| C3 | -0.99081 | 0.14163 | 0.31004 |
| C4 | -0.96966 | 0.09034 | 0.31098 |
| N5 | -0.94937 | 0.0677 | 0.13634 |
| C6 | -0.92813 | 0.01873 | 0.11941 |
| C7 | -0.9047 | 0.00764 | -0.07481 |
| C8 | -0.88068 | -0.04143 | -0.10526 |
| C9 | -0.8796 | -0.08168 | 0.05678 |
| C10 | -0.90417 | -0.07071 | 0.24919 |
| C11 | -0.92771 | -0.0215 | 0.2808 |
| C12 | -0.85449 | -0.13071 | 0.02939 |
| C13 | -0.82953 | -0.15411 | 0.20213 |
| C14 | -0.80508 | -0.20293 | 0.17737 |
| C15 | -0.80178 | -0.22854 | -0.02439 |
| C16 | -0.82688 | -0.20587 | -0.19729 |
| C17 | -0.85325 | -0.15832 | -0.16996 |
| C18 | -1.30036 | -0.67498 | -0.05751 |
| C19 | -1.32109 | -0.65645 | -0.24928 |
| C20 | -1.34466 | -0.60647 | -0.2556 |
| C21 | -1.34762 | -0.57303 | -0.07141 |
| C22 | -1.32726 | -0.59243 | 0.12066 |
| C23 | -1.30486 | -0.64284 | 0.12834 |
| C24 | -1.37106 | -0.52257 | -0.07252 |
| C25 | -1.41466 | -0.51631 | -0.17551 |
| C26 | -1.44027 | -0.46807 | -0.15455 |
| C27 | -1.42331 | -0.42492 | -0.02827 |
| C28 | -1.37822 | -0.42899 | 0.05874 |
| C29 | -1.35247 | -0.47709 | 0.03681 |
| N30 | -1.44845 | -0.38017 | 0.02024 |
| C31 | 0.51675 | 1.22845 | 0.15625 |
| C32 | 0.56149 | 1.23228 | 0.24986 |
| C33 | 0.58421 | 1.28239 | 0.26688 |
| C34 | 0.56222 | 1.32963 | 0.19344 |
| C35 | 0.51715 | 1.32753 | 0.10256 |
| C36 | 0.49513 | 1.27651 | 0.08264 |
| C37 | 0.49523 | 1.37595 | 0.03984 |
| C38 | 0.2251 | 1.72386 | -0.04752 |
| H39 | -1.00517 | 0.15341 | 0.45318 |
| H40 | -0.97012 | 0.06993 | 0.45357 |
| H41 | -0.94976 | 0.08966 | 0.00821 |
| H42 | -0.90457 | 0.03565 | -0.19599 |
| H43 | -0.86343 | -0.04701 | -0.24721 |
| H44 | -0.90545 | -0.09863 | 0.36998 |
| H45 | -0.9446 | -0.01588 | 0.42314 |
| H46 | -0.8287 | -0.13581 | 0.34917 |
| H47 | -0.78957 | -0.21962 | 0.30893 |
| H48 | -0.8264 | -0.22388 | -0.34454 |
| H49 | -0.87178 | -0.14414 | -0.29809 |
| H50 | -1.31906 | -0.67914 | -0.38568 |
| H51 | -1.35949 | -0.59459 | -0.39688 |
| H52 | -1.32891 | -0.57019 | 0.2587 |
| H53 | -1.29141 | -0.65572 | 0.27104 |
| H54 | -1.42884 | -0.54723 | -0.26293 |
| H55 | -1.4716 | -0.46475 | -0.23049 |
| H56 | -1.36424 | -0.39742 | 0.14339 |
| H57 | -1.32008 | -0.47875 | 0.10482 |
| H58 | 0.57807 | 1.19857 | 0.30583 |
| H59 | 0.61663 | 1.2845 | 0.33377 |
| H60 | 0.57923 | 1.36574 | 0.21003 |
| H61 | 0.46267 | 1.27428 | 0.01518 |
| H62 | 0.51523 | 1.40981 | 0.0194 |

Table S3. Fractional atomic coordinates for the unit cell of Im-Q1DCOF with AA stacking.

| Space group PMA2 |  |  |  |
| --- | --- | --- | --- |
| Calculated cell parameters |  |  |  |
|  | a=31.2157Å | b= 21.5565Å | c= 6.0374Å |
|  | α= 90.0000° | β= 90.0000° | γ= 90.0000° |
|  | Rp= 6.32% | Rwp=8.28% |  |
| Atom | x | y | z |
| C1 | -0.92031 | 0.06888 | -0.02978 |
| C2 | -0.87795 | 0.06838 | 0.05023 |
| C3 | -0.85225 | 0.01518 | 0.02681 |
| C4 | -0.86819 | -0.03927 | -0.07623 |
| C5 | -0.90934 | -0.03618 | -0.17436 |
| C6 | -0.93488 | 0.01723 | -0.15251 |
| C7 | -0.84463 | -0.09549 | -0.07167 |
| C8 | -0.82329 | -0.11356 | 0.12491 |
| C9 | -0.80062 | -0.16962 | 0.13737 |
| C10 | -0.7971 | -0.20898 | -0.04826 |
| C11 | -0.81919 | -0.19233 | -0.24342 |
| C12 | -0.84262 | -0.13653 | -0.25479 |
| C13 | -1.29715 | -0.6809 | -0.01104 |
| C14 | -1.30221 | -0.63844 | -0.18691 |
| C15 | -1.32675 | -0.58422 | -0.15963 |
| C16 | -1.34762 | -0.57092 | 0.0433 |
| C17 | -1.34244 | -0.61405 | 0.21839 |
| C18 | -1.31774 | -0.66806 | 0.19188 |
| C19 | -1.37326 | -0.51703 | 0.06891 |
| C20 | -1.41256 | -0.51934 | 0.186 |
| C21 | -1.43864 | -0.46657 | 0.20857 |
| C22 | -1.42667 | -0.40947 | 0.11172 |
| C23 | -1.38728 | -0.40638 | -0.00204 |
| C24 | -1.36096 | -0.45912 | -0.02243 |
| N25 | -1.45062 | -0.35699 | 0.11902 |
| N26 | 0.44495 | 1.11854 | 0.02268 |
| C27 | 0.48812 | 1.12162 | 0.04146 |
| C28 | 0.50965 | 1.17597 | 0.10813 |
| C29 | 0.55316 | 1.17247 | 0.17279 |
| C30 | 0.57524 | 1.22546 | 0.24515 |
| C31 | 0.5541 | 1.28288 | 0.25448 |
| C32 | 0.51069 | 1.28849 | 0.18972 |
| C33 | 0.48899 | 1.23446 | 0.11668 |
| C34 | 0.49051 | 1.34694 | 0.19964 |
| C35 | 0.72714 | 1.26425 | -0.03532 |
| H36 | -0.86582 | 0.10623 | 0.13121 |
| H37 | -0.82182 | 0.01638 | 0.08984 |
| H38 | -0.92177 | -0.07338 | -0.25772 |
| H39 | -0.96437 | 0.0178 | -0.22475 |
| H40 | -0.8244 | -0.08633 | 0.26343 |
| H41 | -0.78676 | -0.18148 | 0.28433 |
| H42 | -0.81843 | -0.22088 | -0.37833 |
| H43 | -0.8582 | -0.12613 | -0.39887 |
| H44 | -1.28826 | -0.64681 | -0.33686 |
| H45 | -1.32957 | -0.55476 | -0.29155 |
| H46 | -1.35665 | -0.60666 | 0.36845 |
| H47 | -1.31497 | -0.69806 | 0.32213 |
| H48 | -1.42299 | -0.55983 | 0.2554 |
| H49 | -1.46639 | -0.47062 | 0.29626 |
| H50 | -1.37746 | -0.3655 | -0.07193 |
| H51 | -1.3325 | -0.45454 | -0.10487 |
| H52 | 0.50568 | 1.08227 | 0.01527 |
| H53 | 0.5692 | 1.1311 | 0.17014 |
| H54 | 0.60665 | 1.2222 | 0.29191 |
| H55 | 0.57089 | 1.32064 | 0.30921 |
| H56 | 0.45758 | 1.23769 | 0.06944 |
| H57 | 0.50691 | 1.38313 | 0.26835 |

Table S4. Comparison of CO production rate with that catalyzed by other metal-free COF photocatalysts and photocatalytic systems

| Sample | Reaction condition | CO Production rate (μmol g-1 h-1) | Selectivity (%) | Ref |
| --- | --- | --- | --- | --- |
| En-Q1DCOF | gas-solid system visible light ≥420 nm | 137.6 | ~100 | This work |
| Mix-Q1DCOF | gas-solid system visible light ≥420 nm | 33.5 | ~100 | This work |
| Im-Q1DCOF | gas-solid system visible light ≥420 nm | 6.5 | ~100 | This work |
| CT-COF | gas-solid system visible light ≥420 nm | 102.7 | ~100 | [1] |
| 2,3-DhaTph CONs | gas-solid system visible light ≥420 nm | 132.2 | ~100 | [2] |
| TAPBB-COF | gas-solid system visible light 200-1000 nm | 24.6 | 95.6 | [3] |
| TT-TAPP | H2O, TEOA/800>λ>200 nm | 18 | 90 | [4] |
| TOT-TAPP | H2O, TEOA/800>λ>200 nm | 34.8 | 90 | [4] |
| En-COF-TAPB-TDOEB | gas-solid system visible light ≥420 nm | 69 | ~100 | [5] |
| TFB-BDF-COF | gas-solid system visible light ≥420 nm | 49.5 | ~100 | [6] |
| TFPT-BDF-COF | gas-solid system visible light ≥420 nm | 158.1 | ~100 | [6] |
| 2N-COF | gas-solid system visible light ≥420 nm | 98 | ~100 | [7] |

References

[1]	K. Lei, D. Wang, L. Ye, M. Kou, Y. Deng, Z. Ma, L. Wang, Y. Kong, ChemSusChem 2020, 13, 1725.

[2]	Y. Guo, Q. Zhang, S. Gao, H. Wang, Z. Li, J. Qiu, Y. Zhao, Z. Liu, J. Wang, Green Chem. 2022, 24, 9530.

[3]	L. j. Wang, R. l. Wang, X. Zhang, J. l. Mu, Z. y. Zhou, Z. m. Su, ChemSusChem 2020, 13, 2973.

[4]	D. Zhou, Q. Chen, J. Zhang, T. Wang, Z. Q. Liu, Angew. Chem. Int. Ed. 2025, 137, e202500329.

[5]	J. Bai, M. Zhang, F. Si, Y. Li, G. Liang, T. Hou, Y. Li, Adv. Funct. Mater. 2025, 35, 2420218.

[6]	J. Sheng, Y. He, J. Li, C. Yuan, H. Huang, S. Wang, Y. Sun, Z. Wang, F. Dong, ACS Nano 2020, 14, 13103.

[7]	S. Gao, Q. Zhang, X. Su, X. Wu, X. Zhang, Y. Guo, Z. Li, J. Wei, H. Wang, S. Zhang, J. Am. Chem. Soc. 2023, 145, 9520.