Compressive Strength of Concrete after 28 days

| Mix Id | Compressive Strength (N/Mm2) |  |  |
| --- | --- | --- | --- |
|  | Ambient Curing | Normal Water Curing | Marine Water Curing |
| GPC-A | 36.6 | 33.5 | 39.8 |
| GPC-B | 35.1 | 13.6 | 14.2 |
| GPC-C | 35.9 | 14.8 | 15.6 |
| GPC-D | 31.4 | 11.5 | 13.5 |

Compressive Strength of Concrete after 56 days

| Mix Id | Compressive Strength (N/Mm2) |  |
| --- | --- | --- |
|  | Normal Water Curing | Marine Water Curing |
| GPC-A | 33.5 | 39.8 |
| GPC-B | 13.6 | 14.2 |
| GPC-C | 14.8 | 15.6 |
| GPC-D | 11.5 | 13.5 |

Split tensile test

| Mix Id | Split Tensile Strength (Mpa) |
| --- | --- |
| GPC-A | 4.7 |
| GPC-B | 3.6 |
| GPC-C | 4.2 |
| GPC-D | 2.9 |

weight loss % of GPC-A

| SAMPLE | Normal curing (%) | Marine curing (%) |
| --- | --- | --- |
| 1 | 3.75% | 1.66% |
| 2 | 5.17% | 2.89% |
| 3 | 4.06% | 2.10% |