| Table 1. Optimization of the conditions in the C-O cross-couplings of phenol with iodobenzene in the present of GO-CPTMS@Pd-TKHPPa |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Base | Catalystn (g) | Time (min) | Yield %b |
| 1 | K2CO3 | - | 160 | - |
| 2 | K2CO3 | 0.1 | 35 | 98 |
| 3 | NaOH | 0.1 | 60 | 98 |
| 4 | Cs2CO3 | 0.1 | 50 | 98 |
| 5 | Et3N | 0.1 | 80 | Trance |
| aReaction conditions: Iodobenzene (1mmol), Phenol (1 mmol), DMF (3 mL), GO-CPTMS@Pd-TKHPP (0.1 g, containing 0.104 mmol of Pd), 80° C, base (1 mmol). bIsolated yield. |  |  |  |  |

| Table 2. Optimization of the conditions in the C- O cross-couplings of phenol with iodobenzene by GO-CPTMS@Pd-TKHPPa |  |  |  |  |
| --- | --- | --- | --- | --- |
| Entry | Solvent | Temp °C | Time (min) | Yield %b |
| 1 | DMF | 80 | 35 | 98 |
| 2 | EtOH | 80 | 100 | 70 |
| 3 | H2O | 80 | 120 | 40 |
| 4 | DMSO | 80 | 60 | 93 |
| 5 | Toluene | 80 | 80 | 65 |
| aReaction conditions: Iodobenzene (1mmol), Phenol (1 mmol), DMF (3 mL), GO-CPTMS@Pd-TKHPP (0.1 g, containing 0.104 mmol of Pd), 80° C, K2CO3 (1 mmol). bIsolated yield. |  |  |  |  |

| Table 3. C-O cross-coupling reactions of aryl halides with phenol using GO-CPTMS@Pd-TKHPP |  |  |  |  |
| --- | --- | --- | --- | --- |
| Yield (%)b, C | Time(min) | X | R | Entry |
| 98 95 90 92 90 90 75 78 90 55 | 35 45 45 45 20 55 55 50 30 60 | I Br Cl I I I Br Br Br Cl | H H H 4-MeO 4-NO2 4-Me 4-Me 4-MeO 4-NO2 4-Me | 1 2 3 4 5 6 7 8 9 10 |
| aReaction conditions: aryl halids (1 mmol), phenol (1 mmol), K2CO3 (1 mmol), GO-CPTMS@Pd TKHPP (0.1 g, containing 0.104 mmol of Pd ), solvent (3 mL) under air atmosphere, at 80 °C. bIsolated yields. cThe product were characterized by comparison of their spectroscopic and physical data with those reported in literature. |  |  |  |  |

| Table 4. Recycling and reuse of GO-CPTMS@Pd- TKHPP in C-O cross-coupling reactionsa |  |
| --- | --- |
| Entry | Yield ( %) |
| 1 | 98 |
| 2 | 96 |
| 3 | 93 |
| 4 | 91 |
| 5 | 90 |
| aReaction conditions: Iodobenzene (1 mmol), phenol (1 mmol), K2CO3 (1 mmol), GO- CPTMS@Pd-TKHPP ( 0.1 g, containing 0.104 mmol of Pd ), solvent (3 mL), under air. |  |

| Table 5. Comparison of catalysts activity in some recently reported synthesis of diaryl ethers |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Reaction type | Solvent | Temperature | Reaction time (h) | Yield | Ref |
| 1 | GO-CPTMS@Pd-TKHPP nanocatalyst | O-arylation of phenols | DMF | 80°C | 0.33-1h | 90-98% | This work |
| 2 | Copper iodide catalyst in conjunction with the addition of Et3N base and sodium dodecyl sulfate (SDS) | C-O Cross-Coupling of Phenols with Aryl Iodides | DMF | 120°C | 7-12 h | 43-93% | 5 |
| 3 | Thermal Nickel-Catalyzed Carbon−Oxygen Cross-Coupling of (Hetero)aryl Halides with Alcohols Enabled by the Use of a Silane Reductant Approach | Carbon−Oxygen Cross-Coupling of (Hetero)aryl Halides | Toluene | 120°C | 24 h | 89% | 22 |
| 4 | Diaryl ethers synthesis: nano-catalysts in carbonoxygen cross-coupling reactions | Crosscoupling reaction of phenols with less reactive aryl chlorides | DMF | 110°C | 2-7 h | 91-98% | 23 |
| 5 | # Photoelectrochemistry-Promoted Ni-Catalyzed C–O Cross-Couplings | Nickel-catalyzed electrochemical cross-coupling reactions | DMSO | 20°C | - | up to 83% | 24 |