Supporting Information

Hierarchical Triple-Channel Architectures Unlock Scalable and High-Efficient Uranium Extraction from Seawater

Hui Wang#; Congwen Cao#; Jianming Chen#; Guanbing Zhou; Tao Liu; Yihui Yuan*; Ning Wang*

1 State Key Laboratory of Marine Resource Utilization in South China Sea

Hainan University, Haikou 570228, China

* Corresponding authors. E-mail addresses: wangn02@foxmail.com (Ning Wang)

yuanyh@hainanu.edu.cn (Yihui Yuan)

# These authors contributed equally to this work.

Table of Contents

Supporting Information	1

1 Supplementary Figures	3

2 Supplementary Tables	13

3 Supplementary References	19

1 Supplementary Figures

Supplementary Figure 1│Schematic representation of enhanced uranium adsorption in seawater by a honeycomb-inspired bulk adsorbent with hierarchical porous channels.

Supplementary Figure 2│Silica gel templates with regularly arranged honeycomb columns and size-matched brass frames.

Supplementary Figure 3│Synthesis of IM-PAO, LP-PAO and HTC-PAO.

Supplementary Figure 4│The physical form of HTC-PAO.

Supplementary Figure 5│SEM images of IM-PAO and LP-PAO.

Supplementary Figure 6│Digital photograph of HTC-PAO block with the size of 60 mm (L) × 55 mm (W) × 10 mm (H).

Supplementary Figure 7│FTIR spectra of PAN, PAO, IM-PAO, LP-PAO, and HTC-PAO are presented.

Supplementary Figure 8│High-resolution XPS spectra for IM-PAO, LP-PAO and HTC-PAO in N 1s area.

Supplementary Figure 9│High-resolution XPS spectra for IM-PAO, LP-PAO and HTC-PAO in C1s area.

Supplementary Figure 10│Mercury intrusion-extrusion curves of IM-PAO, LP-PAO and HTC-PAO.

Supplementary Figure 11│Nitrogen adsorption–desorption isotherms of IM-PAO, LP-PAO and HTC-PAO.

Supplementary Figure 12│Water contact angle measurements for IM-PAO, LP-PAO, and HTC-PAO.

Supplementary Figure 13│Mechanical properties of thin films.

Supplementary Figure 14│Uranium adsorption performance of IM-PAO and LP-PAO in simulated seawater with different concentrations. (V, 5000 mL; Mads, 5 mg).

Supplementary Figure 15│XPS spectra of IM-PAO and LP-PAO before and after uranium adsorption.

Supplementary Figure 16│EDS mapping of HTC-PAO following uranium adsorption.

Supplementary Figure 17│High-resolution U4f XPS spectra of the IM-PAO and LP-PAO.

Supplementary Figure 18│Digital photographs of the HTC-PAO before and after uranium adsorption.

Supplementary Figure 19│Uranium adsorption kinetic data and corresponding fitting curves based on Pseudo first order and Pseudo second order models for IM-PAO, LP-PAO and HTC-PAO. (C0, 4 ppm,16ppm; V, 5000 mL; Mads, 5 mg).

Supplementary Figure 20│Equilibrium adsorption isotherm and the corresponding fitting curves based on Freundlich model and Langmuir model for IM-PAO and LP-PAO.

Supplementary Figure 21│Model establishment and mesh division of IM-PAO, LP-PAO and HTC-PAO.

Supplementary Figure 22│Performance of Cycle Adsorption in HTC-PAO.

Supplementary Figure 23│An advanced marine water recirculation system was engineered for efficient uranium recovery applications.

2 Supplementary Tables

Supplementary Table 1 | Uranium adsorption capacities of IM-PAO, LP-PAO and HTC-PAO at different times.

|  | IM-PAO |  |  | LP-PAO |  |  | HTC-PAO |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 4ppm | 8ppm | 16ppm | 4ppm | 8ppm | 16ppm | 4ppm | 8ppm | 16ppm |
| 0 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 |
| 2 | 48.90 | 98.25 | 187.59 | 73.35 | 171.15 | 244.50 | 195.6 | 171.15 | 268.95 |
| 4 | 73.35 | 162.79 | 286.79 | 85.57 | 268.95 | 391.20 | 244.50 | 317.85 | 513.45 |
| 6 | 97.80 | 213.87 | 352.92 | 110.02 | 317.85 | 489.00 | 268.95 | 391.20 | 709.05 |
| 8 | 122.25 | 258.18 | 415.99 | 134.47 | 391.20 | 586.80 | 293.40 | 435.65 | 782.40 |
| 10 | 136.92 | 289.25 | 458.12 | 171.15 | 415.65 | 635.70 | 305.62 | 489.00 | 846.85 |
| 12 | 146.70 | 317.19 | 494.25 | 195.60 | 464.55 | 684.60 | 317.85 | 537.90 | 890.20 |
| 16 | 158.92 | 342.38 | 521.32 | 207.82 | 489.00 | 731.05 | 334.96 | 586.80 | 934.65 |
| 20 | 171.15 | 361.56 | 539.38 | 220.05 | 513.45 | 745.72 | 342.30 | 635.70 | 929.10 |
| 24 | 183.37 | 377.53 | 552.45 | 244.50 | 537.90 | 770.17 | 347.19 | 660.15 | 998.00 |
| 28 | 195.60 | 389.72 | 565.58 | 256.72 | 557.46 | 792.18 | 359.41 | 684.60 | 1002.44 |
| 32 | 207.82 | 400.69 | 576.73 | 268.95 | 574.57 | 806.85 | 366.75 | 733.50 | 1051.34 |
| 36 | 220.05 | 413.12 | 582.65 | 268.95 | 586.80 | 836.19 | 374.08 | 757.95 | 1063.57 |
| 40 | 220.05 | 422.66 | 588.26 | 281.17 | 603.91 | 843.52 | 378.97 | 782.40 | 1075.79 |
| 44 | 232.27 | 430.09 | 593.79 | 293.40 | 616.14 | 855.75 | 383.86 | 757.95 | 1100.24 |
| 48 | 232.27 | 435.73 | 598.71 | 293.40 | 616.14 | 855.75 | 391.20 | 782.40 | 1100.24 |

Supplementary Table 2 | Fitting parameters of adsorption kinetics data based on pseudo-second-order and pseudo-first-order models.

|  | C0 (ppm) | Pseudo-second-order |  | Pseudo-first-order |  |
| --- | --- | --- | --- | --- | --- |
|  |  | R2 | qe (mg g-1) | R2 | qe (mg g-1) |
| IM-PAO | 4 | 0.9942 | 228.63 | 0.9823 | 221.92 |
|  | 8 | 0.9998 | 433.97 | 0.9929 | 417.16 |
|  | 16 | 0.9970 | 604.46 | 0.9940 | 579.67 |
| LP-PAO | 4 | 0.9910 | 293.44 | 0.9862 | 284.77 |
|  | 8 | 0.9978 | 612.07 | 0.9850 | 588.20 |
|  | 16 | 0.9973 | 860.04 | 0.9918 | 824.08 |
| HTC-PAO | 4 | 0.9903 | 375.25 | 0.9471 | 360.01 |
|  | 8 | 0.9962 | 779.28 | 0.9838 | 752.21 |
|  | 16 | 0.9891 | 1099.80 | 0.9855 | 1050.55 |

Supplementary Table 3 | Fitting parameters of equilibrium adsorption isotherms of IM-PAO, LP-PAO and HTC-PAO based on Langmuir and Freundlich models.

|  | Langmuir model |  | Freundlich model |  |
| --- | --- | --- | --- | --- |
|  | R2 | qm (mg g-1) | R2 | qm (mg g-1) |
| IM-PAO | 0.92532 | 712.16 | 0.68055 | 775.37 |
| LP-PAO | 0.93544 | 1024.38 | 0.71298 | 1119.61 |
| HTC-PAO | 0.95798 | 1343.6 | 0.77258 | 1475.75 |

Supplementary Table 4 | IM–PAO adsorption model parameters.

| Parameters | Value | Unit |
| --- | --- | --- |
| εp | 0.856 | - |
| dp | 1.176E-6 | m |
| Deff | 1.739E-9 | m2∙s-1 |
| k3 | 0.147 | L∙mg-1 |

Supplementary Table 5 | LP–PAO adsorption model parameters.

| Parameters | Value | Unit |
| --- | --- | --- |
| εp | 0.863 | - |
| dp | 1.176E-6 | m |
| Deff | 1.739E-9 | m2∙s-1 |
| k3 | 0.147 | L∙mg-1 |

Supplementary Table 6 | HTC–PAO adsorption model parameters.

| Parameters | Value | Unit |
| --- | --- | --- |
| εp | 0.878 | - |
| dp | 1.176E-6 | m |
| Deff | X = 6.956E-9 | m2∙s-1 |
|  | Y = 6.956E-9 | m2∙s-1 |
|  | Z = 1.739E-9 | m2∙s-1 |
| k3 | 0.147 | L∙mg-1 |

Supplementary Table 7 | Fluid parameters and solid phase density.

| Parameters | Value | Unit |
| --- | --- | --- |
| ρf | 1025 | kg∙m-3 |
| u | 0.796 | m∙s-1 |
| μ | 0.001 | Pa∙s |
| ci | 8 | mg∙L-1 |
| ρs | 1141.100 | kg∙m-3 |

Supplementary Table 8 | The maximum errors and the average errors of the three adsorbents.

| Adsorbents | Maximum error | average error |
| --- | --- | --- |
| IM-PAO | 14.84% | 2.77% |
| LP-PAO | 16.97% | 4.81% |
| HTC-PAO | 10.92% | 6.13% |

Supplementary Table 9 | Uranium adsorption capacity of HTC-PAO adsorbent at different cycle numbers in simulated seawater.

| Recycles | Adsorption capacity (mg g−1) | Elution Capacity (mg g−1) | Elution efficiency (%) |
| --- | --- | --- | --- |
| 1 | 772.20 | 758.33 | 98.20 |
| 2 | 738.26 | 710.96 | 96.30 |
| 3 | 701.79 | 668.70 | 95.29 |
| 4 | 689.00 | 642.45 | 93.24 |
| 5 | 671.55 | 613.08 | 91.30 |

Supplementary Table 10 | Concentration of uranium and competitive metal ions in natural seawater and metal-ion-spiked seawater.

| Metal | Natural seawater (ppb) | Metal ion-spiked seawater (ppb) |
| --- | --- | --- |
| U | 3.3 | 330 |
| V | 1.5 | 150 |
| Mn | 0.2 | 20 |
| Co | 0.05 | 5 |
| Ni | 1.0 | 100 |
| Cu | 0.6 | 60 |
| Pb | 0.03 | 3 |
| Cr | 0.3 | 30 |
| Zn | 4.0 | 400 |

Supplementary Table 11 | Comparison of the uranium adsorption performance in nature seawater between the HTC-PAO and many other recoverable AO-based uranium adsorbents.

|  | Absorbents | Year | qe (mg g−1) | Time (day) |
| --- | --- | --- | --- | --- |
| a | HTC-PAO |  | 14.69 | 35 |
| b | PGP hydrogel1 | 2024 | 9.73 | 11 |
| c | PAO PEI sponge2 | 2024 | 9.79 | 15 |
| d | Y-PAO hydrogel3 | 2024 | 10.07 | 28 |
| e | PAO/PMPC-SH4 | 2024 | 6.26 | 28 |
| f | SF-g-PAO5 | 2024 | 4.95 | 28 |
| g | Cs-PIDO-16 | 2023 | 5.75 | 28 |
| h | PE-PAO@ADH7 | 2024 | 6.76 | 30 |
| i | PAO-CNF hydrogel8 | 2024 | 6.6 | 35 |
| j | h-PAO9 | 2023 | 9.86 | 49 |
| k | PAO-PNF10 | 2023 | 5 | 12 |
| l | PP@MeP-H11 | 2023 | 3.12 | 21 |
| m | PAO-BS12 | 2023 | 2.7 | 10 |
| n | ML-r-PAO@HB13 | 2023 | 9.74 | 28 |
| o | MP-PAO14 | 2022 | 5.8 | 28 |
| p | PAO@CHM15 | 2022 | 7.46 | 28 |
| q | HA-PAO NFMs16 | 2022 | 6.73 | 28 |
| r | PAO-BSPE17 | 2022 | 12.67 | 64 |
| s | PAO-PHMB-A18 | 2021 | 3.19 | 30 |
| t | PAO-CB19 | 2021 | 8.56 | 56 |
| u | PA-PAO/CS NFs20 | 2021 | 4.91 | 10 |
| v | NC-PAO DN hydrogel21 | 2021 | 8.62 | 25 |
| w | AOP@PPLA22 | 2020 | 10.31 | 35 |
| x | Zn2+-PAO23 | 2020 | 9.23 | 28 |
| y | PAO/Alg NFs24 | 2020 | 8.42 | 56 |
| z | Anti-PAO gels25 | 2020 | 9.29 | 30 |

3 Supplementary References

1.	Liu T, et al. Engineering shrinkage resistance of nano-structured hydrogels in seawater for fast uranium capture. Chem. Eng. J. 496, 153832 (2024).

2.	Ou M, Li W, Huang Z, Xu X. Highly efficient extraction of uranium(VI) from seawater by polyamidoxime/polyethyleneimine sponge. Sep. Purif. Technol. 331, 125721 (2024).

3.	Wang H, Yao W, Yuan Y, Shi S, Liu T, Wang N. Yeast‐Raised Polyamidoxime Hydrogel Prepared by Ice Crystal Dispersion for Efficient Uranium Extraction from Seawater. Adv. Sci. 11, 2306534 (2024).

4.	Cao M, et al. Poly(amidoxime)/polyzwitterionic semi-interpenetrating network hydrogel with robust salt-shrinkage resistance for enhanced uranium extraction from seawater. Chem. Eng. J. 481, 148536 (2024).

5.	Huang C, et al. Constructing amidoxime adsorption sites on the core-shell structured natural silk protein for uranium capture. Int. J. Biol. Macromol. 267, 131608 (2024).

6.	Zhang Y, Cai T, Zhao Z, Han B. Chitosan-poly(imide dioxime) semi-interpenetrating network hydrogel for efficient uranium recovery from seawater. J. Radioanal. Nucl. Chem. 333, 31-41 (2023).

7.	Yao Y, et al. Hydrazide and amidoxime dual functional membranes for uranium extraction from seawater. J. Mater. Chem. A. 12, 10528-10538 (2024).

8.	Huang Y, Zou S, Li Z, Na B, Lin S, Zhang S. Tough polyamidoxime-nanocellulose supramolecular composite hydrogels for effective uranium extraction from seawater. Polymer. 298, 126895 (2024).

9.	Luo G, et al. Salt-shrinkage resistant poly(amidoxime) adsorbent for improved extraction of uranium from seawater. Chem. Eng. J. 464, 142569 (2023).

10.	Ye Q-H, Ye H, Hu Z-T, Wu M-B, Yao J. Polyamidoxime nanofiber membranes with hierarchical pores for enhanced uranium extraction from seawater. Compos. Commun. 43, 101725 (2023).

11.	Zhang J, et al. Methyl 4-hydroxybenzoate nanospheres anchored on poly(amidoxime)/polyvinyl alcohol hydrogel network with excellent antibacterial activity for efficient uranium extraction from seawater. Desalination. 548, 116243 (2023).

12.	Wang Y, et al. Polyamidoxime-loaded biochar sphere with high water permeability for fast and effective recovery of uranium from seawater. J. Water Process Eng. 55, 104205 (2023).

13.	Jiao G-J, Ma J, Zhang J, Zhai S, Sun R. Efficient extraction of uranium from seawater by reticular polyamidoxime-functionalized oriented holocellulose bundles. Carbohyd. Polym. 300, 120244 (2023).

14.	Wang H, et al. Macroporous hydrogel membrane by cooperative reaming for highly efficient uranium extraction from seawater. Sep. Purif. Technol. 289, 120823 (2022).

15.	Jiao G-J, Ma J, Zhang J, Li Y, Liu K, Sun R. Porous and biofouling-resistant amidoxime-based hybrid hydrogel with excellent interfacial compatibility for high-performance recovery of uranium from seawater. Sep. Purif. Technol. 287, 120571 (2022).

16.	Xu X, et al. Engineering biaxial stretching polyethylene membrane with poly(amidoxime)-nanoparticle and mesopores architecture for uranium extraction from seawater. Chem. Eng. J. 430, 133159 (2022).

17.	Shi S, et al. High-strength and anti-biofouling nanofiber membranes for enhanced uranium recovery from seawater and wastewater. J. Hazard. Mater. 436, 128983 (2022).

18.	He N, et al. Polyguanidine-modified adsorbent to enhance marine applicability for uranium recovery from seawater. J. Hazard. Mater. 416, 126192 (2021).

19.	Wang D, et al. Blow spinning of pre–acid-activated polyamidoxime nanofibers for efficient uranium adsorption from seawater. Mater. Today. Energy. 21, 100735 (2021).

20.	Liu R, et al. A nanoclay enhanced Amidoxime-Functionalized Double-Network hydrogel for fast and massive uranium recovery from seawater. Chem. Eng. J. 422, 130060 (2021).

21.	Lim YJ, Goh K, Goto A, Zhao Y, Wang R. Uranium and lithium extraction from seawater: challenges and opportunities for a sustainable energy future. J. Mater. Chem. A. 11, 22551-22589 (2023).

22.	Yan B, Ma C, Gao J, Yuan Y, Wang N. An Ion‐Crosslinked Supramolecular Hydrogel for Ultrahigh and Fast Uranium Recovery from Seawater. Adv. Mater. 32, 1906615 (2020).

23.	Xu X, et al. Aqueous Solution Blow Spinning of Seawater‐Stable Polyamidoxime Nanofibers from Water‐Soluble Precursor for Uranium Extraction from Seawater. Small. Methods. 4, 2000558 (2020).

24.	Shi S, Li B, Qian Y, Mei P, Wang N. A simple and universal strategy to construct robust and anti-biofouling amidoxime aerogels for enhanced uranium extraction from seawater. Chem. Eng. J. 397, 125337 (2020).

25.	Yuan Y, et al. Charge balanced anti-adhesive polyacrylamidoxime hydrogel membrane for enhancing uranium extraction from seawater. Chem. Eng. J. 421, 127878 (2021).