Supplementary Information

Biocompatible self-healing hydrogels based on boronic acid-functionalized polymer and laponite nanocomposite applied for water pollutant removal

Xue-Ting Wang a,#, Xudong Deng a,#,*, Tuo-Di Zhang a, Xi Zhang a, Wen-Pu Shi a, Jialiang Lai b, Hongwei Zhou b, Ya-Jing Ye a, Chen-Yan Zhang a, Da-Chuan Yin a,*

a Key Laboratory for Space Bioscience and Biotechnology, School of Life Sciences, Northwestern Polytechnical University, Xi’an 710072, China

b School of Materials and Chemical Engineering, Xi'an Technological University, Xi'an, P. R. China

*Corresponding authors

E-mail addresses: dengxd@nwpu.edu.cn (X. Deng); yindc@nwpu.edu.cn (D-C, Yin).

# These authors contributed equally to this work and should be considered as co-first authors.

# Contents:

Part 1. Materials and Methods

Part 2. Supporting Schemes and Figures.

Scheme S1. Ionization equilibrium of amidated 2-amino phenylboronic acid (2APBA) in aqueous solution.

Scheme S2. The formation of hydrogen bonds between PAA polymer chains at low pH condition.

Scheme S3. Schematic illustration showing how NCgel1 adsorbs heavy metal ions.

Figure S1. 1H-NMR and FTIR of PAA-2APBA.

Figure S2. Visual comparison of the hydrogel with laponite and the hydrogel without laponite.

Figure S3. Shear storage modulus (G’) and loss modulus (G”) of hydrogels over a frequency sweep of 0.5-2.2 Hz.

Figure S4. Hydrogel's degradation tests and thermal stability test.

Figure S5. The stability of NCgel1 and gel1 immersed in PBS for 720h (30 days) at room temperature.

Figure S6. Adsorption tests of organic dyes on hydrogel.

Figure S7. NCgel1 immersed in the solution of CuSO4 (1mg/mL).

Figure S8. Photograph of monolayer-cultured 293T cells (without hydrogel).

Figure S9. Live/dead assay of 293T cells seeded in PAA-2APBA/PVA hydrogels (gel1) and PAA-2APBA/PVA + laponite hydrogels (NCgel1).

Figure S10. Live/dead assay of HT22 cells seeded in PAA-2APBA/PVA hydrogels (gel1) and PAA-2APBA/PVA + laponite hydrogels (NCgel1).

Part 1. Materials and Methods

Materials

Polyacrylic acid (PAA, Mw=1×105 g/mol, 35wt% water solution), N-Ethyl-N’-(3-(dimethylamino)propyl) carbodiimide hydrochloride (EDC, 98%), paraformaldehyde, 2-amino phenylboronic acid hydrochloride (2APBA, 95%), poly(vinyl alcohol) (PVA; Mw = 85000−124000, 99+% hydrolyzed), were all purchased from Sigma-Aldrich (St. Louis, MO, U.S.A.), and were used without further purification. Dulbecco’s modified Eagle’s medium (DMEM) basal medium (high glucose) and fetal bovine serum were obtained from Solarbio (Shanghai, China). The deionized water used in all experiments was purified by a Milli-Q purification system, with a resistivity of >18.2 MΩ cm. Methylene blue and malachite green (MB, MG) were all purchased from Solarbio. Copper sulfate and cadmium chloride (CuSO4 and CdCl2) were obtained from Sinopharm Group Chemical Reagent Co., Ltd. Laponite-XLS XR was a gift from BYK Additives (Shanghai) Co., Ltd. Live/Dead Cell Double Stain Kit (Calcein-AM/PI Double Stain Kit) was obtained from Shanghai Yeasen Biotechnology Co., Ltd. HCl (0.1 M) and NaOH (0.1 M) were used for pH adjustment during the experiment.

Synthesis and characterization of PAA-2APBA

2-aminophenylboronic acid modified polyacrylic acid (PAA-2APBA) was synthesized through EDC chemistry (Scheme 1a). Briefly, PAA (1g, 35wt% aqueous solution) was dissolved in 150 mL of deionized water. EDC (1g) was dissolved in 10 mL of deionized water, and then added dropwise into the PAA solution. The pH was then adjusted to 6.0 by the addition of 0.1 M NaOH, and kept with stir for 10 min. Afterwards, 170 mg of 2APBA dissolved in 5 mL of deionized water was slowly dropped into the mixed solution of PAA and EDC under magnetic stirring, while the pH of the reaction mixture was always maintained at 6.0 via addition of 0.1 M NaOH or HCl over the 4 h reaction time at room temperature. The reaction was finally stopped by adjusting the pH to 7.0 using 0.1 M NaOH, after which the 2APBA modified PAA was purified by dialysis against a large excess of water using a prewashed dialysis membrane (MWCO = 14 kDa). The dialysis was stopped when the conductivity of the dialysate was less than 5 μS·cm−1, after which the PAA-2APBA product was recovered by freeze-drying and the obtained product was stored at -20°C. In order to investigate the effect of different feeding ratios of carboxyl groups in PAA and amino groups in 2APBA on hydrogels, three groups of PAA-2APBA was prepared with different molar ratios, namely carboxyl groups: amino groups = 5:1, 2.5:1, and 1:1. For convenience, the PAA-2APBA with different grafting rates was named as precursor5, precursor2.5 and precursor1, and the subsequent hydrogels prepared by different PAA-2APBA were named as gel5 or NCgel5, gel2.5 or NCgel2.5 and gel1 or NCgel1 accordingly.

Grafting density of PAA-2APBA was characterized by 1H-NMR using a Bruker AVANCE 400 MHz spectrometer using D2O (99.8% D, Cambridge Isotope Laboratories) as the solvent. Integration of the NMR signals arising from the -CH2- of PAA (δ=1.1-1.6 ppm), the -CH- of PAA (δ=1.79 ppm and δ=2.52 ppm) and the aromatic protons of the PBA group (δ=7.0−7.7 ppm), which indicated a degree of substitution of PBA groups per vinyl repeat unit. Furthermore, Fourier-transform infrared (FTIR) spectroscopy using a KBr pellet technique (Bruker Tensor 27 FTIR spectrometer) was performed to characterize the PAA-2APBA.

Preparation of PAA-2APBA/PVA + laponite nano-composite hydrogels

For preparing PAA-2APBA/PVA + laponite hydrogels, the precursor solutions of PVA (30 mg/mL) and PAA-2APBA + laponite (containing 80% v/v of a 30 mg/mL PAA-2APBA stock solution well mixed with 20% v/v of a 30 mg/mL laponite stock solution) were first prepared in deionized water. The two precursor solutions were then loaded separately into two barrels of a double-barrel syringe and coextruded through a static mixer into a mold of dimensions specified for each subsequent test (Scheme 1b). In the precursor solution PAA-2APBA + laponite, the proportion of laponite was also increased to 30% v/v and 40% v/v, respectively, to determine the effect of laponite content on the nano-composite hydrogel.

For convenience, the PAA-2APBA/PVA + laponite hydrogels prepared using the precursor PAA-2APBA with the feeding ratio between carboxyl and amino groups of 5:1 was named ‘NCgel5’. Similarly, NCgel2.5 and NCgel1 were named after the PAA-2APBA precursor.

Characterization of nano-composite hydrogel

pH adaptability of hydrogels

In order to prove that the gelation at a relatively wide pH range, a layer of PVA precursor solution (30 mg/mL) was first spread on the bottom of the glass bottle with a syringe, and then 0.1M HCL or 0.1M NaOH was used to adjust the pH of the PVA precursor solution while using pH test paper to determine the approximate pH of the PVA precursor solution. Next, the pre-configured precursor solution PAA-2APBA+laponite (containing 80% v/v of a 30mg/mL PAA-2APBA stock solution well mixed with 20% v/v of a 30mg/mL laponite stock solution) was injected into the pH-adjusted PVA precursor solution using a syringe, and the mixture was allowed to stand at room temperature for 1 minutes after being homogenized. The glass bottle was inverted to observe whether it formed a hydrogel.

Self-healing and injectable performance

To proceed the qualitative self-healing test, the PAA-2APBA/PVA hydrogel was assessed alone first (i.e., without laponite). The hydrogel disk was cut in half and the two halves were moved back into contact without applying additional pressure. For the nano-composite hydrogel, laponite dispersion (30 mg / mL) was added to the precursor solution of PAA-2APBA in a volume ratio of 4: 1, and then mixed with PVA solution (30 mg / mL) at room temperature to quickly cross-link to form nano-composite hydrogel for a similar qualitative self-healing test. In addition, to test the injectability, the PVA and PAA-2APBA + laponite was first added into a 2.5 mL syringe and allowed to stand for 5 minutes at room temperature to fully crosslink. Two different dyes were used to stain the crosslinked hydrogel in the syringe (blue: methylene blue solution; red: sulforhodamine B solution). Then the syringe was pushed to determine if the hydrogel can be squeezed out through a 0.5 mm diameter needle.

Rheological properties

The rheological properties of hydrogels were tested using a TA rheometer (DHR 2) at 25 °C. Hydrogels were prepared 1h in advance. After complete gelation, the hydrogel was compressed to a sheet with a thickness of 1 mm and a diameter of 20 mm by the rheometer. Next, the gels were subjected to a dynamic frequency sweep (0.5 to 2.2 Hz) to determine their shear storage modulus (G’) and shear loss modulus (G”). The healing tests were conducted by adjusting the oscillation displacement from being relatively small (0.02 rad, 1.468Hz) to large (0.5 rad, 1.468Hz), in which the large oscillation displacement would break the internal integrity of the gel. Then hydrogels were allowed to heal for 180 s, and the oscillation displacement returned to the small value (0.02 rad, 1.468Hz). During the whole process, the G’ and G” were recorded as a function of time.

Degradation experiment

The synthesized hydrogels were immersed into PBS at pH = 7.4 at room temperature, and were then taken out every 1 h to measure the weight change. Every time the hydrogel is taken out and weighed, the pendent water on the surface must be removed by absorbent paper. Formula 1 was used to determine the mass loss rate of the hydrogel (where W0 represents the initial mass of the hydrogel, Wt represents the mass after the hydrogel is degraded, and the unit is gram). After several times, hydrogel was left In PBS to observe the longest degradation time.

Degradation ratio（%）=W0-WtW0×100%   (1)

Scanning electron microscopy

Scanning electron microscopy (SEM, Verios G4, FEI) was used to observe the surface morphology of the hydrogel to further study the effect of nanoparticle introduction on the apparent morphology of the hydrogel. Precursor solution of PVA (30 mg/mL) and PAA-2APBA+laponite (containing 80% v/v of a 30 mg/mL HA-2APBA stock solution well mixed with 20% v/v of a 30 mg/mL laponite stock solution) were prepared in deionized water. At room temperature, the mixture was thoroughly mixed at a volume ratio of 1:1 to form a hydrogel. Then the gel was frozen at -80 °C for 4 hours, and lyophilized thereafter in a freeze dryer for 48 hours. The obtained hydrogel lyophilized sample was vacuum sprayed with gold for 100 s, and observed and photographed with a SEM at a voltage of 10kV.

Thermal stability analysis

Freeze-dried hydrogel samples (3-6 g) were placed in a Synchronous Thermal Analyzer (STA 449F3, NETZSCH). The protective gas was set to argon (Ar), the purge gas and protective gas flow are 60 mL/min, and the temperature range is 35-800 °C. The heating rate was set as 10 K/min. The obtained experimental data is plotted with temperature (°C) as the abscissa and mass loss percentage (%) as the ordinate to determine the thermal stability of the hydrogel material.

Adsorption experiments of organic dyes

The water solution of methylene blue (0.5% w/v) and malachite green (0.5% w/v,) were set as the model waste water containing organic pollutants with positive charges. NCgel1 was placed in the prepared methylene blue solution, and then 0.2 mL of supernatant of the solution was taken every hour for the first 5 h and 24 h. The absorbance was measured at a wavelength of 665 nm for methylene blue and 625 nm for malachite green with a microplate reader. At 28 h, the adsorbed organic dye was centrifuged, and the supernatant was taken to measure the absorbance value.

Adsorption of metal ions

The in situ synthesized nano-composite hydrogels were used directly added into the solutions to adsorb copper ions and cadmium ions, without undergoing the freeze-drying step. During the adsorption process, the mixture is shaken and sampled at different time points (0, 10, 20, 30, 40, 50, 60 min). After the adsorption is completed, the supernatant is left to stand and the metal ion concentration in the solution is detected by atomic absorption spectrophotometry. The equations (2) was used to study the adsorption of the hydrogel. Qe (mg/g) were calculated by formula (2) to indicated the adsorption. Ct and Vt were the sampled ion concentrations and the volume of the suspension respectively, and m was the mass of NCgel1. V0 = 50 mL, and C0=2 mg/L for both copper ions and cadmium ions.

Qe=C0V0-CtVtm                       (2)

Cytotoxity of hydrogel and nano-composite hydrogel

In order to confirm the biocompatibility of the hydrogel, we selected two cells of different origin: human kidney epithelial cells (293T) and mouse hippocampal neuron cells (HT22). Both cells were cultured in DMEM high glucose medium containing 10% (v/v) fetal bovine serum, 100 U/mL penicillin, and 100 μg/mL streptomycin in a cell culture bottle maintained at 37 °C in 5% CO2. After reaching 80% confluence, the cells were detached using 0.25% trypsin - 1 mM EDTA and resuspended in fresh culture medium. For preparing a thin layer of the PAA-2APBA/PVA gel at the bottom of each well of a 24-well plate, a 100 μL aliquot of a precursor solution containing 30 mg/mL PAA-2APBA was first added to each well followed by another 100 μL aliquot of a precursor solution containing 30 mg/mL PVA. Then, let it stand for a few minutes to allow it to crosslink completely until a thin layer of hydrogel is formed at the bottom of the 24-well plate. The cytotoxity of nano-composite hydrogels were evaluated using the similar process, except that the PAA-2APBA precursor solution is added with 20% v/v of 30 mg/mL laponite when preparing the hydrogel. A total of 1 mL of suspended cells was subsequently seeded on the thin layer gels at a density of 10000 cells/well (5000 cells/cm2). Then an extra 1 mL of medium was added in order to provide adequate nutrients for cell growth. Cells seeded on a bare polystyrene well were used as controls. After 24 and 48 h of culture, cell growth in the wells was monitored using light microscopy.

Calcein-AM/PI Double Stain Kit were used to stain the cells and an inverted fluorescence microscope was used to observe and intuitively judge the survival of cells. Briefly, the working solution of Calcein-AM (2 μM) and the working solution of PI (4.5 μM) was first prepared in dark first. The cells which have been cultured for 24h or 48h, were carefully washed in the 24-well plate twice with 1x Assay Buffer, and then the cells were stained with the working solutions at 37 °C in 5% CO2 for 30 minutes in the dark. The living cells showing yellow-green fluorescence were detected under an inverted fluorescence microscope using 490 nm excitation light. In addition, dead cells (red fluorescence) were observed under excitation light of 545 nm.

Part 2. Supporting schemes and figures.

Scheme S1. Ionization equilibrium of amidated 2-amino phenylboronic acid (2APBA) in aqueous solution. Intramolecular B−O bond formation leads to the formation of tetrahedral geometry at the boron center that promotes boronate ester formation at different pH values.

Since the modified PAA is grafted with 2APBA by amidation between a carboxyl group and an amino group, and the 2APBA can adapt to a wider pH environment through its conformational change (intramolecular ring opening and closed ring), and can also interact with dihydroxy carbohydrates or polymers containing multiple side -OH chains to form reversible covalent bonds (Scheme S1)(Yang, Lee et al. 2006, Deng, Attalla et al. 2018).

Scheme S2. The formation of hydrogen bonds between PAA polymer chains at low pH condition.

Scheme S3. Schematic illustration showing how NCgel1 adsorbs heavy metal ions.

Figure S1. (a) A photograph of freeze-dried PAA-2APBA, showing a soft cotton-like structure; (b) The FTIR of PAA-2APBA: blue line is the precursor5; red line for precursor2. 5; black line for the precursor1. (c-f) 1H-NMR spectrum (400 MHz) of 2APBA-functionalized polyacrylic acid (PAA-2APBA) (7 mg·mL-1 in D2O). (c) 1H-NMR spectrum of precursor5, the integral analysis revealed that the grafting rate is 14%. Peak assignments: δ 7.48 (s, 1H), 7.33 (d, J = 44.9 Hz, 2H), 7.05 (s, 1H), 2.81 (s, 13H), 2.47 – 1.24 (m, 28H), 1.03 (td, J = 7.3, 0.7 Hz, 7H)；(d) 1H-NMR spectrum of precursor2.5, the integral analysis revealed that the grafting rate is 30%. Peak assignments: δ 7.49 (s, 1H), 7.28 (s, 2H), 7.03 (s, 1H), 2.81 (s, 4H), 1.90 (t, J = 109.0 Hz, 13H), 1.03 (t, J = 7.1 Hz, 2H). (e) 1H-NMR spectrum of precursor1, the integral analysis revealed that the grafting rate is 36%. Peak assignments: δ 7.47 (s, 1H), 7.26 (s, 3H), 7.03 (s, 1H), 2.80 (s, 5H), 1.82 (dt, J = 16.9, 6.6 Hz, 12H), 1.03 (t, J = 7.2 Hz, 3H); (f) Polyacrylic acid (PAA) purified after freeze-drying. The signal at δ ~ 2.9 is likely a side-product related to dimethylamino groups (from EDC) grafted to the backbone as a result of N-acyl transfer, a reaction that does not significantly affect the functional properties of the polymer product (Deng, Attalla et al. 2018).

1H-NMR and FTIR of PAA-2APBA

After freeze-drying, the synthesized PAA-2APBA exhibited a soft, flocculent structure (Figure S1a), and it was easy to dissolve in water. The FTIR spectra of PAA-2APBA analysis also indicated that 2APBA was grafted onto PAA via an amide bond (Figure S1b). As for precursor5 (blue line), the signal at 1635 cm-1 was assigned to the stretching vibration of C = O and amide band Ⅰ, the peak at 1558 cm-1 in the spectrum was assigned to the in-plane bending vibration of NH and amide band Ⅱ, and the signal at 1400 cm-1 was assigned to the stretching vibration of C-N and amide band Ⅲ. As for the precursor2.5 (red line) and precursor1 (black line), the signal at 1650 cm-1 was assigned to the stretching vibration of C = O and amide band Ⅰ, the peak at 1462 cm-1 in the spectrum was assigned to the skeleton vibration of substituted benzenes. In addition, 1H-NMR analysis indicated that 2APBA was successfully grafted onto the PAA polymer chain, and the integral analysis of PAA-2APBA conjugates revealed that the grafting rates of the precursors of precursor5, precursor2.5, and precursor1 were 14%, 30%, and 36%, respectively (Figure S1c-f). It is shown that the grafting rate of PAA-2APBA increases with the increase of the amount of 2APBA feed during the reaction.

Figure S2. Visual comparison of the hydrogel with laponite (left, cloudy) and the hydrogel without laponite (right, clear).

Figure S3. Shear storage modulus (G’) and loss modulus (G”) of hydrogels over a frequency sweep (0.5-2.2 Hz). (a) PAA-2APBA/PVA hydrogels; (b) PAA-2APBA/PVA+laponite nano-composite hydrogels.

G’ is substantially higher than G”, which indicates the hydrogels or nano-composite hydrogels behaved as gels.

Figure S4. Hydrogel's degradation tests and thermal stability test. (a) hydrogel degradation tests in PBS with different grafting rates of PAA-2APBA, and the effect of the presence or absence of laponite on hydrogel degradation; (b) thermogravimetric analysis curve of hydrogels and nanocomposite hydrogels; (c) degradation test of NCgel1 in glucose solution (0.5 mg/mL, left) and fructose solution (0.5 mg/mL, right). Ⅰ,0h; Ⅱ,1h; Ⅲ, 2h; Ⅳ 3h; Ⅴ 4h; Ⅵ 5h.

The PAA-2APBA/PVA hydrogels and nano-composite hydrogels were used for degradation experiments in vitro. The solution of the degradation test is the phosphate buffer saline (PBS) at pH 7.4. As shown in Figure S4a, the degradation rates of gel5, gel2.5 and gel1 (purple line, black line, and blue line) were decrease in order. After 24h, gel1 can still maintain 70% of the initial weight, while gel5 was almost completely degraded at about 4h, which indicated the stability of the hydrogel increases with the grafting rate of modified PAA. Nano-composite hydrogel exhibited higher stability (black line, blue line, and purple line), especially NCgel1 (gel1 + laponite) and NCgel2.5 (gel2.5 + laponite) which can maintain about 98% of the initial weight at 24 h. This is probably due to the laponite can play as the role of lapping and cross-linking, and inhibit the degradation of hydrogel to a certain extent (Gaharwar, Mukundan et al. 2014, Sharma, Dinda et al. 2016, Li, Liu et al. 2017), which is consistent with the results from the SEM observations. After placing NCgel1 for 120 h, it can still stably exist in the PBS buffer. What’s more, after NCgel1 and gel1 were respectively placed in PBS for 720 h (30 days), NCgel1 could still hold its integrity as compared with the totally degraded gel1 (Figure S4). In addition, the thermostability of the gel and the polymer was characterized by thermogravimetric analysis, in which the whole hydrogel withstands higher temperatures environments (Figure S4b). Under the premise of the same grafting rate, the hydrogel doped with laponite showed stronger thermal stability, and its degradation degree at high temperature was lower than the hydrogel without doped nanoparticles.

The borate bond-based self-healing hydrogels also possess glucose/fructose responsiveness (Kitano, Kataoka et al. 1991). As shown in Figure S4c, we studied the differential response function of the nanocomposite hydrogel in fructose and glucose solutions at the same concentration. During the experiment, the concentrations of glucose and fructose were both 0.5 mg/mL. In order to facilitate observation, the hydrogel was dyed blue by the methylene blue solution. The volume of the hydrogel was small at 0h, and the volume of the hydrogel gradually expands over time. In addition to the dissociation of the three-dimensional network during the competitive binding process, the hydrogel also swells when it absorbs water. In addition, as time goes by, the color of the solution darkens to varying degrees, which indicates that the hydrogel exhibits a significant difference in degradation, and the degradation rate of the hydrogel in the fructose solution is faster. In about 3 hours, the structure of the hydrogel in the fructose solution was loose, while the hydrogel in the glucose solution only swells in volume, and its structure is still relatively complete. At 6 hours, the hydrogel in both fructose and glucose solutions tended to dissociate. In general, the degradation rate of the hydrogel in the fructose solution is faster than that in the glucose solution. When glucose or fructose wereadded to a borate hydrogel-based system, glucose or fructose can interact with 2APBA against PVA competitively. Glucose or fructose has only one binding site, unlike PVA which can cross-link with PAA-2APBA polymer chains to form a three-dimensional structure (Springsteen and Wang 2002). This build-in property brings the nano-composite hydrogels to have potential application value in preparing glucose-responsive or fructose-responsive injectable drug carriers (Yang, Lee et al. 2006, Wang, Ma et al. 2010, Zhang, Guan et al. 2012, Guan and Zhang 2013).

Figure S5. The stability of NCgel1 and gel1 immersed in PBS for 720 h (30 days) at room temperature.

When the centrifuge tube was inverted, NCgel1 was still kept at the bottom stably, while only a small amount of gel1 remained at the bottom of the tube.

Figure S6. (a) The original methylene blue solution (left, at the bottom), and the solution after 24 hours of hydrogel adsorption (right, at the bottom); the hydrogel was centrifuged at 1500 rpm for 5 minutes. (b) The chemical formulas of methylene blue, malachite green, and hydrogel; (c) the effect of pH on the adsorption performance of hydrogel.

It can be clearly seen that the methylene blue in the solution is adsorbed into the hydrogel, and the remaining liquid is almost clear. Methylene blue and malachite green both possess positive charges, while hydrogels possess negative charges, and the two are more easily adsorbed together by electrostatic interaction.

When the pH of the dye solution is 3.0, the adsorption efficiency of NCgel1 is relatively poor, which is probably because the carboxyl group in PAA is protonated which shielded their interactions with the dye molecules.

Figure S7. NCgel1 immersed in the solution of CuSO4 (1mg/mL) for 1h (left) and 2h (right).

NCgel1 gradually turns blue due to the adsorption of copper ions.

Figure S8. Photograph of monolayer-cultured 293T cells (without hydrogel).

The fixed cells were stained with crystal violet, which showed that 293T is easy to reunite under normal culturing conditions.

Figure S9. Live/dead assay of 293T cells seeded in PAA-2APBA/PVA hydrogels (gel1) and PAA-2APBA/PVA + laponite hydrogels (NCgel1). Scale bar=50 μm. (a, d) photos of 293T cultured on a polystyrene well plate after 24 h (a) and 48 h (d) of seeding; (b, e) photos of 293T cultured in gel1 after 24 h (b) and 48 h (e) of seeding; (c, f) photos of 293T cultured in NCgel1 after 24 h (c) and 48 h (f) of seeding.

293T is an adherent cell, but the adherence is not strong, and it is easy to clump or suspend, causing cell death (Figure S7). Therefore, the control group of cells cultured in bare plate has a slightly higher mortality rate than cells cultured with hydrogel (Figure S8a and d). 293T cells have a good survival rate both in gel1 (Figure S8b and e) and NCgel1 (Figure S8c and f). The agglomeration of cells under a fluorescent microscope, which forms structure like spheroid, is mainly the result of the adhesion of cells together due to the presence of hydrogels.

Figure S10. Live/dead assay of HT22 cells seeded in PAA-2APBA/PVA hydrogels (gel1) and PAA-2APBA/PVA + laponite hydrogels (NCgel1). Scale bar=50 μm. (a, d) photos of HT22 cultured on a polystyrene well plate after 24 h (a) and 48 h (d) of seeding; (b, e) photos of HT22 cultured in gel1 after 24 h (b) and 48 h (e) of seeding; (c, f) photos of HT22 cultured in NCgel1 after 24 h (c) and 48 h (f) of seeding.

HT22 and 293T cells were used for testing the cell compatibility of hydrogels, and CA-PI was used to indicate the live and death of cells. HT22 cells adhered to the wall firmly and spread well. The cell survival rate of the HT22 cells was good in both the control and experimental groups (Figure S10). In the presence of hydrogels, some cells bind together to form spheroid-like structure. The results of HT22 cells also proved the good biocompatibility of the hydrogels no matter whether it contains laponite or not. Previous reports have confirmed that PAA hydrogels have good biocompatibility (de Lima, Elter et al. 2019), and the PBA-containing hydrogel can maintain good biocompatibility after being combined with other substances (Smithmyer, Deng et al. 2018). Laponite has also been proven to be with low toxicity (Gonzaga, Poli et al. 2019). Normally cultured 293T was easy to agglomerate (Figure S8), and the agglomeration was more obvious in the presence of hydrogel, but this does not affect the survival of cells (Figure S9). Accordingly, the hydrogels tested would have potential application value in the biomedical field, such as drug delivery(Brudno and Mooney 2015, Li and Mooney 2016), wound repair(Xue and Jackson 2015), cell culture scaffold(Feng, Liang et al. 2020, Qi, Zhang et al. 2020), similar as previously reported hydrogels.

References:

Brudno, Y. and D. J. Mooney (2015). "On-demand drug delivery from local depots." Journal of Controlled Release 219: 8-17.

de Lima, G. G., J. K. Elter, B. S. Chee, W. L. E. Magalhaes, D. M. Devine, M. J. D. Nugent and M. J. C. de Sa (2019). "A tough and novel dual-response PAA/P(NiPAAM-co-PEGDMA) IPN hydrogels with ceramics by photopolymerization for consolidation of bone fragments following fracture." Biomedical Materials 14(5).

Deng, X. D., R. Attalla, L. P. Sadowski, M. S. Chen, M. J. Majcheir, I. Urosev, D. C. Yin, P. R. Selvaganapathy, C. D. M. Filipe and T. Hoare (2018). "Autonomously Self-Adhesive Hydrogels as Building Blocks for Additive Manufacturing." Biomacromolecules 19(1): 62-70.

Feng, L., S. J. Liang, Y. Y. Zhou, Y. X. Luo, R. Y. Chen, Y. Y. Huang, Y. Q. Chen, M. G. Xu and R. Yao (2020). "Three-Dimensional Printing of Hydrogel Scaffolds with Hierarchical Structure for Scalable Stem Cell Culture." Acs Biomaterials Science & Engineering 6(5): 2995-3004.

Gaharwar, A. K., S. Mukundan, E. Karaca, A. Dolatshahi-Pirouz, A. Patel, K. Rangarajan, S. M. Mihaila, G. Iviglia, H. B. Zhang and A. Khademhosseini (2014). "Nanoclay-Enriched Poly(epsilon-caprolactone) Electrospun Scaffolds for Osteogenic Differentiation of Human Mesenchymal Stem Cells." Tissue Engineering Part A 20(15-16): 2088-2101.

Gonzaga, V. D. M., A. L. Poli, J. S. Gabriel, D. Y. Tezuka, T. A. Valdes, A. Leitao, C. F. Rodero, T. M. Bauab, M. Chorilli and C. C. Schnnitt (2019). "Chitosan-laponite nanocomposite scaffolds for wound dressing application." Journal of Biomedical Materials Research Part B-Applied Biomaterials.

Guan, Y. and Y. J. Zhang (2013). "Boronic acid-containing hydrogels: synthesis and their applications." Chemical Society Reviews 42(20): 8106-8121.

Kitano, S., K. Kataoka, Y. Koyama, T. Okano and Y. Sakurai (1991). "Glucose-Responsive Complex-Formation between Poly(Vinyl Alcohol) and Poly(N-Vinyl-2-Pyrrolidone) with Pendent Phenylboronic Acid Moieties." Makromolekulare Chemie-Rapid Communications 12(4): 227-233.

Li, J. Y. and D. J. Mooney (2016). "Designing hydrogels for controlled drug delivery." Nature Reviews Materials 1(12).

Li, T., Z. L. Liu, M. Xiao, Z. Z. Yang, Z. Y. Liu, X. J. Zhou and J. W. Wang (2017). "In vitro and in vivo studies of a gelatin/carboxymethyl chitosan/LAPONITE (R) composite scaffold for bone tissue engineering." Rsc Advances 7(85): 54100-54110.

Qi, X. L., M. Y. Zhang, T. Su, W. H. Pan, X. Q. Tong, Q. K. Zeng, W. Xiong, N. Jiang, Y. N. Qian, Z. P. Li, X. J. He, L. L. Shen, Z. G. Zhou and J. L. Shen (2020). "Biocompatible Hydrogels Based on Food Gums with Tunable Physicochemical Properties as Scaffolds for Cell Culture." Journal of Agricultural and Food Chemistry 68(12): 3770-3778.

Sharma, C., A. K. Dinda, P. D. Potdar, C. F. Chou and N. C. Mishra (2016). "Fabrication and characterization of novel nano-biocomposite scaffold of chitosan-gelatin-alginate-hydroxyapatite for bone tissue engineering." Materials Science & Engineering C-Materials for Biological Applications 64: 416-427.

Smithmyer, M. E., C. C. Deng, S. E. Cassel, P. J. LeValley, B. S. Sumerlin and A. M. Kloxin (2018). "Self-Healing Boronic Acid-Based Hydrogels for 3D Co-cultures." Acs Macro Letters 7(9): 1105-1110.

Springsteen, G. and B. H. Wang (2002). "A detailed examination of boronic acid-diol complexation." Tetrahedron 58(26): 5291-5300.

Wang, B. L., R. J. Ma, G. Liu, X. J. Liu, Y. H. Gao, J. Y. Shen, Y. L. An and L. Q. Shi (2010). "Effect of Coordination on the Glucose-Responsiveness of PEG-b-(PAA-co-PAAPBA) Micelles." Macromolecular Rapid Communications 31(18): 1628-1634.

Xue, M. L. and C. J. Jackson (2015). "Extracellular Matrix Reorganization During Wound Healing and Its Impact on Abnormal Scarring." Advances in Wound Care 4(3): 119-136.

Yang, X. P., M. C. Lee, F. Sartain, X. H. Pan and C. R. Lowe (2006). "Designed boronate ligands for glucose-selective holographic sensors." Chemistry-a European Journal 12(33): 8491-8497.

Zhang, X., Y. Guan and Y. J. Zhang (2012). "Ultrathin Hydrogel Films for Rapid Optical Biosensing." Biomacromolecules 13(1): 92-97.