Wearable pressure sensors based on carbonized graphene coated waste paper aerogel

Ang Li1,2, Ce Cui1,2, Weijie Wang1,2, Yue Zhang1,2, Jianyu Zhai1,2, Ronghui Guo1,2 ,  Shaojian Lin1,2, Wenfeng Qin3, Erhui Ren1,2, Hongyan Xiao1,2, Mi Zhou1, Jinwei Zhang1

- College of Biomass Science and Engineering, Sichuan University, Chengdu 610065, China

- Yibin Industrial Technology Research Institute of Sichuan University

- Aviation Engineering Institute, Civil Aviation Flight University of China, Guanghan, China

Table S1. Comparison of the sensitivity between C-GWA-based pressure sensor and other reported sensors based on 3D porous materials using graphene as a conductive filler.

| Active materials | Pressure regions (kPa) | Sensitivity (kPa-1) | Limit Detection (Pa) |
| --- | --- | --- | --- |
| rGO/PANI sponge(Ge et al. 2018) | 0-27 | 0.042-0.0152 | - |
| Graphene/CNTs sponge(Kuang et al. 2015) | 2-2.5 | 0.19 | 36 |
| rGO@PU/ANFS nanocomposites(Tang et al. 2019) | ＜40 40-58 | 1.06 2.28 | - |
| Cutting graphene aerogel(Yang et al. 2019) | 0-1.5 | 0.46 | 500 |
| rGO-PI foam(Yang et al. 2018) | 0.4 4-14 | 0.36 0.01 | - |
| Graphene-PU sponge(Yao et al. 2013) | 0-2 2-10 | 0.26 0.03 | 9 |
| AuNPs-GMC-PDMS film(Wang et al. 2020) | <1 1-10 10-50 | 5.37 1.56 0.5 | 4.4 |
| rGO-PANI sponge(Huang et al. 2019) | 0-6 >6 | 0.77 0.05 | - |
| Go-AgNF-PI sponge(Khan et al. 2018) | 0-10 | 0.572 | - |
| rGO@BC aerogel(Wei et al. 2021) | 0-0.16 0.16-2.54 2.54-22.2 | 0.87 13.89 2.71 | 47 |
| This work | 0-0.7 0.7-3.5 3.5-7 | 31.6 7.3 3.12 | 2.5 |

References

Ge G, Cai Y, Dong Q, Zhang Y, Shao J, Huang W, Dong X (2018) A flexible pressure sensor based on rGO/polyaniline wrapped sponge with tunable sensitivity for human motion detection. Nanoscale 10:10033-10040.

Huang J, Wang H, Li Z, Wu X, Wang J, Yang S (2019) Improvement of piezoresistive sensing behavior of graphene sponge by polyaniline nanoarrays. J Mater Chem C 7:7386-7394.

Khan FA, Ajmal CM, Bae S, Seo S, Moon H, Baik S (2018) Silver Nanoflower Decorated Graphene Oxide Sponges for Highly Sensitive Variable Stiffness Stress Sensors. Small 14:e1800549.

Kuang J, Dai Z, Liu L, Yang Z, Jin M, Zhang Z (2015) Synergistic effects from graphene and carbon nanotubes endow ordered hierarchical structure foams with a combination of compressibility, super-elasticity and stability and potential application as pressure sensors. Nanoscale 7:9252-9260.

Tang Y, Guo Q, Chen Z, Zhang X, Lu C (2019) In-situ reduction of graphene oxide-wrapped porous polyurethane scaffolds: Synergistic enhancement of mechanical properties and piezoresistivity. Compos Part A-appl S 116:106-113.

Wang J et al. (2020) Fabrication of a Sensitive Strain and Pressure Sensor from Gold Nanoparticle-Assembled 3D-Interconnected Graphene Microchannel-Embedded PDMS. ACS Appl Mater Interfaces.

Wei S, Qiu X, An J, Chen Z, Zhang X (2021) Highly sensitive, flexible, green synthesized graphene/biomass aerogels for pressure sensing application. Compos Sci Technol 207:108730-108737.

Yang C et al. (2019) Graphene Aerogel Broken to Fragments for a Piezoresistive Pressure Sensor with a Higher Sensitivity. ACS Appl Mater Interfaces 11:33165-33172.

Yang J, Ye Y, Li X, Lü X, Chen R (2018) Flexible, conductive, and highly pressure-sensitive graphene-polyimide foam for pressure sensor application. Compos Sci Technol 164:187-194.

Yao HB et al. (2013) A flexible and highly pressure-sensitive graphene-polyurethane sponge based on fractured microstructure design. Adv Mater 25:6692-6698.

Corresponding Author. Ronghui Guo, E-mail address:ronghuiguo214@126.com (R. H. Guo);

Shaojian Lin, E-mail address: linshaojian8866@163.com (S. J. Lin)