Supporting Information

Next-gen wearable energy harvester using PVDF-doped CuO composite nanofiber-based piezoelectric nanogenerators

Bindhu Amrutha 1,†, Ponnan Sathiyanathan 2, †, Mohammad Shamim Reza 3, Hongdoo Kim 3, Arun Anand Prabu 1,*

1 Department of Chemistry, School of Advanced Sciences, Vellore Institute of Technology, Vellore 632014, Tamil Nadu, India

2 Vel Tech Rangarajan Dr.Sagunthala R&D Institute of Science & Technology, Chennai, 600062, Tamil Nadu, India

3 Department of Materials Science and Engineering, College of Engineering, Kyung Hee University, Yongin-si, Gyeonggi-do – 17104, Republic of Korea

† These authors contributed equally to this work.

* Corresponding author E-mail: anandprabu@vit.ac.in

Fig. S1 a- f High-resolution 2-D AFM images of 0PCu, 1PCu, 3PCu, 5PCu, and 7PCu NFs. a’-f’ 3-D AFM images of corresponding NFs

Table S1: Fiber diameter distribution of neat and composite PVDF NFs.

| Sample code | Distribution of the fiber diameter (nm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Mean | Standard deviation | Min | Max |
| 0PCu | 365 | 105 | 179 | 689 |
| 1PCu | 310 | 86 | 144 | 666 |
| 3PCu | 300 | 80 | 184 | 540 |
| 5PCu | 289 | 72 | 162 | 454 |
| 7PCu | 210 | 48 | 139 | 386 |

Table S2: β-phase content of neat and composite PVDF NFs.

| Sample code | Absorption Intensity |  | F(β)% |
| --- | --- | --- | --- |
|  | Aα | Aβ |  |
| 0PCu | 0.0311 | 0.1545 | 79 |
| 1PCu | 0.0430 | 0.239 | 81 |
| 3PCu | 0.0291 | 0.1785 | 83 |
| 5PCu | 0.0261 | 0.2111 | 86 |
| 7PCu | 0.0193 | 0.1279 | 84 |

Table S3: Surface morphology (AFM) study of neat and composite PVDF NFs.

| # Sample code | # Ra (nm) | # Rq (nm) |
| --- | --- | --- |
| # 0PCu | # 170.0 | # 215.7 |
| # 1PCu | # 431.0 | # 542.0 |
| # 3PCu | # 510.0 | # 638.0 |
| # 5PCu | # 1161.0 | # 1499.0 |
| # 7PCu | # 568.0 | # 768.0 |