Supplementary Information of Direct thermal resistance measurement of a single ripplocation in graphite

Authors: Tianqi Bai1,2,†, Tao Zhang3,4,5,†, Songfeng Pei 6,7,†, Ruilin Mao2, Fachen Liu1,2, Jiade Li2, Ruochen Shi2, Jinlong Du2*, Lede Xian3,5,8*, Wencai Ren6,7*, Zhongfan Liu9,10, Peng Gao1,2,3,9,11,12*.

Affiliations:

1 Academy for Advanced Interdisciplinary Studies, Peking University, Beijing 100871, China.

2 International Center for Quantum Materials, and Electron Microscopy Laboratory, School of Physics, Peking University, Beijing 100871, China.

3 Tsientang Institute for Advanced Study, Zhejiang 310024, China.

4 Department of Materials Science and Engineering, City University of Hong Kong, Hong Kong 999077, China

5 Songshan Lake Materials Laboratory, Dongguan, Guangdong 523808, China.

6 Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang 110016, China.

7 School of Materials Science and Engineering, University of Science and Technology of China, Shenyang 110016, China.

8 Max Planck Institute for the Structure and Dynamics of Matter, Luruper Chaussee 149, 22761 Hamburg, Germany.

9 Beijing Graphene Institute, Beijing 100095, China.

10 National Laboratory for Molecular Sciences, College of Chemistry and Molecular Engineering, Peking University, Beijing 100871, China.

11 Interdisciplinary Institute of Light-Element Quantum Materials and Research Center for Light-Element Advanced Materials, Peking University, Beijing 100871, China.

12 Collaborative Innovation Center of Quantum Matter, Beijing 100871, China.

†These authors contributed equally to this work.

*Corresponding author.

Email: jldu@pku.edu.cn; lede.xian@mpsd.mpg.de; wcren@imr.ac.cn; pgao@pku.edu.cn.

Methods

Sample preparation

Natural graphite was oxidized to graphene oxide (GO) using H2SO4 and KMnO4. The GO was purified and homogenized to create a GO slurry consisting mostly most of single layers with diameter ranging from 5 μm to 10 μm by high pressure (50 MPa) homogenization for one hour. Utilizing the scanning centrifugal casting method, GO films were prepared [1]. The reduction process was carried out from room temperature to 300ºC of 1 ºC per minute to eliminate the majority of oxygen-containing groups. The defects were partially remedied through the graphitization process, involving high temperature annealing at 2600-3000 ºC for one hour, resulting in graphite films with in-plane thermal diffusivities ranging from 488 to 932 mm2 s-1.

Characterization

The HAADF images were recorded at 300 kV using an aberration-corrected FEI Titan Themis G2. The convergence semi-angle was 30 mrad, and the collection semi-angle range was 39–200 mrad for HAADF imaging. The STEM-EELS data was acquired on a Nion U-HERMES200 microscope equipped with both a monochromator and aberration correctors. The EELS datasets were acquired with 60 kV beam energy and 20&35 mrad convergence semi-angle and 25 mrad collection semi-angle. The typical energy resolution of acquired data under these conditions was 10-18 meV. Off-axis collection was used to enhanced signal due to extinction effect of the center gamma point [2]. In our experiments, we chose a uniform off-axis setting as shown in Fig. S6b-c, which ensures that more signals corresponding to certain energy are collected. The scanning step size in Fig. 2c is 1/7.5 and 1/10 nm, and the typical spatial resolution was ~0.3 nm. The typical dwell times of each pixel was 1600 ms. The scanning step size in Fig. 3 is 25 nm, and the typical dwell times of each pixel was 1200 ms.

The heating effect of the electron beam can be ignored because the beam current for measuring vibration signals is small and the sample conducts heat well. The temperature increment is roughly ΔT≃(Ib/eκ)(dE/dx), where Ib below 0.1 nA is the beam current after passing through the monochromator and κ ~100 W m-1 K-1 is sample’s thermal conductivity. The energy loss rate per electron dE/dx∼0.1 eV/nm. The estimated order of magnitude of ΔT is 0.1 mK, far below our current measurement accuracy.

The in-situ heating device consists of our homemade sample holder and current control system, which allows a constant current to be applied to the sample for local heating. The typical value of the total resistance of the heating circuit in the experiment is about 3 kΩ. After a long enough time of applying a current (generally 1~2 hours), the sample becomes stable in the field of view without drifting, and the temperature distribution on the sample no longer changes with time. In this case, steady-state thermal transport is achieved, i.e., there is a stable temperature gradient on the sample. Then, the STEM-EELS mapping experiments were performed.

EELS Data processing

All the acquired vibrational spectra were processed by using the custom-written MATLAB code and Gatan Microscopy Suite. More specifically, the EEL spectra were firstly aligned. Subsequently, the 3D filtering (BM3D) algorithms were applied for removing the Gaussian noise [3]. The background arising from both the tail of the ZLP and the non-characteristic phonon losses was fitted by employing the modified Pearson-VII function with two fitting windows and then subtracted in order to obtain the vibrational signal [4]. The Lucy-Richardson algorithm was then employed to ameliorate the broadening effect induced by the finite energy resolution, taking the elastic ZLP as the point spread function. The spectra were summed along the direction parallel to the interface for obtaining line-scan data with a good signal-to-noise ratio. In addition, we employed a multi-Gaussian peak fitting method to extract the polariton peaks from the composed signal. The temperature map was obtained by fitting the EEG and EEL signals at each pixel. For the local temperature fitting, we followed the method in the Ref.46 (main text), and fitted the temperature T according to the relationship log(Iloss/Igain)=1kBTℏω. Using fitnlm function in MATLAB, we performed a linear fit through the origin on the experimental data based on the least-squares fitting, and obtain the slope 1kBT and error range.

Finite element method

Finite element analysis was performed using COMSOL Multiphysics software. Geometric models matching the EELS acquisition areas in Figs. 3c and 3e were constructed, with dimensions of 600 nm × 50 nm and 675 nm × 50 nm, respectively. The models incorporated the experimentally measured anisotropic thermal conductivity of the graphite film: κx​=1540 W m−1 K−1 (in-plane) and κy​=20 W m−1 K−1 (out-of-plane). RBs were treated as thermal boundaries, with heat flow between adjacent RBs constrained to follow the in-plane direction of the graphite layers. Boundary conditions were defined based on experimental temperature measurements: the left boundaries of both models were fixed at 884.79 K and 787.66 K, respectively. Thermal flux magnitudes of 3.54×1011 W m−2 and 1.90×1011 W m−2 were applied to ensure temperature gradients in pristine bulk regions matched experimental values. TBR values were assigned to RBs until simulated temperature drops across the adjacent RBs agreed with experimental results, thereby extracting the absolute TBR of the RBs.

DFT Parameters

The phonon properties were calculated using the first principle method implemented in the Vienna Ab-initio Simulation Package (VASP). The lattice constant of graphite was chosen to be 2.456 Å. The optimized interlayer separation was 3.458 Å. The local density approximation (LDA) was employed for the exchange-correlation functional [5]. Phonon band structures were computed using density functional perturbation theory (DFPT). A plane-wave cutoff energy of 550 eV and a Brillouin zone mesh density of 0.157 Å-1 were used. The forces and energy convergence thresholds were set as 0.001 eV/Å and 1 × 10−7 eV, respectively. During the structural optimization process, all systems were optimized with convergence criteria of 0.01 eV/Å for forces and 1× 10−5 eV for energy. The uniaxial strain effects were simulated by applying strains along both the zigzag and armchair directions.

MD Simulation Parameters

The structural deformation simulations were performed using the molecular dynamics (MD) method implemented in the Large-scale Atomistic/Molecular Massive Parallel Simulator (LAMMPS). A rectangular slab model with 15 layers of graphene in an AB-stacking pattern, was constructed to investigate the flexural behavior of multilayer graphene under compression. Periodic boundary conditions were applied in all directions. Interlayer and intralayer interactions were described using the Kolmogorov-Crespi (KC) interaction potential [6] and the Reactive Empirical Bond Order (REBO) Potential [7], respectively. The slab model was optimized first by minimization algorithm and the optimized box lengths are a = 425.837 Å, b = 2.467 Å and c =153.55 Å. To induce flexural deformation during compression, small opposing displacements were applied along the z-axis at 1/3 and 2/3 of the armchair direction (a-direction) across twenty cycles. In each cycle, 0.5 Å indentations were imposed on atoms within 2 Å of these two points, followed by structural relaxation and energy minimization. After completing the indentation cycles, the system automatically contracted by 0.5%. Subsequently, a new 0.5% uniaxial strain was applied along the x-axis, and the system evolved under the default microcanonical (NVE) ensemble, followed by energy minimization and global relaxation. The MD process was performed with a timestep of 1 fs for a total 5000 steps. Atomistic simulations and strain tensor analyses were visualized using the open-source software OVITO.

FIG. S1. Measured tensile strain at the ripplocation boundary (RB) is 3.86% higher than in strain-free regions.

FIG. S2. Structural evolution of RBs with bending angle θ in graphite films.​​ a–d, STEM-HAADF images at θ = 45° (a), 60° (b), 90° (c), and 116° (d) (scale bars: 2 nm). As the bending angle increases, the density of nanoscale pores rises, while the number of intact layers between adjacent pores decreases.​

FIG. S3. Strain-dependent phonon dispersion of graphite along high-symmetry directions (Γ–M–K–Γ).​​ ​(a) Armchair and ​(b) zigzag directions under ​0%​​ (black), ​​+1.5%​​ tensile (green), –1.5%​​ compressive (orange), ​​+3%​​ tensile (purple), and ​–3%​​ compressive (blue) uniaxial strain.

FIG. S4. ​Sample fabricated by focused ion beam (FIB) for thermal transport measurements. (a) Four-electrode chip configuration enabling programmable current pathway and ​localized Joule heating​ at designated terminals. (b) Directional heat transfer induced by current application (I=10 mA) to right-side electrodes. (c) Graphite film mechanically anchored​ by FIB-deposited amorphous carbon. Electrical connections between the sample corners and four electrodes were established using amorphous carbon, ensuring current continuity.

FIG. S5. Finite element model for quantifying TBR and equivalent length​ of RBs. (a) Model corresponding to ​an isolated ripplocation band​ (as in Fig. 3c). (​b) Model corresponding to ​two adjacent ripplocation bands​ (as in Fig. 3e).

​Temperature gradient across a ripplocation band​ is defined as:

∇T=∆TL=Tgreen-Tbluexgreen-xblue                       （1）

where Tgreen​ and Tblue​ are ​temperatures measured at positions 0.1 nm left of the RB's left boundary and 0.1 nm right of its right boundary, respectively; x denotes the spatial coordinate. TBR values were iteratively assigned to RBs until simulated temperature drops across the adjacent RBs agreed with experimental results, thereby extracting the absolute TBR of the individual RB.

The equivalent length (ELRB​)​​ quantifies the additional thermal path introduced by a single RB, calculated by:

ELRB=Tpurple-Tblue∇Tbulk                       （2）

Tblue​ and Tpurple​ are temperatures ​at left-side (0.1 nm inside defect-free region) and right-side (0.1 nm inside RB) boundaries​ of the RB (see markers); ∇Tbulk​ is the reference temperature gradient in pristine regions.

FIG. S6. Off-axis EELS configuration for momentum-resolved phonon spectroscopy in graphite. (a) Schematic illustrating the off-axis EELS geometry. (b) Phonon spectral intensity distribution in reciprocal space for graphite within specific energy windows by FRFPM, with dashed circle and solid circle represent the EELS entrance aperture before and after off-axis respectively.

Frequency resolved frozen phonon multislice method (FRFPM) proposed by Zeiger et al [8]. was performed to verify the off-axis direction. The graphite system was fully relaxed under NPT ensemble and then in NVE ensemble using AIREBO potential [7]. Subsequently, we employed a method similar to the hotspot thermostat [9] used in Zeiger et al.'s work [10] to generate a series of frequency-resolved atomic trajectories with a grid of Nbin = 50 peak frequencies from 1 THz to 50 THz in steps of 1.0 THz. The frozen phonon multislice calculations were performed using MD Frozen Phonon module embedded in abTEM package [11] with slice thickness of 0.2 nm. ​The dominant phonon energy intervals for heat transport are concentrated within 41-60 meV and 81-100 meV. Optimized signal acquisition of these specific phonon modes is achieved through the off-axis geometry illustrated in Fig. S6b and Fig. S6c, maximizing phonon spectral intensity collection efficiency.​

Table. S1. Strain-dependent energy shifts of ZA phonon modes under in-plane and out-of-plane strain fields (tensile and compressive strain compared to strain-free state).​​

| Strain magnitude Strain direction | 5% tensile strain | 5% compressive strain |
| --- | --- | --- |
| In-plane | 4.3 meV | -7.5 meV |
| Out-of-plane | -0.7 meV | 1.1 meV |

The out-of-plane tensile applied to graphite exerts a significantly weaker influence on phonon energy compared to equivalent in-plane strain. This effect was most evident at the 3.86% tensile strain​ localized at RBs (Fig. S1), justifying its deliberate exclusion from our analysis.​

References

[1]	Q. Wei et al., Adv. Mater. 32, 1907411 (2020).

[2]	A. Li, P. M. Zeiger, Z. He, M. Xu, S. J. Pennycook, J. Rusz, and W. Zhou, Phys. Rev. Lett. 133, 046101 (2024).

[3]	J. Zhou et al., Nature 570, 500 (2019).

[4]	B. D. Levin, K. Venkatraman, D. M. Haiber, K. March, and P. A. Crozier, Microscopy and Microanalysis 25, 674 (2019).

[5]	J. P. Perdew, K. Burke, and M. Ernzerhof, Phys. Rev. Lett. 77, 3865 (1996).

[6]	A. N. Kolmogorov and V. H. Crespi, Phys. Rev. B 71, 235415 (2005).

[7]	W. B. Donald, A. S. Olga, A. H. Judith, J. S. Steven, N. Boris, and B. S. Susan, J. Phys.: Condens. Matter 14, 783 (2002).

[8]	P. M. Zeiger and J. Rusz, Phys. Rev. Lett. 124, 025501 (2020).

[9]	R. Dettori, M. Ceriotti, J. Hunger, C. Melis, L. Colombo, and D. Donadio, Journal of Chemical Theory and Computation 13, 1284 (2017).

[10]	P. M. Zeiger and J. Rusz, Phys. Rev. B 104, 104301 (2021).

[11]	J. Madsen and T. Susi, Open Res Eur 1, 24 (2021).