Stabilizing Interfacial Structure of LiCoO2 with Ultrahigh Capacity and Prolonged Cyclability at 4.6V

Fig. S1. SEM images of (a) LCO and (b) LCO@LGPO.

Fig. S2. (a) The SEM image and corresponding (b) EDX mappings of LCO.

Fig. S3. The fitted equivalent circuit of Nyquist plots.

II

I

Fig. S4. Transmission electron microscope images of the LCO and LCO@LGPO coating layer, Fourier transform results and inverse Fourier transform results

(f)

(e)

(d)

(c)

(b)

(a)

Fig. S5. Electron Backscattering Diffraction (EBSD) metal element analysis of cross-sectional microstructures of post-cycling electrode slices of LCO-coated LGPO after 200 cycles, (a) C, (b)O, (c) F,(d) Al, (e) Fe,(f) Co.

Fig. S5. The whole spectra of LCO and LCO@LGPO probed by XPS depth profile.

Fig. S7. Diagram of crystal structure of (a) LCO and (b) LCO@LGPO.

Table S1. The doping concentration of Zr, P and Co in all samples obtained from ICP-MS.

| Samples | Mole ratio /% |  |  |
| --- | --- | --- | --- |
|  | Zr | P | Co |
| LCO@LGPO | 0.2415 | 0.1667 | 61.1645 |
| LCO | / | / | 62.2504 |

Table S2. Refined refinement lattice parameters of LCO@LGPO and LCO samples.

| Sample | a (Å) | c (Å) | c/a ratio | Refinement parameters |
| --- | --- | --- | --- | --- |
| LCO@LGPO | 2.8537 | 14.1851 | 4.9708 | Rp: 3.88%,Rwp:5.02% |
| LCO | 2.8556 | 14.2086 | 4.9757 | Rp: 4.04%,Rwp:5.52% |

Table S3. The mass and volume percentage of each element in the cross-section of LCO@LGPO cathode material.

| Element | Wt% | Wt% Sigma | At% |
| --- | --- | --- | --- |
| C | 23.98 | 0.14 | 40.18 |
| O | 11.92 | 0.06 | 14.99 |
| F | 1.81 | 0.04 | 1.92 |
| Al | 53.50 | 0.11 | 39.90 |
| Fe | 0.33 | 0.02 | 0.12 |
| Co | 8.46 | 0.06 | 2.89 |
| All | 100 |  | 100 |